| (a) | (b) |
| --- | --- |
| (c) | (d) |
| (e) |  |

Figure S1. SEM images of the photocatalyst: (a) COF-5; (b) TiO2; (c) AuNP; (d) TiO2@COF-5; (e) AuNP@COF-5

Figure S2. XPS spectra of COF-5

(b)

(a)

Figure S3. Photodegradation kinetic fitting (a) PFO and (b) PSO

Figure S4. Absorbance spectrums of each photocatalysts

Table S1. Elemental concentration of composite COF-5 by XPS analysis

| Atomic concentration (%) | AuNP@COF-5 | TiO2@COF-5 |
| --- | --- | --- |
|  | O 1s : 30.82 C 1s : 69.16 Au 4f : 0.01 | O 1s : 28.97 C 1s : 70.48 Ti 2p : 0.56 |

Table S2. Parameters of photodegradation kinetic models

| Photocatalysts | PFO | PSO | Bi-phasic |
| --- | --- | --- | --- |
| COF-5 | A = 0.52 k1= 0.42 R2= 0.76 | A = 0.56 k2= 1.18 R2= 0.88 | A1 = 0.38 kf= 1.82 A2 = 0.47 ks= 0.01 R2= 0.98 |
| TiO2 | A = 0.64 k1= 0.43 R2= 0.67 | A = 0.69 k2= 0.89 R2= 0.83 | A1 = 0.44 kf= 3.33 A2 = 0.56 ks= 0.01 R2= 0.99 |
| AuNP | A = 0.61 k1= 0.36 R2= 0.77 | A = 0.66 k2= 0.92 R2= 0.90 | A1 = 0.44 kf= 1.90 A2 = 0.56 ks= 0.01 R2= 0.98 |
| TiO2@COF-5 | A = 0.81 k1= 0.51 R2= 0.83 | A = 0.87 k2= 0.94 R2= 0.93 | A1 = 0.62 kf= 1.54 A2 = 0.38 ks= 0.03 R2= 0.98 |
| AuNP@COF-5 | A = 0.77 k1= 0.46 R2= 0.85 | A = 0.82 k2= 0.92 R2= 0.95 | A1 = 0.59 kf= 1.30 A2 = 0.41 ks= 0.02 R2= 0.98 |