Supporting Information

Liquid-mediated mechanosynthesis of Zn-BDC coordination polymers via water- and DMF-assisted ball milling

Shi-Qiang Wang,*a Shaza Darwish,b Fan Feng,a Shan Xu,a Kunli Goh,a Rong Wang,*a,c and Michael J. Zaworotko*b

aSingapore Membrane Technology Centre, Nanyang Environment and Water Research Institute, Nanyang Technological University, 1 Cleantech Loop, 637141, Singapore.

bBernal Institute, Department of Chemical Sciences, University of Limerick, Limerick V94 T9PX, Ireland.

cSchool of Civil and Environmental Engineering, Nanyang Technological University, Singapore, 639798, Singapore.

*E-mail: shiqiang.wang@ntu.edu.sg; rwang@ntu.edu.sg; xtal@ul.ie

Figure S1. PXRD patterns of the starting materials and products obtained by neat and water-assisted BM using Zn5(CO3)2(OH)6 and Na2BDC.

Figure S2. PXRD patterns of the starting materials and product obtained by DMF-assisted BM using Zn5(CO3)2(OH)6 and H2BDC.

.

Figure S3. PXRD patterns of the starting materials and product obtained by DMF/H2O-assisted BM using Zn5(CO3)2(OH)6 and H2BDC.

Figure S4. PXRD patterns of the experimental MOF-2 sample synthesized by rapid solution-mixing and the corresponding simulated pattern.

Table S1. Summary of reported Zn-BDC coordination polymers using DMF and/or water as the solvents.

| Zn-BDC systems | Year | refcode | SG | a/Å | b/Å | c/Å | α/º | β/º | γ/º | Z | V/Å3 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| [Zn(BDC)(H2O)]·DMF (MOF-2) 2D | 1998 | GECXUH | P21/n | 6.72 | 15.49 | 12.43 | 90 | 102.8 | 90 | 4 | 1261.0 |
|  | 2001 | GECXUH01 | P21/n | 6.73 | 15.52 | 12.45 | 90 | 102.8 | 90 | 4 | 1268.7 |
|  | 2005 | GECXUH02 | P21/n | 6.65 | 15.22 | 12.61 | 90 | 104.1 | 90 | 4 | 1237.7 |
|  | 2009 | GECXUH02 | P21/n | 6.72 | 15.48 | 12.44 | 90 | 102.8 | 90 | 4 | 1261.9 |
| [Zn4O(BDC)3] (MOF-5) 3D | 1999 | SAHYOQ | Fm-3m | 25.88 | 25.88 | 25.88 | 90 | 90 | 90 | 24 | 17343.6 |
| [Zn(BDC)(H2O)2]n 1D | 1999 | DIKQET | C2/c | 14.95 | 5.00 | 12.16 | 90 | 103.6 | 90 | 4 | 883.9 |
|  | 2001 | DIKQET01 | C2/c | 14.99 | 5.03 | 12.10 | 90 | 103.82 | 90 | 4 | 886.0 |
|  | 2002 | DIKQET02 | C2/c | 15.09 | 5.06 | 12.19 | 90 | 103.6 | 90 | 4 | 904.7 |
|  | 2003 | DIKQET03 | C2/c | 15.03 | 5.05 | 12.13 | 90 | 103.8 | 90 | 4 | 892.7 |
|  | 2016 | DIKQET04 | Cc | 14.99 | 5.04 | 12.11 | 90 | 103.8 | 90 | 4 | 888.5 |
| [Zn(BDC)(H2O)]n 3D | 2001 | IFABIA | C2/c | 17.98 | 6.35 | 7.26 | 90 | 91.5 | 90 | 4 | 828.6 |
|  | 2001 | IFABIA01 | C2/c | 17.98 | 6.36 | 7.26 | 90 | 91.5 | 90 | 4 | 829.4 |
|  | 2003 | IFABIA02 | Cc | 18.01 | 6.34 | 7.25 | 90 | 91.4 | 90 | 4 | 828.4 |
|  | 2015 | IFABIA03 | C2/c | 17.95 | 6.35 | 7.25 | 90 | 91.4 | 90 | 4 | 826.8 |
| [Zn3(BDC)3(H2O)2]·4DMF 2D | 2001 | IFACAT | P21/c | 13.06 | 9.66 | 18.46 | 90 | 106.9 | 90 | 2 | 2229.2 |
|  | 2006 | IFACAT01 | P21/c | 13.05 | 9.66 | 18.46 | 90 | 106.9 | 90 | 2 | 2224.9 |
|  | 2006 | IFACAT02 | P21/c | 12.97 | 9.76 | 18.34 | 90 | 108.7 | 90 | 2 | 2198.6 |
| [Zn(BDC)(DMF)]n 2D | 2005 | DAXNOG | C2/m | 11.14 | 14.02 | 7.99 | 90 | 106.3 | 90 | 4 | 1197.3 |
|  | 2006 | DAXNOG01 | P-1 | 7.99 | 8.96 | 9.06 | 103.2 | 100.7 | 99.8 | 2 | 603.9 |
|  | 2016 | DAXNOG02 | C2/m | 11.19 | 14.14 | 7.98 | 90 | 106.9 | 90 | 4 | 1197.3 |
|  | 2016 | DAXNOG03 | P21/c | 7.91 | 14.17 | 11.54 | 90 | 107.6 | 90 | 4 | 1107.6 |
| Zn5(OH)4(BDC)3·2DMF 3D | 2006 | REDROI | P21/c | 6.41 | 14.16 | 20.10 | 90 | 95.3 | 90 | 2 | 1815.5 |