Supplementary Materials

Unlocking Ghana’s Kaolin Potential: Enhancing the Adsorption Capacity of Kaolin through Acid Activation for Environmentally Friendly Remediation of Used Automotive Oil

Andrew Nyamful¹, Charles K. Klutse¹˒²*, Kwarteng Yamoah¹, Anita Asamoah¹˒³, Ebenezer A. Asare³, Wilfred S. Massiasta¹, Juliet Attah⁴, Latifa Mohammed⁵, Cynthia Laar⁶, Abu Yaya⁷, Andrews Danquah⁸, Joseph K. Adjei⁹, Isaac B. Kudu³, Samuel N. A. Nettey¹⁰, Samuel Amiteye¹⁰, Godwin Amenorpe¹⁰, Eric E. Bayari¹¹ and Nathaniel O. Boadi¹²

¹ Graduate School of Nuclear and Allied Sciences, University of Ghana, P. O. Box AE1, Atomic, Accra, Ghana

² Nuclear Power Institute, Ghana Atomic Energy Commission, Kwabenya, Accra, Ghana

³ Environmental Resource Research Centre, National Nuclear Research Institute, Ghana Atomic Energy Commission, P. O. Box LG80, Legon, Accra, Ghana

⁴ Nuclear and Analytical Chemistry Research Centre, National Nuclear Research Institute, Ghana Atomic Energy Commission, Ghana

⁵ Institute of Industrial Research, Council for Scientific and Industrial Research, P. O. Box LG576, Accra, Ghana

⁶ Water Resources Research Centre, National Nuclear Research Institute, Ghana Atomic Energy Commission, Ghana

⁷ Department of Materials Science and Engineering, University of Ghana, Legon, Accra, Ghana

⁸ Department of Molecular Biology and Biotechnology, School of Biological Sciences, University of Cape Coast, Ghana

⁹ Environmental Research Group, Department of Chemistry, University of Cape Coast, Ghana

¹⁰ Agriculture and Radiation Processing, School of Nuclear and Allied Sciences, University of Ghana, Ghana

¹¹ School of Physical Sciences, Department of Earth Science, P. O. Box 24, Navrongo, Upper East Region, Ghana

¹² Department of Chemistry, Kwame Nkrumah University of Science and Technology, Kumasi, Ghana

Corresponding author: cklutse@gmail.com; +233 (0)54 500 9068

SMF 1: Freundlich isotherm plots for Na and Pb adsorption using raw and acid-treated kaolin adsorbents; K0Na and K0Pb are for the raw kaolin used for the adsorption of Na and Pb while K3Na and K3Pb are for the 3-M acid-treated kaolin used for the adsorption of Na and Pb

SMT 1. Adsorption parameters for Freundlich model for the 3 M acid-treated kaolin and raw kaolin adsorbents, where Kf indicates adsorption capacity, n Freundlich exponent with its inverse being the surface heterogeneity factor reflecting adsorption intensity

| Adsorbents | Kf (L/mg) | n | R2 |
| --- | --- | --- | --- |
| K0Na | 6.68190043 | 1.56128025 | 0.9738 |
| K3Na | 13.6678436 | 1.88501414 | 0.9141 |
| K0Pb | 6.3664891 | 1.52788388 | 0.9828 |
| K3Pb | 17.6522472 | 2.1353833 | 0.8396 |

SMT 2. RL values for the Langmuir model or the 3 M acid-treated kaolin and raw kaolin adsorbents

| Concentration (mg/L) | RL Values |  |  |  |
| --- | --- | --- | --- | --- |
|  | K0Na | K0Pb | K3Na | K3Pb |
| 5 | 0.6581 | 0.6752 | 0.4747 | 0.4747 |
| 10 | 0.4904 | 0.5097 | 0.3589 | 0.3112 |
| 15 | 0.3909 | 0.4094 | 0.2718 | 0.2315 |
| 20 | 0.3249 | 0.3420 | 0.2187 | 0.1843 |
| 25 | 0.2780 | 0.2937 | 0.1830 | 0.1530 |
| 30 | 0.2429 | 0.2574 | 0.1573 | 0.1309 |
| 35 | 0.0279 | 0.2290 | 0.1379 | 0.1143 |
| 40 | 0.1940 | 0.2063 | 0.1228 | 0.1015 |