Supporting Material

D2O metabolic labeling combined with AuNPs@PVP/SA hydrogel-based SERS platform for rapid quantitative detection of active lactic acid bacteria

Shijie Liuab, Lijun Zhaoab, Yueyu Baic, Qian Dingab, Yangyang Maab*, Miaoyun Liab**, Dong Liangab, Yanxia Liuab, Haoyun Liab, Lingxia Sunab

a College of Food Science and Technology, Henan Agricultural University, Zhengzhou, 450002, P.R. China

b Sauce braised and prefabricated products modern production school enterprise research and development center, Henan Agricultural University, Zhengzhou, 450002, P.R. China

c Livestock Breeding Research Institute, Henan University, Zhengzhou, 450046, P.R. China

* Corresponding author. Tel.: 86-371-63558150; E-mail: qiyu17@163.com

** Corresponding author. Tel.: 86-371-63558150; E-mail: limy7476@126.com

Fig. S1 (A), PLSDA teo-dimensional diagram; (B), 5-fold cross-validation result chart; (C), 1000 replacement checks.

Table S1 Calculated enhancement factor of AuNPs@PVP/SA hydrogel

| SERS sensor | IRS (a.u.) | ISERS (a.u.) | EF |
| --- | --- | --- | --- |
| AuNPs@PVP/SA hydrogel | 80.99 | 181593.87 | 2.24×103 |

Note: CRS and CSERS ; IRS and ISERS were Raman spectral intensity values of D2O at 2438 cm-1 (O–D stretching vibration) before and after using AuNPs@PVP/SA hydrogel substrate, respectively.

## Table S2 Tentative attribution of average SERS spectra of two LAB collected based on this strategy

| L. plantarum HAY1 | P. pentosaceus HAZ1 | ## Tentative attribution |
| --- | --- | --- |
| 569 | 564 | carbohydrate |
| 784 | 784 | glycoside ring pattern of NAG and NAM |
| 1092 | 1092 | O=P-O stretching vibration of nucleic acid |
| 1317 | 1319 | amide III |
| 1441 | 1444 | bending vibration of CH2/CH3 |
| 1566 |  | amide Ⅱ |
| 1674 | 1677 | amide I |
| 1801 |  | C=O group stretching vibration |
| 1940 | 1935 | C=C=C triple bond vibration |
| 2040-2300 | 2040-2300 | C－D bond |
| 2922 | 2922 | C－H bond |

Table S3 Screening results of different characteristic peaks of SERS average fingerprints of two species LAB

| Variable range | Raman shift/cm-1 | Tentative attribution | VIP |
| --- | --- | --- | --- |
| X323~X329 | 1092 cm-1 | O=P-O stretching vibration of nucleic acid | 2.88 |
| X73~X82 | 564~569 cm-1 | carbohydrate | 1.94 |
| X173~X181 | 784 cm-1 | ## glycoside ring pattern of NAG and NAM | 1.22 |
| X683~X686 | 1801 cm-1 | C=O group stretching vibration | 0.91 |

Table S4 Digital quantitative model of active LAB based on D2O-probed Raman spectroscopy with AuNPs@PVP/SA hydrogel as substrate material

| Mixing ratio | Digital quantitative model |
| --- | --- |
| L. plantarum Y1:P. pentosaceus Z1=10:0 | y=13690.69x-8323.93, R2=0.99 |
| L. plantarum Y1:P. pentosaceus Z1=7:3 | y=12668.29x-9478.39, R2=0.99 |
| L. plantarum Y1:P. pentosaceus Z1=5:5 | y=14434.52x-10446.01, R2=0.99 |
| L. plantarum Y1:P. pentosaceus Z1=3:7 | y=10241.54x-7274.83, R2=0.99 |
| L. plantarum Y1:P. pentosaceus Z1=0:10 | y=845.23x-5470.96, R2=0.99 |

Table S5 Evaluation results of practical application of this strategy

| Samples | This method | Plate counting method | Accuracy（%） | RSD（%） |
| --- | --- | --- | --- | --- |
| LB liquid medium | (1.81±0.02)×106 | (1.84±0.04)×106 | 98.37 | 2.12 |
|  | (1.82±0.03)×104 | (1.83±0.02)×104 | 99.45 | 2.84 |
|  | (1.76±0.04)×102 | (1.79±0.03)×102 | 98.32 | 3.01 |
| MRS liquid medium | (1.87±0.03)×106 | (1.86±0.02)×106 | 100.54 | 2.21 |
|  | (1.86±0.03)×104 | (1.84±0.04)×104 | 101.09 | 2.64 |
|  | (1.74±0.05)×102 | (1.77±0.03)×102 | 98.31 | 3.15 |
| Yogurt | (1.80±0.03)×106 | (1.82±0.02)×106 | 98.90 | 2.31 |
|  | (1.79±0.04)×104 | (1.81±0.02)×104 | 98.90 | 2.45 |
|  | (1.84±0.02)×102 | (1.88±0.03)×102 | 97.87 | 3.18 |
| Sausage | (1.85±0.04)×106 | (1.89±0.03)×106 | 97.88 | 3.56 |
|  | (1.74±0.05)×104 | (1.79±0.02)×104 | 97.21 | 3.84 |
|  | (1.75±0.03)×102 | (1.80±0.03)×102 | 97.22 | 2.84 |