Supplementary information 
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Figure. S1. STEM images of AgCuCC catalyst and EDX mappings.
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AI-generated content may be incorrect.]Figure S2. PXRD spectra acquired at room temperature for Ag50Cu50CC 150.4 heated at: 400 °C for 40 min (a), 300 °C for 40 min (b) and as-synthesized (c), Carbon cloth (d).

[image: ][image: ]Figure S3. (a) Faradaic efficiency (FE%) of CO and (b) partial current density (J₍CO₎) at various applied potentials vs. RHE of AgCu/CC and AgCu/CC annealed at 300 °C.
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