Extended Data Table 1 Percentage of material Composition based on CE-5 sample analyzed by machine learning of XRD pattern and previously analyzed Apollo sample (Fig. 1a)

| Crystal | Composition | Percentage （wt%, CE-5） | Percentage （wt%, Apollo） |
| --- | --- | --- | --- |
| orthoproxyene | (Mg, Fe)SiO3 | 19.66 | 2.49 |
| augite | (Ca, Na)(Mg, Fe, Al, Ti)(Si, Al)2O6 | 15.08 |  |
| plagioclase | NaAlSi3O8-CaAl2Si2O8 | 8.75 | 35.59 |
| silica (amorphous) | SiO2 | 7.58 | 31.67 |
| pyroxene | (Mg, Fe, Ca, Al, Ti)SiO3 | 6.85 | - |
| troilite | FeS | 6.04 | - |
| olivine | (Mg, Fe)2SiO4 | 5.55 | 6.22 |
| pigoenite | (Ca, Mg, Fe)(Mg, Fe)Si2O6 | 5.17 | 10.06 |
| yeelimite | Ca3(AlO2)3SO4 | 3.89 | - |
| ilmenite | FeTiO3 | 3.51 | 4.09 |
| chromite | FeCr2O4 | 3.35 | 0.65 |
| whitelockite | Ca9(MgFe)(PO4)PO3OH | 3.05 | 0.42 |
| pyrite | FeS2 | 2.08 | - |
| rutile | TiO2 | 1.75 | - |
| hapkeite | Fe2Si | 1.65 | - |
| cristobalite | β-SiO2 | 1.46 | 0.50 |
| quartz | α-SiO2 | 1.37 | 0.35 |
| pyrrhotite | Fe1-xS (x = 0~0.2) | 1.27 | - |
| zeolite linde type L | Si36O72 | 1.20 | - |

Extended Data Figure 1 | Element components of a) CE-5 sample analyzed by machine learning of XRD pattern and b) previously analyzed Apollo sample (Fig. 1a).

Extended Data Table 2 Element components of CE-5 sample analyzed by machine learning of XRD pattern and previously analyzed Apollo sample (Fig. 1a)

| Element | Percentage (CE-5, %) | Percentage (Apollo, %) |
| --- | --- | --- |
| H | 0.66 | 0 |
| O | 60.07 | 60.82 |
| Na | 0.46 | 0.29 |
| Mg | 1.96 | 3.84 |
| Al | 6.19 | 10.66 |
| Si | 11.69 | 16.31 |
| P | 2.63 | 0 |
| S | 0.1 | 0 |
| K | 0 | 0.05 |
| Ca | 6.59 | 5.92 |
| Ti | 1.8 | 0.17 |
| Cr | 0.19 | 0 |
| Mn | 0 | 0.03 |
| Fe | 7.66 | 1.9 |

Extended Data Figure 2 | X-ray photoelectron spectroscopy (XPS) survey spectra of CE-5 sample, as C 1s peak at ~284.6 eV should be from the substrate, it was not be labeled.

Extended Data Figure 3 | High resolution XPS spectra of a) O 1s, b) Na 1s, c) Mg 1s, d) Al 2p, e) Si 2p, f) P 2p, g) S 2p, h) Ca 2p, i) Ti 2p, j) Cr 2p, and l) Fe 2p of CE-5 sample.

Extended Data Figure 4 | a) and b) Scanning electron microscopy (SEM) images of CE-5, c) energy dispersive X-ray spectroscopy (EDX) of selected area of CE-5 in (b), inset: element distribution, in which C element should be from the substrate.

Extended Data Figure 5 | SEM-EDX elemental distribution maps of a) the CE-5 sample with b) O, c) Si, d) Al, e) Fe 2p, f) Mg, g) Ti, h) Ca, and i) S.

Extended Data Figure 6 | a) Dark-field TEM image and b) EDX spectra of selected area of a).

Extended Data Table 3 Element components through distinct measuring technology

|  | XRD | SEM EDX | TEM EDX | XPS | ICP |
| --- | --- | --- | --- | --- | --- |
| H | 0.66 | 0a | 0 | 0 | 0 |
| O | 60.07 | 63.81 | 70.29 | 54.84 | 0 |
| Na | 0.46 | 0 | 0 | 0.54 | 1.61 |
| Mg | 1.96 | 2.95 | 5.38 | 1.46 | 10.33 |
| Al | 6.19 | 4.02 | 7.76 | 10.62 | 13.29 |
| Si | 11.69 | 10.99 | 10.13 | 17.33 | 0 |
| P | 2.63 | 0 | 0.29 | 1.55 | 0 |
| S | 0.1 | 0.27 | 0.36 | 0.97 | 0 |
| K | 0 | 0 | 0.13 | 0 | 0 |
| Ca | 6.59 | 2.41 | 1.08 | 5.64 | 24.26 |
| Ti | 1.8 | 0.8 | 0.17 | 1.86 | 7.49 |
| Cr | 0.19 | 0 | 0.03 | 0.23 | 0.43 |
| Fe | 7.66 | 14.75 | 4.39 | 4.98 | 42.59 |

athe number ‘0’ represents none of the certain element was detected through this technology.

Extended Data Figure 7 | The Brunauer-Emmett-Teller (BET) analysis. a) surface area measured from nitrogen adsorption-desorption isotherms, and b) the corresponding pore size distribution of CE-5 sample. The measured BET surface area of 2.78 m2/g.