Table 1. Chemical Composition (wt.%) of the Alloys

| Alloy designation | C | N | Cr | Ni | Si | Mn | Cu | P | S | Fe | Remark |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| HMBASE 26 | 0.44 | 0.017 | 3.60 | 0.35 | 0.40 | 24.10 | 0.31 | 0.022 | 0.002 | Bal. | Experimental |
| HMN015 | 0.38 | 0.15 | 3.50 | 0.48 | 0.37 | 23.9 | 0.39 | 0.011 | 0.006 | Bal. | Experimental |
| HMN015V | 0.48 | 0.13 | 3.60 | 0.50 | 0.38 | 24.8 | 0.32 | 0.012 | 0.001 | Bal. | Experimental |
| CF3 | 0.019 | 0.022 | 18.27 | 8.61 | 0.59 | 0.95 | 0.27 | 0.032 | 0.007 | Bal. | Commercial |

Table 2. Room- and Cryogenic-temperature (-196 ℃) Tensile and Charpy Impact Test Data of the Alloys

| Alloy designation | Mechanical property |  |  | Impact toughness | Remark |
| --- | --- | --- | --- | --- | --- |
|  | Yield strength (MPa at RT.) | Tensile strength (MPa at RT.) | Elongation (% at RT.) | Charpy v-notch impact energy (J/㎟ at -196 ℃) |  |
| HMBASE 26 | 279 | 646 | 58 | 163 | Experimental |
| HMN015 | 318 | 641 | 57 | 169 | Experimental |
| HMN015V | 394 | 717 | 48 | 114 | Experimental |
| CF3 | 213 | 506 | 63 | 167 | Commercial |

Table 3. Quantify the content of various phases from X-ray diffraction (XRD) testing

| Alloy designation | Test | α-ferrite (wt.%) | α´-martensite (wt.%) | ε-Martensite (wt.%) | γ-austenite (wt.%) |
| --- | --- | --- | --- | --- | --- |
| HMBASE 26 | before test | 0.00 | 0.00 | 0.00 | 100 |
|  | after tensile test | 0.00 | 0.8 | 2.9 | 96.3 |
| HMN015 | before test | 0.00 | 0.00 | 0.00 | 100 |
|  | after tensile test | 0.00 | 0.00 | 0.00 | 100 |
| HMN015V | before test | 0.00 | 0.00 | 0.00 | 100 |
|  | after tensile test | 0.00 | 0.00 | 0.00 | 100 |
| CF3 | before test | 23.4 | 0.00 | 0.00 | 76.6 |
|  | after tensile test | 23.4 | 60.5 | 0.6 | 15.5 |

Table 4. α´-martensite Content Calculated by the Equations 4 and 5 after the Measurement of α-ferrite Content Using the Feritscope before and

after the Room-temperature Tensile Test and Cryogenic-temperature Impact Test of the Alloys

| Alloy designation | Test | Ferritescope readings (α-ferrite, wt.%) | α´-martensite (wt.%) | Remark |
| --- | --- | --- | --- | --- |
| HMBASE 26 | before test | 0.00 | 0.00 | Experimental |
|  | after tensile test | 0.00 | 0.00 |  |
|  | after impact test | 0.17 | 0.29 |  |
| HMN015 | before test | 0.00 | 0.00 | Experimental |
|  | after tensile test | 0.00 | 0.00 |  |
|  | after impact test | 0.00 | 0.00 |  |
| HMN015V | before test | 0.00 | 0.00 | Experimental |
|  | after tensile test | 0.00 | 0.00 |  |
|  | after impact test | 0.00 | 0.00 |  |
| CF3 | before test | 4.30 | - | Commercial |
|  | after tensile test | 30.5 | 44.5 |  |
|  | after impact test | 38.4 | 58.0 |  |