Iron-modified calcinated coconut fiber biochar for simultaneous removal of copper and zinc: optimization, production cost assessment, and machine Learning modeling

Xuan Thanh Bui1·Khuat Thuy Trang1·Phacharapol Induvesa2·Nguyen Thuy Chung1*

1 Department of Environmental Science and Technology, School of Chemistry and Life Sciences, Hanoi University of Science and Technology, Hanoi, Vietnam.

2 Department of Environmental Science, Faculty of Science, Silpakorn University, Nakhon Pathom, Thailand.

* Corresponding author’s e-mail: chung.nguyenthuy@hust.edu.vn

TABLES

Table 1 Physicochemical characteristic of RBC and AcBC

| Material | SBET* (m2/g) |  | Smic** (m2/g) | Smic/SBET | Sext*** (m2/g) | Pore Diameter**** (nm) | pHpzc | Elemental contents (%) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  |  |  | C | O | Si | Al | Ca | K | Fe | Na | Cl | S |
| RBC | 5.06 |  | 1.82 | 0.36 | 3.22 | 53.05 | 7.10 | 40.22 | 37.00 | 10.09 | 8.09 | 3.92 | 0.67 | - | - | - | - |
| AcBC | 100.92 |  | - | - | 107.77 | 7.53 | 7.60 | 40.77 | 38.64 | 5.22 | 2.42 | 2.01 | 0.57 | 6.11 | 1.89 | 1.76 | 0.67 |

*BET experiments were conducted out gas temperature at 150 °C and measured using N2 adsorption with the Brunauer-Emmett-Teller (BET) method.

**Pore surface area calculated using the t plot method.

***External surface area calculated using the t plot method.

****Pore diameter calculated using D-H method.

Table 2 Characteristic parameters of monometallic system adsorption kinetic models

| Model | Parameter | Unit | RBC |  | AcBC |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Cu | Zn | Cu | Zn |
| Experiment result | Qe | mg/g | 13.16 | 8.73 | 16.96 | 12.02 |
| PFO | Qe,cal | mg/g | 12.21 | 7.75 | 14.87 | 10.18 |
|  | K1 | min⁻¹ | 0.02 | 0.02 | 0.27 | 0.24 |
|  | R2 | - | 0.8938 | 0.8922 | 0.9069 | 0.9036 |
| PSO | Qe,cal | mg/g | 13.01 | 8.35 | 15.38 | 10.56 |
|  | K2 | g·mg⁻¹·min⁻¹ | 0.002 | 0.003 | 0.02 | 0.03 |
|  | R2 | - | 0.9334 | 0.9479 | 0.9403 | 0.9380 |
| WM | kid | mg.g⁻¹min⁻⁰·⁵ | 3.46 | 2.09 | 9.52 | 6.14 |
|  | n | - | 0.19 | 0.20 | 0.08 | 0.09 |
|  | C | mg/g | 0.0000 | 0.0000 | 0.0000 | 0.0005 |
|  | R2 | - | 0.9623 | 0.9861 | 0.9911 | 0.9989 |
| Boyd | KB | min-1 | 0.0068 | 0.0056 | 0.0308 | 0.0236 |
|  | R2 | - | 0.9312 | 0.9273 | -0.0553 | -0.1363 |

Table 3 Characteristic parameters of simultaneous two-metal system adsorption kinetic models

| Model | Parameter | Unit | RBC |  | AcBC |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Cu | Zn | Cu | Zn |
| Experiment result | Qe | mg/g | 9.72 | 4.96 | 12.84 | 7.99 |
| PFO | Qe,cal | mg/g | 9.25 | 4.63 | 11.96 | 7.31 |
|  | K1 | min⁻¹ | 0.02 | 0.04 | 0.04 | 0.03 |
|  | R2 | - | 0.8814 | 0.8406 | 0.8145 | 0.8387 |
| PSO | Qe,cal | mg/g | 9.64 | 4.74 | 12.14 | 7.61 |
|  | K2 | g·mg⁻¹·min⁻¹ | 0.005 | 0.011 | 0.020 | 0.008 |
|  | R2 | - | 0.9303 | 0.9156 | 0.9264 | 0.9185 |
| WM | kid | mg.g⁻¹min⁻⁰·⁵ | 3.39 | 2.05 | 5.78 | 2.79 |
|  | n | - | 0.16 | 0.13 | 0.12 | 0.15 |
|  | C | mg/g | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
|  | R2 | - | 0.9574 | 0.9747 | 0.9689 | 0.9805 |
| Boyd | KB | min-1 | 0.0112 | 0.0150 | 0.0175 | 0.0103 |
|  | R2 | - | 0.9112 | 0.7377 | 0.8206 | 0.8416 |

Table 4 Characteristic parameters of monometallic system adsorption isotherm models

| Model | Parameter | Unit | RBC |  | AcBC |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Cu | Zn | Cu | Zn |
| Langmuir | Qe,cal | mg/g | 16.77 | 15.18 | 34.75 | 29.69 |
|  | KL | L/mg | 0.21 | 0.14 | 0.17 | 0.05 |
|  | R2 | - | 0.9461 | 0.9022 | 0.8119 | 0.8805 |
|  | RL(C = 5 mg/L) | - | 0.45 | 0.57 | 0.67 | 0.90 |
|  | RL(C = 100 mg/L) | - | 0.04 | 0.07 | 0.09 | 0.32 |
| Freundlich | Kf | (mg/g)(L/mg)1n | 5.51 | 3.95 | 11.29 | 4.40 |
|  | n | - | 3.93 | 3.34 | 3.81 | 2.54 |
|  | R2 | - | 0.8592 | 0.8507 | 0.9445 | 0.9739 |
| Temkin | A | l/g | 3.35 | 1.76 | 77.41 | 5.99 |
|  | B | - | 2.97 | 2.91 | 3.56 | 3.44 |
|  | R2 | - | 0.9141 | 0.8932 | 0.8507 | 0.8932 |
| D-R | QS | mg/g | 15.04 | 12.65 | 30.24 | 21.71 |
|  | Kdr | mol2/Kj2 | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
|  | R2 | - | 0.8313 | 0.7631 | 0.7012 | 0.6884 |

Table 5 Characteristic parameters of simultaneous two-metal system adsorption isotherm models

| Model | Parameter | Unit | RBC |  | AcBC |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Cu | Zn | Cu | Zn |
| Langmuir | Qe,cal | mg/g | 15.18 | 19.22 | 29.69 | 21.59 |
|  | KL | L/mg | 0.13 | 0.05 | 0.05 | 0.26 |
|  | R2 | - | 0.9022 | 0.5940 | 0.8805 | 0.6371 |
|  | RL(C = 5 mg/L) | - | 0.088 | 0.80 | 0.41 | 0.72 |
|  | RL(C = 100 mg/L) | - | 0.01 | 0.19 | 0.05 | 0.13 |
| Freundlich | Kf | (mg/g)(L/mg)1n | 3.95 | 4.32 | 4.40 | 11.00 |
|  | n | - | 3.34 | 3.45 | 2.54 | 6.91 |
|  | R2 | - | 0.8507 | 0.7983 | 0.9739 | 0.7200 |
| Temkin | A | l/g | 1.76 | 16.03 | 5.99 | 2171.73 |
|  | B | - | 2.91 | 1.95 | 3.44 | 1.63 |
|  | R2 | - | 0.8932 | 0.6520 | 0.8293 | 0.6801 |
| D-R | QS | mg/g | 12.65 | 13.62 | 18.88 | 19.75 |
|  | Kdr | mol2/Kj2 | 0.0000 | 0.0000 | 0.0000 | 0.0000 |
|  | R2 | - | 0.7631 | 0.2978 | 0.6084 | 0.6578 |

Table 6 Performance metrics of machine learning models for predicting adsorption capacity

| Model | R2 train | Root mean squared error (train) | Mean squared error (train) | R2 test | Root mean squared error (test) | Mean Squared Error (test) |
| --- | --- | --- | --- | --- | --- | --- |
| X | 0.9998 | 0.0016 | 0 | 0.9263 | 0.059 | 0.0034 |
| E | 1 | 0 | 0 | 0.9176 | 0.0624 | 0.0038 |
| G | 0.993 | 0.0137 | 0.0001 | 0.9165 | 0.0628 | 0.0039 |
| R | 0.9884 | 0.0177 | 0.0003 | 0.8951 | 0.0704 | 0.0049 |
| CAT | 0.9959 | 0.0053 | 0 | 0.8726 | 0.0776 | 0.006 |
| LGB | 0.6596 | 0.0963 | 0.0092 | 0.5635 | 0.1436 | 0.0206 |

Table 7 Estimation of AcBC Production Cost

| Process stage | Operation step | Cost estimation method | Cost (USD/Kg) |
| --- | --- | --- | --- |
| Raw material preparation | Collection of raw material | Free collection of coconut fiber from local farms | 0 |
|  | Natural drying | Air drying | 0 |
|  | Labor cost for material preparation (sieving, preliminary washing, and drying) | Labor rate (USD/h) × time (h): 0.5 × 1.0 | 0.5 |
| RBC production | Pyrolysis of coconut fiber | Furnace power (kW) × operation time (h) × electricity cost (USD/kWh): 2.0 × 1.0 × 0.08 | 0.16 |
|  | Washing | Laboratory water and electricity cost for producing distilled water: 5.0 L DI water/kg biochar | 0.8 |
|  | Drying | Oven power (kW) × operation time (h) × electricity cost (USD/kWh): 1.2 × 4.0 × 0.08 | 0.38 |
|  | Labor cost | Labor rate (USD/h) × time (h): 0.5 × 1.0 | 0.5 |
| Modification (AcBC production) | FeCl₃·6H₂O | 0,164 g × 10 USD/kg | 1.64 |
|  | FeSO₄·7H₂O | 0,336 g × 4 USD/kg | 1.34 |
|  | Magnetic stirring (24h) | Stirrer power (kW) × operation time (h) × electricity cost (USD/kWh): 0.06 × 24 × 0.08 | 1.15 |
|  | Drying | Oven power (kW) × operation time (h) × electricity cost (USD/kWh): 1.2 × 4.0 × 0.08 | 0.38 |
| Subtotal (RBC production) |  |  | 2.34 |
| Subtotal (AcBC production) |  |  | 6.85 |
| Overhead cost |  | 10% of base cost | 0.83 |
| Total estimated cost |  |  | 7.54 |

Table 8 Comparison of Treatment Efficiency and Production Cost between RBC and AcBC

| Material | C₀ (mg/L) | S/L ratio (g/L) | Efficiency Cu/Zn | Ce(mg/L, Cu/Zn) | Time (mins) | Column A QCVN 40 | Cost (USD/m³) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| AcBC | 5 | 1 | 90% / 89% | 0.5 / 0.6 | 5 (Cu)-30 (Zn) | approved | 7.5 |
| RBC |  | 1 | 89% / not approved | 0.3 | 480 | approved (Cu) | 3.2 |
| AcBC | 20 | 2 (Cu) – 2.5 (Zn) | 96% / 95% | 0.5 / 0.5 | 120 | approved | 15 – 18.75 |
| RBC |  | 5 (Cu) – 5.5 (Zn) | 96% / 95% | 0.7 / 0.5 | 240 | approved | 16 – 17.6 |

Table 9 Comparison of the Qe with  other magnetic biochar

| Reference | Biomass origin | Modification precusor | Contaminant | Qe (mg/g) |
| --- | --- | --- | --- | --- |
| [36] | Straw | FeSO4⋅7H2O, FeCl3⋅6H2O, NaOH | Cu2+ | 149.2 |
| [62] | Commercial biochar | FeSO4·7H2O, NaBH4 |  | 66.16 |
| [63] | Kelp | FeCl3 |  | 55.86 |
|  | Hijikia | FeCl3 |  | 47.75 |
| [34] | Pinecone | FeSO4.7H2O, MnSO4, NaOH |  | 13.4 |
|  | White popinac |  |  | 10.4 |
|  | Sugarcane bagasse |  |  | 19.8 |
| RBC | Coconut fiber | FeSO4⋅7H2O, FeCl3⋅6H2O, NaOH |  | 16.77 |
| AcBC |  |  |  | 34.75 |
| [63] | Kelp | FeCl3 | Zn2+ | 22.22 |
|  | Hijikia | FeCl3 |  | 19.13 |
| [64] | Empty fruit branch | FeCl3 |  | 1.18 |
| RBC | Coconut fiber | FeSO4⋅7H2O, FeCl3⋅6H2O, NaOH |  | 15.18 |
| AcBC |  |  |  | 29.69 |