Table 1: Energy gap between the lowest excited singlet and lowest excited triplet states (∆Est), spin-orbit coupling matrix element (SOCME), reorganization energy (λrISC), rISC rates (KrISC), activation energy (∆G), the change in torsion angle (△Θs1) as the molecule transitions from S0 geometry to S1 geometry, and the change in torsion angle (△Θt1) as the molecule transitions from S0 geometry to T1 geometry of CMAs at 298.15K

| Molecule | △Est (eV) | SOCME (S1-T1) (cm-1) | λrISC (eV) | ∆G (eV) | △Θs1 (degrees) | △Θt1 (degrees) | KrISC (s-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CMA1 | 0.14 | 7.45 | 0.17 | 0.14 | +88.1 | -31.3 | 1.42x108 |
| CMA2 | 0.25 | 4.40 | 0.03 | 0.65 | -17.5 | -20.8 | 2.61x10-1 |
| CMA3 | 0.28 | 2.24 | 0.38 | 0.29 | -20.6 | +0.5 | 3.01x104 |
| CMA4 | 0.28 | 0.97 | 0.21 | 0.29 | -23.5 | +1.8 | 7.81x103 |
| CMA5 | - | 3.48 | - | - | -16.2 | - | - |