# Gold-Decorated Carbon Dots Carrying Doxorubicin Enhance Selectivity in A549 Lung Cancer Cells Through Nucleus Targeting and Improved Loading

# Supplementary Materials

Iroda Saydullaeva1,2, Serdar Özçelik2,*

1 Engineering Physics Institute, Samarkand State University, Samarkand, Uzbekistan

2 Department of Chemistry, Izmir Institute of Technology, Urla-Izmir 35430, Türkiye

* Corresponding author. E-mail: serdarozcelik@iyte.edu.tr or iroda_55@hotmail.com

Figure S1. Optical properties of doxorubicin. (a) UV-Vis absorption spectrum showing maximum absorbance at ~480 nm. (b) Photoluminescence emission spectrum with peak intensity at ~590 nm. Data used for quantification of doxorubicin conjugation to nanoparticles.

Figure S2. Comprehensive spectroscopic characterization of gel chromatography fractions. (a,c) UV–Vis absorption spectra and (b, d) photoluminescence (PL) emission spectra of all collected fractions obtained after purification of DOX@C-dot (a, b) and DOX@AuNP@C-dot (c, d) conjugates. The spectral profile of free DOX solution is included for comparison, confirming the successful conjugation of DOX to C-dots.

Table 1: Quantitative Analysis of Doxorubicin Loading onto Carbon Dots across Various Sample Fractions.

| Sample | A350 | A480 | C-dot (mg/L) | DOX (mg/L) | Mass | Mass DOX (µg) | DLE (%) | C-dot/Dox ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | C-dot (µg) |  |  |  |
| F.1 | 0.05 | 0.01 | 0.01 | 0 | 3.5 | 0.93 | 21 | 3.76 |
| F.2 | 0.73 | 0.13 | 0.05 | 0.01 | 52.44 | 11.65 | 18.2 | 4.5 |
| F.3 | 2.35 | 0.29 | 0.17 | 0.03 | 169.02 | 25.13 | 12.9 | 6.73 |
| F.4 | 2.65 | 0.25 | 0.19 | 0.02 | 190 | 21.65 | 10.2 | 8.78 |
| F.5 | 2.63 | 0.21 | 0.19 | 0.02 | 188.77 | 18.09 | 8.7 | 10.44 |
| F.6 | 2.25 | 0.17 | 0.16 | 0.02 | 161.68 | 14.78 | 8.4 | 10.94 |
| F.7 | 2.44 | 0.25 | 0.18 | 0.02 | 175.34 | 21.63 | 11 | 8.11 |
| F.8 | 2.22 | 0.21 | 0.16 | 0.02 | 159.26 | 18.63 | 10.5 | 8.55 |
| F.9 | 1.59 | 0.17 | 0.11 | 0.02 | 114.01 | 14.79 | 11.5 | 7.71 |
| F.10 | 1.36 | 0.15 | 0.1 | 0.01 | 97.94 | 12.73 | 11.5 | 7.7 |
| F.11 | 1.69 | 0.12 | 0.12 | 0.01 | 120.94 | 10.35 | 7.9 | 11.68 |
| F.12 | 2.15 | 0.13 | 0.16 | 0.01 | 154.52 | 10.87 | 6.6 | 14.22 |
| F.13 | 2.2 | 0.1 | 0.16 | 0.01 | 157.9 | 8.96 | 5.4 | 17.63 |
| F.14 | 1.84 | 0.09 | 0.13 | 0.01 | 132.32 | 8.1 | 5.8 | 16.33 |
| F.15 | 1.38 | 0.08 | 0.1 | 0.01 | 99.06 | 6.95 | 6.6 | 14.26 |
| F.16 | 3.05 | 3.25 | 0.22 | 0.28 | 218.56 | 282.61 | 56.4 | 0.77 |
| DOX | 0 | 0.54 | 0 | 0.05 | 0 | 46.87 | 99.9 | 0 |

Table 2: Molar Ratio Analysis of DOX Molecules per C-dot Particle across Various Sample Fractions.

| Sample | Mass C-dot (µg) | Mass DOX (µg) | Mass Ratio (C-dot /DOX) | DLE (%) | Moles C-dot (pmol) | Moles DOX (nmol) | Molar Ratio (DOX/C-dot) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| F.1 | 3.50 | 0.93 | 3.76 | 21.00 | 37.07 | 1.71 | 46.2 |
| F.2 | 52.44 | 11.65 | 4.50 | 18.20 | 555.34 | 21.43 | 38.6 |
| F.3 | 169.02 | 25.13 | 6.73 | 12.90 | 1789.94 | 46.24 | 25.8 |
| F.4 | 190.00 | 21.65 | 8.78 | 10.20 | 2012.12 | 39.83 | 19.8 |
| F.5 | 188.77 | 18.09 | 10.44 | 8.70 | 1999.09 | 33.28 | 16.6 |
| F.6 | 161.68 | 14.78 | 10.94 | 8.40 | 1712.21 | 27.19 | 15.9 |
| F.7 | 175.34 | 21.63 | 8.11 | 11.00 | 1856.87 | 39.80 | 21.4 |
| F.8 | 159.26 | 18.63 | 8.55 | 10.50 | 1686.58 | 34.28 | 20.3 |
| F.9 | 114.01 | 14.79 | 7.71 | 11.50 | 1207.38 | 27.21 | 22.5 |
| F.10 | 97.94 | 12.73 | 7.70 | 11.50 | 1037.19 | 23.42 | 22.6 |
| F.11 | 120.94 | 10.35 | 11.68 | 7.90 | 1280.77 | 19.04 | 14.9 |
| F.12 | 154.52 | 10.87 | 14.22 | 6.60 | 1636.38 | 20.00 | 12.2 |
| F.13 | 157.90 | 8.96 | 17.63 | 5.40 | 1672.18 | 16.49 | 9.9 |
| F.14 | 132.32 | 8.10 | 16.33 | 5.80 | 1401.28 | 14.90 | 10.6 |
| F.15 | 99.06 | 6.95 | 14.26 | 6.60 | 1049.06 | 12.79 | 12.2 |
| F.16 | 218.56 | 282.61 | 0.77 | 56.40 | 2314.57 | 519.96 | 224.6 |

Table 3: Absorbance Data and Calculated DLE for DOX@AuNP@C-dot Fractions

| Sample | A350 | A480 | AuNP@C-dot (mg/L) | Dox (mg/L) | Mass AuNP@C-dot (µg) | Mass Dox (µg) | DLE (%) | AuNP@C-dot/Dox ratio |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| F.1 | 0.04 | 0.01 | 0.01 | 0 | 2.98 | 0.92 | 23.57 | 3.24 |
| F.2 | 1.64 | 0.29 | 0.12 | 0.03 | 118 | 25.08 | 17.53 | 4.71 |
| F.3 | 3.24 | 2.45 | 0.23 | 0.21 | 232.21 | 213.37 | 47.89 | 1.09 |
| F.4 | 3.28 | 3.3 | 0.24 | 0.29 | 235.59 | 286.78 | 54.9 | 0.82 |
| F.5 | 3.12 | 3.14 | 0.22 | 0.27 | 223.97 | 272.9 | 54.92 | 0.82 |
| F.6 | 3.01 | 0.55 | 0.22 | 0.05 | 216.22 | 47.98 | 18.16 | 4.51 |
| F.7 | 2.4 | 0.24 | 0.17 | 0.02 | 172.52 | 21.04 | 10.87 | 8.2 |
| F.8 | 2.17 | 0.22 | 0.16 | 0.02 | 155.61 | 19.34 | 11.06 | 8.05 |
| F.9 | 2.13 | 0.22 | 0.15 | 0.02 | 152.8 | 19.32 | 11.23 | 7.91 |
| F.10 | 2.05 | 0.21 | 0.15 | 0.02 | 147.41 | 18.63 | 11.22 | 7.91 |
| F.11 | 2.06 | 0.2 | 0.15 | 0.02 | 148.01 | 17.35 | 10.49 | 8.53 |
| F.12 | 2.07 | 0.19 | 0.15 | 0.02 | 148.42 | 16.54 | 10.03 | 8.98 |
| F.13 | 1.84 | 0.19 | 0.13 | 0.02 | 132.27 | 16.16 | 10.89 | 8.19 |
| F.14 | 1.67 | 0.16 | 0.12 | 0.01 | 120.08 | 14.13 | 10.53 | 8.5 |
| F.15 | 1.38 | 0.16 | 0.1 | 0.01 | 99.38 | 13.46 | 11.93 | 7.38 |
| F.16 | 0.75 | 0.11 | 0.05 | 0.01 | 54.15 | 9.75 | 15.26 | 5.55 |

Table 4: Molar Ratio Analysis of DOX Molecules per C-dot Particle across Various Sample Fractions.

| Sample | Mass AuNP@ C-dot (µg) | Mass DOX (µg) | Mass Ratio | DLE (%) | Moles AuNP@C-dot (pmol) | Moles DOX (nmol) | Molar Ratio (DOX/ particle) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| No-1 | 2.98 | 0.92 | 3.24 | 23.57 | 30.38 | 1.69 | 55.6 |
| No-2 | 118.00 | 25.08 | 4.71 | 17.53 | 1204.00 | 46.14 | 38.3 |
| No-3 | 232.21 | 213.37 | 1.09 | 47.89 | 2369.27 | 392.57 | 165.7 |
| No-4 | 235.59 | 286.78 | 0.82 | 54.90 | 2403.74 | 527.64 | 219.5 |
| No-5 | 223.97 | 272.90 | 0.82 | 54.92 | 2285.20 | 502.09 | 219.7 |
| No-6 | 216.22 | 47.98 | 4.51 | 18.16 | 2206.15 | 88.28 | 40.0 |
| No-7 | 172.52 | 21.04 | 8.20 | 10.87 | 1760.27 | 38.71 | 22.0 |
| No-8 | 155.61 | 19.34 | 8.04 | 11.06 | 1587.68 | 35.59 | 22.4 |
| No-9 | 152.80 | 19.32 | 7.91 | 11.23 | 1559.04 | 35.55 | 22.8 |
| No-10 | 147.41 | 18.63 | 7.91 | 11.22 | 1504.04 | 34.27 | 22.8 |
| No-11 | 148.01 | 17.35 | 8.53 | 10.49 | 1510.22 | 31.92 | 21.1 |
| No-12 | 148.42 | 16.54 | 8.97 | 10.03 | 1514.37 | 30.43 | 20.1 |
| No-13 | 132.27 | 16.16 | 8.19 | 10.89 | 1349.60 | 29.73 | 22.0 |
| No-14 | 120.08 | 14.13 | 8.50 | 10.52 | 1225.24 | 25.99 | 21.2 |
| No-15 | 99.38 | 13.46 | 7.38 | 11.93 | 1014.02 | 24.76 | 24.4 |
| No-16 | 54.15 | 9.75 | 5.55 | 15.26 | 552.47 | 17.94 | 32.5 |

## STEP-BY-STEP DLE CALCULATION

For pooled active fractions F7–F10 of DOX@AuNP@C-dot:

Step 1 — Sum DOX mass across fractions: 21.04 + 19.34 + 19.32 + 18.63 = 78.33 µg

Step 2 — Sum AuNP@C-dot mass across fractions: 172.52 + 155.61 + 152.80 + 147.41 = 628.34 µg

Step 3 — Apply DLE formula: DLE (%) = [mass DOX / (mass AuNP@C-dot + mass DOX)] × 100 = [78.33 / (628.34 + 78.33)] × 100 = [78.33 / 706.67] × 100 = 11.08%

For pooled active fractions F7–F10 of DOX@C-dot (for comparison):

Total DOX = 21.63 + 18.63 + 14.79 + 12.73 = 67.78 µg Total C-dot = 175.34 + 159.26 + 114.01 + 97.94 = 546.55 µg DLE = [67.78 / (546.55 + 67.78)] × 100 = 11.03%