Table 5. Effect of different variables and their interactions on internal fit (µm)
	Factor 
	Type III Sum 
of Squares 
	df
	Mean 
Square
	F
	P
	Partial Eta Square (95% CI)

	Sintering condition
	55993.06
	2
	27996.53
	226.34
	<.001*
	0.94 
(0.90-0.96)

	Measurement point
	312009.58
	3
	88891.62
	1016.80
	<.001*
	0.97 
(0.96-0.98)

	Sintering condition× Measurement point
	33141.67
	7
	4714.32
	54.00
	<.001*
	0.80 
(0.73-0.84)


95% CI, 95% confidence interval for mean; df: degree of freedom. *Statistically significant at P<.05.


