Table 1. Integrated mechanism-observable-method mapping for PBXs and solid propellants.

| Material problem and loading context | Dominant mechanism and target observable | Mechanism-compatible representation | Critical qualification |
| --- | --- | --- | --- |
| PBX mesoscale fracture | Interface debonding, binder-ligament failure and microcrack coalescence; local damage and specimen response. | CZM or DEM for distributed interface/contact damage; XFEM for a dominant crack after localisation [1,13,20,64]. | Separate interface and bulk failure parameters; validate local damage as well as global response. |
| PBX crack from a cavity or notch | Sharp crack initiation and propagation; crack path, failure load and growth history. | XFEM for one or a few dominant cracks; PFM or PD when distributed initiation and interacting topology must be represented [26,81]. | Use independently measured fracture properties and demonstrate mesh/internal-length sensitivity. |
| PBX impact, hot-spot formation and ignition | Mechanical damage or fracture; dissipative heating, temperature, reaction progress and ignition delay. | Coupled PD for distributed damage and thermo-chemical fields; DEM or an explicit mesoscale formulation when contact or friction is central [65,68]. | Mechanical agreement does not validate temperature or ignition; energy partition and local thermal validation are required. |
| Solid-propellant dewetting and rate-dependent failure | Viscoelastic interface separation, matrix deformation and distributed mesodamage. | Rate-/temperature-dependent CZM for represented interfaces; PFM for distributed matrix/fracture fields; DEM when explicit force networks are required [8,21,63]. | Calibrate across rate, temperature and loading mode; avoid fitting all parameters to one global curve. |
| Solid-propellant dominant or mixed-mode crack | Crack-tip blunting and mode-I/mixed-mode growth at specimen or grain scale. | XFEM or CZM for one or a few cracks; PD or PFM for non-prescribed interacting topology [16,66]. | Validate crack path and load response under withheld rates or mode mixities. |
| Crystal fracture or fracture-deflagration coupling | Anisotropic cleavage or co-evolution of damage, heat release and burning surface. | PFM or PD with anisotropic constitutive relations for crystal fracture; coupled multiphysics formulations for deflagration [67,69]. | Direct PBX crystal-fracture evidence and local thermochemical validation remain limited. |