Additional Data Figure legends.

Additional Data Figure 1. CO2 release from plastic (PET) bottle. (a) Used empty PET bottle (500 ml) was washed with fresh water, and CO2 concentration was measured after each washing. Before washing the empty bottle, the CO2 concentration was 2.8% (v/v). The unit of the vertical axis is ppm (a) CO2 is released at different periods and units of the vertical axis ppm. (b) The washed bottle was left at 20°C or 50°C, and CO2 concentration that was released into the glass bottle was measured at different periods. The left and right columns represent 50°C and 20°C experiments, respectively. The unit of the vertical axis is %(v/v), and the values are the mean of four experiments ± S.D. *: p < 0.05, **: p < 0.01.

Additional Data Figure 2. CO2 absorption and release from plastic bottles. After plastic bottles (250 ml) were filled with CO2 (left column) or carbonated beverage (right column) for 5 h at 20°C, they were washed three times with fresh water and then left in the room for 5 h. The released CO2 was measured directly using CO2 analyzers. HDPE; high-density polyethylene, LDPE; low-density polyethylene, PP; polypropylene, Teflon; tetrafluoro polyethylene, PC: polycarbonate, and PET: polyethylene terephthalate. In addition, b): the following materials were used: rubber I (1 × 100 × 100 mm), rubber II (3 × 100 × 199 mm), acrylic rods (3-mm diameter), polyethylene mesh (92-#18, 10 × 60 cm), nylon mesh (PA-2, 6 u, 10 × 600 cm), were used. These materials were inserted into the glass bottle and treated with CO2 gas or carbonated beverage for 5 h at 20°C and followed the same procedures as described above. The vertical axis shows CO2 concentration (% in volume). The values are the mean of four experiments ± S.D.

Additional Data Figure 3. Release of H2 and CH4 gas. After polymer bags were filled with H2 (a) or CH4 (b), the bags were sealed and sunken into water. The bag volumes were measured at the stated periods. The columns from left to right represent cellulose, polyethylene, polyurethane, and latex, respectively. The vertical axis shows the ratio of the initial H2 or CH4 volumes to the latter volumes, and the values are the mean of four experiments ± S.D.

Additional Data Figure 4. Photos of plants. a) Taiwan pineapple with 26 leaves grown in the top cut glass bottle (10-cm diameter) b) placed in a PE bag; c) cyclamen with 39 cm leave assembly, and d) whole cycad on the center and “yasude” plant on the upper left of the panel.