Supplementary

Machine learning-assisted construction of CDs@Fe-SA nanozymes colorimetric paper-based sensing of acrolein in baked food

Guo-Qi Zhang1, Hui-Ting Hu1, Shi-jun Tang3, Wen-Cai Jiang1, Lei Jia1, Si-Yu Yang1, Xiao-Mei Li1, Zhi-Bo Hou2*, Yan Zhao1*

1: Department of Chemisty, School of Science, Xihua University, Chengdu 610039, China

2: Department of Mathematics, School of Science, Xihua University, Chengdu 610039, China

3: Sichuan Engineering Research Center for lntelligent Control and Simulation Testing Technology of New EnergyVehicles, Xihua University, Chengdu 610039, China

*Corresponding author: Zhi-Bo Hou, Yan Zhao

Phone: +8618382270862

Full postal address: No. 999 Hongguang Road, PiDu District, Chengdu, China

E-mail: houzhibo@mail.xhu.edu.cn; yanzhao@mail.xhu.edu.cn;

Fig. S1 The BET test results of Fe-SA.

Fig. S2 Double reciprocal plots of CDs (A), Fe-SA(B), CDs@Fe-SA(C) with respect to H2O2; Double reciprocal plots of CDs (D), Fe-SA (E), CDs@Fe-SA (F) with respect to TMB.

Fig. S3 (A) pH of the buffer solution during incubation; (B) Incubation time; (C) Incubation temperature; (D) Reaction time; (E) Reaction temperature; (F) NAC concentration; (G)CDs concentration; (H)Fe-SA concentration

Fig. S4 (A) pH of buffer solution; (B) Reaction temperature; (C) Reaction time

Fig. S5 Selection experiment (K) and interference experiment (L) of acrolein.

.

| Table. S1 Comparison of BET data for CDs@Fe-SA and Fe-SA. |  |  |
| --- | --- | --- |
| Materials | CDs@Fe-SA | Fe-SA |
| SBET (m2·g-1) | 705.7 | 904.8 |
| Total pore volume (cm3·g-1) | 0.639 | 0.803 |
| Average pore diameter (nm) | 3.622 | 3.548 |
| Pore diameter (nm) | 3.07-108.5 | 3.06-143.8 |

| Table. S2 Comparison of kinetic parameters of CDs, Fe-SA, and CDs@Fe-SA. |  |  |  |
| --- | --- | --- | --- |
| Catalyst | Substance | Km (mM) | Vmax ×10-8 (M·s-1) |
| CDs | H2O2 | 1.209 | 412 |
|  | TMB | 1.37 | 484 |
| Fe-SA | H2O2 | 0.72 | 512 |
|  | TMB | 1.11 | 518 |
| CDs@Fe-SA | H2O2 | 0.522 | 608 |
|  | TMB | 0.892 | 531 |

| Table. S3 Detection of acrolein in real samples by microplate reader and recovery method (n=3) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | Spiked (mM) | Found (mM) | Recovery (%) | RSD (%) |
| French fries | 0.0 | 0.120 | - | - |
|  | 0.2 | 0.215 | 101.5 | 0.71 |
|  | 0.4 | 0.401 | 97.25 | 0.38 |
|  | 0.8 | 0.814 | 100.3 | 0.56 |
| Biscuit | 0.0 | 0.085 | - | - |
|  | 0.2 | 0.199 | 97.00 | 1.54 |
|  | 0.4 | 0.409 | 101.0 | 0.37 |
|  | 0.8 | 0.801 | 99.50 | 0.95 |
| Bread | 0.0 | 0.360 | - | - |
|  | 0.2 | 0.215 | 99.50 | 2.13 |
|  | 0.4 | 0.421 | 101.3 | 0.36 |
|  | 0.8 | 0.806 | 98.75 | 0.57 |

| Table. S4 Detection of acrolein in real samples by paper-based spiked recovery method (n=3) |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | Spiked (mM) | Found (mM) | Recovery (%) | RSD (%) |
| French fries | 0.0 | 0.103 | - | - |
|  | 0.8 | 1.030 | 115.9 | 3.67 |
|  | 1.2 | 1.387 | 107.0 | 3.82 |
|  | 1.6 | 1.942 | 115.0 | 3.85 |
| Biscuit | 0.0 | 0.095 | - | - |
|  | 0.8 | 0.971 | 109.5 | 2.73 |
|  | 1.2 | 1.368 | 106.1 | 4.06 |
|  | 1.6 | 1.747 | 103.3 | 1.24 |
| Bread | 0.0 | 0.350 | - | - |
|  | 0.8 | 0.876 | 105.1 | 1.60 |
|  | 1.2 | 1.283 | 104.0 | 4.08 |
|  | 1.6 | 1.853 | 113.6 | 4.67 |