Supplementary Information

Table S1. Independent variables and coded levels used in the Box–Behnken design.

| Coded level | A: Anthocyanin concentration (%) | B: Pectin proportion | C: Total polysaccharide concentration (%) |
| --- | --- | --- | --- |
| −1 | 0.05 | 0.50 | 2.0 |
| 0 | 0.10 | 0.75 | 2.5 |
| +1 | 0.15 | 1.00 | 3.0 |

Table S2. Box–Behnken experimental design and measured encapsulation efficiency of ASD-loaded hydrogel beads.

| Run | Anthocyanin concentration (%) | Pectin proportion | Total polysaccharide concentration (%) | Encapsulation efficiency (%) |
| --- | --- | --- | --- | --- |
| 1 | 0.05 | 0.50 | 2.5 | 39.13 |
| 2 | 0.05 | 0.75 | 3.0 | 44.63 |
| 3 | 0.10 | 0.50 | 2.0 | 40.82 |
| 4 | 0.10 | 0.75 | 2.5 | 50.51 |
| 5 | 0.10 | 0.50 | 3.0 | 44.57 |
| 6 | 0.15 | 0.75 | 3.0 | 50.69 |
| 7 | 0.15 | 0.75 | 2.0 | 50.57 |
| 8 | 0.05 | 0.75 | 2.0 | 44.20 |
| 9 | 0.10 | 0.75 | 2.5 | 49.12 |
| 10 | 0.10 | 1.00 | 2.0 | 46.79 |
| 11 | 0.10 | 0.75 | 2.5 | 49.21 |
| 12 | 0.10 | 0.75 | 2.5 | 50.57 |
| 13 | 0.15 | 1.00 | 2.5 | 49.93 |
| 14 | 0.15 | 0.50 | 2.5 | 49.05 |
| 15 | 0.10 | 1.00 | 3.0 | 48.35 |
| 16 | 0.05 | 1.00 | 2.5 | 47.28 |
| 17 | 0.10 | 0.75 | 2.5 | 49.98 |

Table S3. Analysis of variance, model adequacy, and validation statistics for the quadratic response surface model.

A. Analysis of variance

| Source | Sum of squares | df | Mean square | F value | p value | Significance |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 196.69 | 9 | 21.85 | 31.81 | < 0.0001 | *** |
| A | 78.13 | 1 | 78.13 | 113.72 | < 0.0001 | *** |
| B | 44.09 | 1 | 44.09 | 64.17 | < 0.0001 | *** |
| C | 4.29 | 1 | 4.29 | 6.25 | 0.0410 | * |
| AB | 13.21 | 1 | 13.21 | 19.23 | 0.0032 | ** |
| AC | 0.0240 | 1 | 0.0240 | 0.0350 | 0.8570 | ns |
| BC | 1.20 | 1 | 1.20 | 1.75 | 0.2280 | ns |
| A² | 1.37 | 1 | 1.37 | 1.99 | 0.2009 | ns |
| B² | 36.90 | 1 | 36.90 | 53.71 | 0.0002 | *** |
| C² | 13.42 | 1 | 13.42 | 19.53 | 0.0031 | ** |
| Residual | 4.81 | 7 | 0.6870 |  |  |  |
| Lack of fit | 2.90 | 3 | 0.9665 | 2.02 | 0.2530 | ns |
| Pure error | 1.91 | 4 | 0.4774 |  |  |  |
| Cor. total | 201.50 | 16 |  |  |  |  |

Significance codes: *** p < 0.001; ** p < 0.01; * p < 0.05; ns, not significant.

B. Model adequacy and validation

| Statistic | Value | Statistic | Value |
| --- | --- | --- | --- |
| Standard deviation | 0.8288 | R² | 0.9761 |
| Mean response | 47.38 | Adjusted R² | 0.9454 |
| Coefficient of variation (%) | 1.75 | Predicted R² | 0.7550 |
| Adequate precision | 19.2623 | Predicted optimum EE (%) | 51.182 |
| Experimental EE at practical optimum (%) | 51.48 ± 0.57 | Relative deviation from predicted value (%) | 0.58 |

Practical optimum: 0.12% anthocyanin, pectin proportion 0.825, and 2.6% total polysaccharides. Values are reported as mean ± SD for the validation experiment.