Supplementary material

Glycine-induced synthesis of vaterite via direct aqueous mineral carbonation of flue gas desulfurization gypsum

Xuemin Liu a, Zhihe Pan c, Huaigang Cheng c, Zhien Zhang d*, Fangqin Cheng c*, Bo Wang b*

a Jinxi Industries Group Co., LTD, Taiyuan 030027, People’s Republic of China

b Institute of Process Engineering, Chinese Academy Sciences, Beijing 100190, People’s Republic of China

c Institute of Resources and Environmental Engineering, Shanxi University, Taiyuan 030006, People’s Republic of China

d Department of Chemical and Biomedical Engineering, West Virginia University, Morgantown, WV 26506-6695, United State of America

*Corresponding authors: Zhien Zhang, Fangqin Cheng, and Bo Wang

Fax: +86 0351-7018553; Tel: +86 0351-7018553

E-mail: zhien.zhang@mail.wvu.edu, cfangqin@sxu.edu.cn, and wangbo@ipe.ac.cn

# Fig. S1. Scanning electron microscope images of products from FGDG carbonation in the presence of gylcine (wt%) a) 0, b) 5, c)10, d) 15, e) 20, f) 40.

Fig. S2. Fourier transform infrared spectra of carbonation products prepared with different glycine concentration.

Fig. S3. Thermogravimetry and differential scanning calorimetry curve of mineralization products under 20 wt% glycine.

# Fig. S1.

# Fig. S1. Scanning electron microscope images of products from FGDG carbonation in the presence of gylcine (wt%) a) 0, b) 5, c)10, d) 15, e) 20, f) 40.

# All carbonation products obtained at different concentration of glycine were analyzed by SEM (Fig. S1). The as-prepared samples obtained in the absence of glycine shown sphere-like and rhombohedral particles structure (Fig. S1a), which are similar with our previous result (Wang et al. 2019). However, the sphere-like vaterite gradually increased with increasement of glycine concentration, and finally vaterite was dominated phase (Fig. S1b-f). The SEM images furtherly revealed that these microspheres were composed of the aggregation of numerous primary nanoparticles (Fig. S1e-f). Many vaterite microspheres were observed to be interconnected with each other demonstrating there were a tendency of conglutination or clustering between vaterite particles.

# Fig. S2.

Fig. S2. Fourier transform infrared spectra of carbonation products prepared with different glycine concentration.

# Carbonation products were analyzed by FTIR. With the increase of the concentration of glycine, the characteristic peak of calcite at 712 cm-1 gradually weakened, and the characteristic peak of vaterite (745 cm-1) gradually increased (Fig. S2).

# Fig. S3.

# Fig. S3. Thermogravimetry and differential scanning calorimetry curve of mineralization products under 20 wt% glycine.

# Fig. S3 shows the TG-DSC curve of carbonation product at the glycine concentration of 20 wt%. TG curve has three temperature ranges of weight loss at 50–200 °C, 200–600 °C and 600–850 °C were ascribed to water evaporation, glycine decomposition and CaCO3 decomposition respectively. For DSC curve, the endothermic peaks near 100 °C and 782 °C are due to water evaporation and CaCO3 decomposition. The exothermic peak near 498 °C is due to the phase transformation of vaterite to calcite under high temperature. The TG results further showed that there was a small amount of glycine in CaCO3 products, which could stabilize the metastable vaterite and prevent it from transforming into calcite (Lai et al. 2015; Luo et al. 2015).

References

Lai Y, Chen L, Bao W, Ren Y, Gao Y, Yin Y, Zhao Y (2015) Glycine-mediated, selective preparation of monodisperse spherical vaterite calcium carbonate in various reaction systems. Cryst Growth Des 15:1194–1200 doi: 10.1021/cg5015847

Luo J, Kong F, Ma X (2015) Role of aspartic acid in the synthesis of spherical vaterite by the Ca(OH)2–CO2 reaction. Cryst Growth Des 16:728–736 doi:10.1021/acs.cgd.5b01333Wang B, Pan Z, Du Z, Wang B, Pan Z, Du Z, Cheng H, Cheng F (2019) Effect of impure components in flue gas desulfurization (FGD) gypsum on the generation of polymorph CaCO3 during carbonation reaction. J Hazard Mater 369:236–243 doi: 10.1016/j.jhazmat.2019.02.002