Supplementary Information for

Fast Sheath-driven Electrothermal Artificial Muscles

with High Power Densities

Xinghao Hu1,4†, Jingjing Jia2,5, Yingming Wang1, Xintian Tang3, Shaoli Fang2, Yilun Wang1, Jian Wang1, Ray H. Baughman2†, and Jianning Ding1,4

1 Institute of Intelligent Flexible Mechatronics, Jiangsu University, Zhenjiang, 212013, PR China

2 The Alan G. MacDiarmid NanoTech Institute, The University of Texas at Dallas, Richardson, Texas 75080, USA

3 State Key Laboratory of Robotics and System, Harbin Institute of Technology, Harbin 150001, Heilongjiang Province, China

4 Jiangsu Collaborative Innovation Center of Photovoltaic Science and Engineering, Changzhou University, Changzhou 213164, China

5 Institute of Materials Engineering, Beijing Institute of Collaborative Innovation, Beijing 100094, China.

Corresponding authors. Email: ray.baughman@utdallas.edu; huxh@ujs.edu.cn

Keywords: artificial muscle, thermal muscle, carbon nanotube muscle, electrothermal actuator, sheath run artificial muscle

Figures and Tables

Supplementary Figure 1. Microstructure for sheath-driven artificial muscles with different polymer cores, before twist insertion to obtain complete coiling. SEM cross-section images for (a) CNT_PDMS@CNT; (b) Kevlar_PDMS@CNT; (c) PI_PDMS@CNT. (d) SEM image of a PI yarn. SEM micrographs showing the sheath-core structure for (e) Kevlar_PDMS@CNT and (f) PI_PDMS@CNT muscles. The muscle sheath for (e) and (f) was cracked by untwisting the muscle while it was immersed in liquid nitrogen.

Supplementary Figure 2. SEM images for sheath-driven PI_PDMS@CNT muscles with spring indices of (a) 1.77; (b) 1.49; (c) 1.29; (d) 1.38.

Supplementary Figure 3. Thermal gravimetric measurements of residual mass as a function of temperature for a hybrid PDMS@CNT muscle, which shows that the PDMS evaporates at around 450℃. The temperature scan rate was 2℃/min.

Supplementary Figure 4. The thermal actuation of a sheath-driven PI_PDMS@CNT muscle. (a) The time dependence of contractile stroke for a neat CNT muscle actuated using a 0.05 Hz, 0.31 W/cm square-wave power input. (b) The stress dependence of contractile stroke and work capacity for the CNT muscle used in (a) and the same actuation frequency and power. (c, d) During thermal mechanical analysis temperature scans at 5℃/min, (c) tensile actuation as a function of temperature for different applied loads. (d) The stress dependence of contractile stroke and work capacity for the muscle used in (c).

Supplementary Figure 5. Actuation for sheath-driven PI_PDMS@CNT muscles and hybrid PDMS@CNT muscles. Tensile actuation as a function of time for sheath-driven PI_PDMS@CNT muscle when driven by a 10.4 kW/g square-wave power input with frequencies of (a) 1 Hz; (b) 8 Hz. The applied tensile stress was 15.6 MPa. (c) The frequency dependence of stroke rate for a PI_PDMS@CNT and a PDMS@CNT muscle. The applied loads were 15.6 MPa and 14.3 MPa, respectively. The applied square-wave power was 10.4 kW/g. (d) The contractile stroke and work capacity as a function of applied tensile stress for a coiled PI_PDMS@CNT muscle and PDMS@CNT muscle for a 0.3 Hz, 5.4 kW/g square-wave power input. The spring indices for these muscles are 1.55 and 1.56, respectively. The weight percent of PDMS to CNT is 20 wt % for sheath-driven and hybrid muscles. The yarn diameter for sheath-driven muscle and hybrid muscle are 68 m and 78 m, respectively.

Supplementary Figure 6. Contractile efficiencies for sheath-driven muscles and hybrid muscles for an applied square-wave power input of 10.4 kW/g. (a) Contractile conversion efficiency as a function of applied square-wave frequency for a sheath-driven muscle and a hybrid muscle. The applied tensile stresses are 15.6 MPa for the sheath-driven muscle and 14.7 MPa for the hybrid muscle. (b) Contractile conversion efficiency as a function of applied tensile stress for the sheath-driven muscle and the hybrid muscle used in (a). The applied square-wave frequency is 1 Hz for both muscles.

Supplementary Figure 7. Actuation of a hybrid PDMS@CNT yarn muscle when a 5.9 V/cm square-wave voltage is applied. Contractile stroke as a function of time for a PDMS@CNT hybrid muscle when driven by square-wave voltage with frequencies of (a) 0.4 Hz; (b) 1 Hz; (c) 3 Hz; (d) 8 Hz. The applied mechanical load is 12.6 MPa for these applied frequencies.

Supplementary Figure 8. Contractile stroke as a function of input power for a PI_PDMS@CNT muscle, a PDMS@CNT muscle, and a neat CNT muscle when driven by a 0.05 Hz square-wave voltage.

Supplementary Figure 9. Isometric stress generation by a sheath-driven PI_PDMS@CNT yarn muscle when applying a 15 V/cm square-wave voltage. (a) The generated stress as a function of the applied pre-strain for the sheath-driven muscle and the PDMS@CNT hybrid muscle when driven by a 0.1 Hz square-wave voltage. (b) The time dependence of stress for a PI_PDMS@CNT yarn muscle when driven by a square-wave voltage with frequencies of 0.2 Hz, 0.5 Hz, and 1 Hz, respectively.

Supplementary Figure 10. Calculated temperatures for a PDMS@CNT hybrid muscle when applying a 1 Hz square-wave power of 2 W/mm3. (a) Modeling results showing the time dependence of temperature for muscle surface and muscle center. (b) Surface and internal temperatures for hybrid muscle in non-actuated and actuated states, which indicates that the temperature from muscle surface to muscle center are almost the same.

Supplementary Figure 11. Calculated average temperatures of sheath and core for sheath-driven muscles with sheath-core ratios of (a) 0.16; (b) 3; (c) 0.5, when driven by a 2 W/mm3 square-wave input power.

Supplementary Table 1. Mechanical properties of polymer fibers that were used as the core of sheath-driven muscles.

| Fiber | Tensile strength (GPa) | Tensile modulus (GPa) | Elongation at break (%) |
| --- | --- | --- | --- |
| Kevlar 29 | 2.8 | 125 | 2.4 |
| Polyimide fiber (P84®) | 3.1 | 271 | 2.0 |