Supplementary Material

Facile extraction and Characterization of Calcium Hydroxide from Paper Mill Waste Sludge of Bangladesh

Mohammad Robel Molla1⸸, Most. HosneyAra Begum1,⸸*, Syed Farid Uddin Farhad1,*  A. S. M. Asadur Rahman2, Nazmul Islam Tanvir1, Muhammad Shahriar Bashar3, Riyadh Hossen Bhuiyan4, Md. Sha Alam5, Mohammad Sajjad Hossain1, and Mir Tamzid Rahman6

⸸ Contributed equally to this work.

1BCSIR Laboratories, Dhaka, Bangladesh Council of Scientific and Industrial Research, Dhaka-1205 Bangladesh

2Department of Chemistry, Comilla University, Cumilla-3506

3Institute of Fuel Research and Development, Bangladesh Council of Scientific and Industrial Research, Dhaka-1205 Bangladesh

4Fiber and Polymer Research Division, Bangladesh Council of Scientific and Industrial Research, Dhaka-1205 Bangladesh

5Institute of Mining, Mineralogy & Metallurgy, Bangladesh Council of Scientific and Industrial Research, Joypurhat-5900, Bangladesh

6Department of Chemistry, Jahangirnagar University, Savar, Dhaka-1342, Bangladesh

*Correspondence address:

Dr. Hosne Ara Begum, CSO

& Dr. Syed Farid Uddin Farhad, PSO

Industrial Physics Division,

BCSIR Laboratories, Dhaka, BCSIR, Dhaka-1205

Email: hosneyara@gmail.com ; s.f.u.farhad@bcsir.gov.bd

Figure S1: Photographs of two representative raw samples (in polybags) and products (in plastic vials) of PMS collected from two different sources.

Figure S2: Reference FTIR (a) and Raman (b) spectra of portlandite, calcite, and aragonite from RRUFF database. The corresponding data ID is included in the parenthesis of the curve legends.

Figure S3: Room temperature Raman spectra of pure Ca(OH)2 and the same Ca(OH)2 sample after exposure to the air in 144 h to monitor the CaCO3 formation. The room temperature Raman spectra of pure CaCO3 is also included in the graph for comparison. Major Raman peak of Ca(OH)2  is slightly red-shifted from 359.72 cm-1 to 357.66 cm-1 presumably due to the strain generation in the sample understudy owing to the formation of CaCO3 in the air-exposed Ca(OH)2 sample.

Table S1: Acid and base treatment of dried raw sludge at approximately constant pH value

| Acid and Base treatment of dry sludge |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Batch Number | Weight of taken sample (g) | Volume of water added in sample | 1M HCl (mL) | pH (in HCl) | 3M NaOH (mL) | pH (in NaOH) | Weight of Product, Ca(OH)2 (g) | Weight of Pulp Residue (g) | Loss of Product (g) |
| S-a A | 2.01 | 130 mL | 40 mL | 1.95 | 105 mL | 13.494 | 1.20 | 0.37 | 0.43 |
| S-a B | 4.01 | 250 mL | 70 mL | 1.72 | 210 mL | 13.483 | 2.20 | 0.75 | 1.05 |
| S-a C | 6.03 | 300 mL | 80 mL | 2.32 | 210 mL | 13.482 | 3.28 | 1.49 | 1.23 |
| S-a D | 8.01 | 350 mL | 150 mL | 2.34 | 280 mL | 13.432 | 4.57 | 1.76 | 1.67 |
| S-a E | 10.01 | 450 mL | 180 mL | 2.25 | 330 mL | 13.493 | 6.50 | 1.91 | 1.59 |
| S-b A | 2.00 | 130 mL | 35 mL | 2.00 | 90 mL | 13.429 | 1.13 | 0.25 | 0.62 |
| S-b B | 4.01 | 200 mL | 75 mL | 2.17 | 170 mL | 13.484 | 2.65 | 0.45 | 0.90 |
| S-b C | 6.01 | 350 mL | 130 mL | 2.12 | 380 mL | 13.472 | 4.28 | 1.57 | 0.15 |
| S-b D | 8.01 | 450 mL | 280 mL | 2.15 | 400 mL | 13.489 | 6.14 | 1.68 | 0.18 |
| S-b E | 10.01 | 600 mL | 260 mL | 2.13 | 410 mL | 13.487 | 7.75 | 1.73 | 1.26 |

Figure S4: Reference X-ray diffractograms of portlandite, calcite, and aragonite from the RRUFF database of same data presented in Figure S2. The corresponding data ID is included in the parenthesis of the curve legends.

Figure S5: X-ray diffractograms (wide 2θ scanning range) of two representative source and synthesized samples.

Figure S6: Predominant Bragg peak (101) of Ca(OH)2 and (104) of CaCO3 from XRD data were utilized  to extract different diffraction parameter of the product-A and product-B.

Table S2: Extracted diffraction parameters from XRD data of product-A and product-B

| Sample | Xc ± 0.005 | FWHM (deg.) | Area (a.u.) | Prdc. ratio | Crystallite Size (nm) | Micro- strain | Comments |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Product-A | 34.43 | 0.207±0.002 | X1: 520.48 | X1/X2: 3.67 | 41.96 | 2.92E-03 |  |
| Product-B | 34.35 | 0.238±0.002 | Y1: 417.47 |  | 36.49 | 3.36E-03 | 6.77/3.67 = 1.84 |
| Product-A | 29.76 | 0.219±0.005 | X2: 141.86 | Y1/Y2: 6.77 | 39.20 | 3.60E-3 |  |
| Product-B | 29.67 | 0.267±0.010 | Y2: 61.68 |  | 32.15 | 4.40E-3 |  |