SUPPORTING INFORMATION

Evolved Gas Analysis and Mechanistic Modeling of Thermal Degradation Products from Polytetrafluoroethylene using Thermogravimetric Analysis-Mass Spectrometry (TGA-MS) and Density Functional Theory

Benjamin R. Johnson1,2, Aaron D. Ajeti3, Justin R. Toole1, Nijel J. Rogers1, Dairen Jean1, Taylor N. Miller1, Jacob R. Nauman1, Edward L. Zhang1, Amelia J. Kitlinski1, Charles M. Aronov1, Kai D. Palam1, Andon Z. Thomas1, H. Daniel Bahaghighat1, Samuel V. Cowart1,2, Corey M. James1, Pamela L. Sheehan4, Simuck F. Yuk1,2*, Shubham Vyas3*, and Enoch A. Nagelli1,2*

1Department of Chemical and Biological Science and Engineering, United States Military Academy, West Point, NY 10996, USA; 2Photonics Research Center, United States Military Academy, West Point, NY 10996, USA; 3Department of Chemistry, Colorado School of Mines, Golden, CO 80401, USA; 4U.S. Army Combat Capabilities Development Command, Picatinny Arsenal, NJ 07806, USA.

*Co-corresponding authors: simuck.yuk@westpoint.edu, svyas@mines.edu, enoch.nagelli@westpoint.edu

Supplemental information S1: Details of DFT calculations.

Density functional theory (DFT) calculations performed with Gaussian 16 using DFT method ωB97XD/6-311+G(d,p) Single point energies thermally corrected to 298 and 795 K with GoodVibes software. The reverse radical recombination rate constant applied to unimolecular BDEs is 1010 M-1 * s-1. This may be a source of error for predicted dissociation rate constants,1 however the activation energies and the resulting trends should be the same. Bimolecular rate constants were calculated with transition state theory.

Table S1. DFT-calculated pathways of PTFE degradation.

| Reaction (795 K only) | ΔG |  | ΔH | Ea |  |  |  |  |  |  |  | k (s-1) |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C7F16 → C6F13 + CF3 | 44.3 |  | 85.0 | 84.2 |  |  |  |  |  |  |  | 1.02 × 10-4 |  |
| C7F16 → C5F11 + C2F5 | 36.7 |  | 80.0 | 79.4 |  |  |  |  |  |  |  | 1.25 × 10-2 |  |
| C7F16 → C4F9 + C3F7 | 33.9 |  | 79.1 | 78.6 |  |  |  |  |  |  |  | 7.43 × 10-2 |  |
| C7F16 → C7F15 + FA | 89.5 |  | 118.5 | 116.7 |  |  |  |  |  |  |  | 3.74 × 10-17 |  |
| C7F16 → C7F15 + FB | 79.0 |  | 109.4 | 107.1 |  |  |  |  |  |  |  | 2.91 × 10-14 |  |
| C7F16 → C7F15 + FC | 77.5 |  | 107.6 | 105.6 |  |  |  |  |  |  |  | 7.50 × 10-14 |  |
| C7F16 → C7F15 + FD | 77.5 |  | 107.4 | 105.5 |  |  |  |  |  |  |  | 7.49 × 10-14 |  |
| Chain shortening |  | ΔG 298 ¦ 795 K |  |  | ΔH | Ea (ΔG) |  | Rev Ea (ΔG) |  | Ea (ΔH) | Rev Ea (ΔH) |  | k (M-1 s-1) |  | rev k |
| A1) C6F13 → C2F4 + C4F9 |  | 19.7 ¦ -4.93 |  |  | 33.8 ¦ 32.3 | 34.6 ¦ 32.4 |  | 14.9 ¦ 37.3 |  | 36.5 ¦ 36.1 | 2.63 ¦ 3.83 |  | 2.59 × 10-13 ¦ 2.12 × 104 |  | 73.6 ¦ 2.82 × 10-15 |
| B1) C6F13 → C5F11 + CF2 *Ea obtained by Ahrenius plot |  | 39.3 ¦ 16.3 |  |  | 52.8 ¦ 51.6 | 50.2 ¦ 50.2 |  | N/A |  | N/A | N/A |  | 6.56 × 10-21 ¦ 4.93 ×103 |  | 1.00 × 1010 ¦ 1.00 × 1010 |

Chain Shortening involving a 1,2–F atom shift (not included in the original mechanism)

C6F13_C1 radical		C6F13_C2 radical		C3F6       +         C3F7

| Chain shortening | ΔG 298 ¦ 795 K | ΔH | Ea (ΔG) | Rev Ea (ΔG) | Ea (ΔH) | Rev Ea (ΔH) | k (M-1 s-1) | rev k |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1,2–F atom shift | -8.44 ¦ -9.00 | -7.98 ¦ -8.00 | 35.9 ¦ 35.8 | 44.3 ¦ 44.8 | 35.9 ¦ 35.3 | 43.9 ¦ 43.3 | 3.01 × 10-14 ¦ 2.46 × 103 | 1.92 × 10-20 ¦ 8.22 |
| C6F13 → C3F6 + C3F7 | 12.9 ¦ -12.6 | 27.5 ¦ 25.9 | 30.5 ¦ 29.3 | 17.6 ¦ 42.0 | 31.6 ¦ 31.2 | 4.07 ¦ 5.31 | 2.73 × 10-10 ¦ 1.45 × 105 | 0.756 ¦ 48.5 |

| Oxidation Reaction 1 | ΔG 298 ¦ 795 K | ΔH | Ea (ΔG) | Rev Ea (ΔG) | Ea (ΔH) | Rev Ea (ΔH) | k (M-1 s-1) | Rev k |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C) C6F13 + O2 → C6F13O2 | -16.6 ¦ 4.05 | -28.8 ¦ -28.0 | 0 ¦ 4.05 | 26.4 ¦ 26.4 | 0 ¦ 0 | 26.4 ¦ 26.4 | 4.4 ×109 ¦ 4.4 ×109 | 1.10 × 106 ¦ 9.16 × 105 |
| C1) C6F13O2 → C6F13O + O | 46.5 ¦ 30.1 | ¦ 56.2 | 55.4 ¦ 55.4 | 0 ¦ 0 | ¦ 56.2 | 0 ¦ 0 | 3.19 ×10-26 ¦ 0.815 | Diffusion limited |
| C2a) C6F13O → C5F11 + COF2 | -27.1 ¦ -50.3 | -13.0 ¦ -15.0 | 2.13 ¦ 2.25 | 29.1 ¦ 52.6 | 2.32 ¦ 1.60 | 15.4 ¦ 16.6 | ¦ 4.58 ×1012 | ¦ 0.412 |

| Oxidation Reaction 2 | ΔG 298 ¦ 795 K | ΔH | Ea (ΔG) | Rev Ea (ΔG) | Ea (ΔH) | Rev Ea (ΔH) | k (M-1 s-1) | rev k |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C) C6F13 + O2 → C6F13O2 | -16.6 ¦ 4.05 | -28.8 -28.0 | 0 ¦ 4.05 | 26.4 ¦ 26.4 | 0 ¦ 0 | 26.4 ¦ 26.4 | 4.4 ×109 ¦ 4.4 ×109 | 1.10 × 106 ¦ 9.16 × 105 |
| C1) C6F13O2 → C6F13O + O | 46.5 ¦ 30.1 | 55.8 ¦ 56.2 | 55.4 ¦ 55.4 | 0 ¦ 0 | ¦ 56.2 | 0 ¦ 0 | 3.19 ×10-26 ¦ 0.815 | Diffusion limited |
| C2b) C6F13O + H2O → C6F13OH + OH | 1.79 ¦ 2.99 | 0.99 ¦ 1.29 | 13.8 ¦ 32.1 | 12.1 ¦ 29.1 | 3.52 ¦ 4.19 | 2.54 ¦ 2.90 | 434 ¦ 2.53 × 104 | 8970 ¦ 1.68 × 105 |
| C3) C6F13OH → C6F12=O + HF | -6.10 ¦ -24.5 | 5.04 ¦ 4.66 | 43.4 ¦ 43.8 | 49.5 ¦ 68.3 | 43.5 ¦ 43.0 | 38.4 ¦ 38.3 | 8.51 × 10-20 ¦ 15.5 | 2.87 × 10-24 ¦ 2.8 × 10-6 |
| C4) C6F12=O + H2O → C5F11COOH + HF | -9.10 ¦ -7.60 | -10.1 ¦ -9.74 | 42.3 ¦ 62.2 | 51.4 ¦ 69.8 | 30.3 ¦ 30.6 | 40.4 ¦ 40.4 | 5.99 × 10-19 ¦ 1.28 × 10-4 | 1.27 × 10-25 ¦ 1.04 × 10-6 |
| C5) C5F11COOH → CO2 + HF + C5F10 | -44.4 ¦ -55.1 | 11.7 ¦ 4.97 | 64.9 ¦ 63.9 | 109.3 ¦ 118.9 | 65.5 ¦ 65.2 | 53.8 ¦ 60.2 | 1.69 × 10-35 ¦ 4.54 × 10-5 | 4.53 × 10-68 ¦ 3.33 × 10-20 |

| COF2 hydrolysis | ΔG 298 ¦ 795 K | ΔH 298 ¦ 795 K | Ea (ΔG) 298 ¦ 795 K | Rev Ea (ΔG) 298 ¦ 795 K | Ea (ΔH) 298 ¦ 795 K | Rev Ea (ΔH) 298 ¦ 795 K | k (M-1 s-1) 298 ¦ 795 K | rev k 298 ¦ 795 K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| COF2 + H2O → COFOH + HF | -8.06 ¦ -7.58 | -8.50 ¦ -7.98 | 46.1 ¦ 64.6 | 54.1 ¦ 72.2 | 35.0 ¦ 35.3 | 43.5 ¦ 43.3 | 1.01 × 10-21 ¦ 2.89 × 10-5 | 1.24 × 10-27 ¦ 2.39 × 10-7 |
| COFOH + H2O → CO2 + HF | -22.9 ¦ -37.5 | -14.4 ¦ -14.2 | 30.3 ¦ 26.6 | 53.2 ¦ 64.1 | 30.4 ¦ 30.9 | 44.8 ¦ 45.0 | 3.58 × 10-10 ¦ 8.30 × 105 | 5.57 × 10-27 ¦ 4.07 × 10-5 |

| TFE/HFP/c–C4F8 | ΔG 298 ¦ 795 K | ΔH 298 ¦ 795 K | Ea (ΔG) 298 ¦ 795 K | Rev Ea (ΔG) 298 ¦ 795 K | Ea (ΔH) 298 ¦ 795 K | Rev Ea (ΔH) 298 ¦ 795 K | k (M-1 s-1) 298 ¦ 795 K | rev k 298 ¦ 795 K |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| D1) C2F4 + CF2 → c-C3F6 | -27.7 ¦ -6.83 | -40.2 ¦ -39.1 | 19.3 ¦ 39.4 | 47.0 ¦ 46.2 | 7.79 ¦ 8.74 | 48.0 ¦ 47.9 | 4.15 × 10-2 ¦ 247.9 | 2.12 × 10-22 ¦ 3.3 |
| D2) c-C3F6 → CF3CF=CF2 | -27.6 ¦ -27.7 | -27.2 ¦ -27.2 | 55.4 ¦ 54.6 | 83.0 ¦ 82.2 | 56.2 ¦ 55.9 | 83.4 ¦ 83.1 | 1.48 × 10-28 ¦ 1.67 × 10-2 | 8.11 × 10-49 ¦ 4.09 × 10-10 |
| D3) C2F4 + C2F4 → c-C4F8 | -11.6 ¦ -13.8 | -48.9 ¦ -49.1 | 71.5 ¦ 69.4 | 83.1 ¦ 83.2 | 38.7 ¦ 38.6 | 87.6 ¦ 87.6 | 1.44 × 10-23 ¦ 1.33 × 10-6 | 1.62 × 10-50 ¦ 2.13-10 |

| Tetrafluoroethylene (TFE) oxidation (1st possibility) | ΔG 298 ¦ 795 K | ΔH | Ea (ΔG) | Rev Ea (ΔG) | Ea (ΔH) | Rev Ea (ΔH) | k (M-1 s-1) | rev k |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| E1) C2F4 + O2 → C2F4O2 triplet | 27.9 ¦ 44.9 | 18.1 ¦ 19.2 | 35.1 ¦ 51.4 | 7.2 ¦ 6.5 | 25.9 ¦ 26.6 | 7.78 ¦ 7.36 | ¦ 0.121 | ¦ 2.71 ×1011 |
| E2) C2F4O2 triplet → C2F4O2 ring | -55.9 ¦ -51.7 | -58.4 ¦ -59.1 | Diffusion limited |  |  |  |  |  |
| E3) C2F4O2 ring → 2 COF2 | -98.0 ¦ -120.2 | -84.7 ¦ -86.3 | Diffusion limited (also can not find a transition state due to singlet to triplet to singlet crossover) |  |  |  |  |  |
| E4a1) COF2 + HF → CF3OH | 4.14 ¦ 14.5 | -6.03 ¦ -5.63 | 47.1 ¦ 53.6 | 43.0 ¦ 39.0 | 43.0 ¦ 38.0 | 43.0 ¦ 43.6 | 1.64 ×10-22 ¦ 0.0313 | 1.78 ×10-19 ¦ 310.6 |
| E4a2) CF3OH + OH → CF3O + H2O | -0.54 ¦ -1.79 | 0.32 ¦ - 0.123 | 13.0 ¦ 24.1 | 13.5 ¦ 25.9 | 3.41 ¦ 5.77 | 3.41 ¦ 5.89 | 1.89 ×103 ¦ 4.01 ×106 | 7.54 ×102 ¦ 1.29 ×106 |

*E1 to E3 is suspected to be one smooth reaction as it is extremely thermodynamically driven.

| Hexafluoropropylene (HFP) oxidation | ΔG 298 ¦ 795 K | ΔH | Ea (ΔG) | Rev Ea (ΔG) | Ea (ΔH) | Rev Ea (ΔH) | k (M-1 s-1) | rev k |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| F1) C3F6 + O2 → C3F6O2 triplet | 33.6 ¦ 51.8 | 23.0 ¦ 24.3 | 39.9 ¦ 58.4 | 6.32 ¦ 6.64 | 29.4 ¦ 30.1 | 6.37 ¦ 5.80 | 3.37 ×10-17 ¦ 1.47 ×10-3 | 1.44 ×108 ¦ 2.48 ×1011 |
| F2) C3F6O2 + H2O → C3F6OOH + OH * this reaction possibly goes through an O–O homolytic cleavage instead | 27.0 ¦ 27.1 | 26.9 ¦ 27.5 | 32.9 ¦ 50.9 | 5.93 ¦ 23.8 | 22.5 ¦ 23.4 | -4.37 ¦ -4.08 | 4.69 ×10-12 ¦ 0.165 | 2.78 ×108 ¦ 4.70 ×106 |
| F3) C3F6OOH → C3F6Oring + OH | -25.9 ¦ -41.3 | -17.4 ¦ -18.2 | 14.8 ¦ 14.9 | 40.8 ¦ 56.2 | 14.5 ¦ 14.2 | 32.0 ¦ 32.4 | 80.1 ¦ 1.33 ×109 | 7.60 ×10-18 ¦ 6.00 ×10-3 |
| F4) C3F6Oring→ CF2 + C2F4=O | 15.4 ¦ -7.48 | 29.1 ¦ 28.1 | 37.5 ¦ 36.4 | 22.1 ¦ 43.9 | 38.5 ¦ 38.3 | 9.39 ¦ 10.2 | 1.97 ×10-15 ¦ 1.58 ×103 | 3.69 ×10-4 ¦ 13.9 |
| F5) C2F4=O + H2O → CF3COOH + HF | -9.00 ¦ -7.64 | -9.89 ¦ -9.50 | 42.1 ¦ 61.7 | 51.1 ¦ 69.3 | 30.3 ¦ 30.6 | 40.2 ¦ 40.1 | 8.74 ×10-19 ¦ 1.84 ×10-4 | 2.20 ×10-25 ¦ 1.46-6 |

Possible alternative to F2, F3

| alternate | ΔG 298 ¦ 795 K | ΔH | Ea (ΔG) | Rev Ea (ΔG) | Ea (ΔH) | Rev Ea (ΔH) | k (M-1 s-1) | rev k |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C3F6O2 → O + C3F6Oring | -12.4 ¦ -25.6 | -5.1 ¦ -5.1 | -5.47 ¦ -5.47 | N/A | N/A | N/A | 5.32 × 1017 ¦ 1.67 ×1015 | N/A |

Calculated through the unimolecular reverse recombination rate constant, may not be accurate, but wanted report it.

References:

(1)	Rossi, M.; Golden, D. M. Rate of Decomposition of Hexafluoroazomethane and the Absolute Rate of Recombination of Trifluoromethyl Radical at Higher Temperatures. Int J Chem Kinet 1979, 11 (7), 775–788. https://doi.org/10.1002/kin.550110709.

Supplemental information S2: Microkinetic model Python script

Table S2. Microkinetic model Python script of PTFE degradation in Figure 7 of main text.

"""

Created on Wed Sep 17 13:16:50 2025

@author: benjamin.johnson2

"""

# Import packages

import math

# Output file

outfile = open("MKM_jump_v2_20_deact.csv", "w")

outfile.write("CF2-CF2,CF2-*-CF2,CF3-*-CF2,CF2-O2-CF2,C2F4(g),C3F6(g),COF2,Time (s),Temp (C)\n")

# Initialize some variables

time = 0. # s

temperature_start = 450 + 273.15 # K

temperature = temperature_start

heating_rate = 20 # K/min

gas_constant = 1.98720e-3 # kcal/(mol K)

k_B = 1.38065e-23 # Boltzmann constant; J/K

h_P = 6.62607e-34 # Planck constant, J s

num_cycles = 0

init_time_step = 1e-10

big_time_step = 1e-3

small_time_step = init_time_step

clutch = 0

clutch_limit = 25

# Initialize concentration array:

# [0]: CF2-CF2- regular bond        A

# [1]: CF2-*-CF2- activated bond    B

# [2]: CFCF3-*-CF2- F-shifted bond  C

# [3]: CF2-O2-CF2- Oxygenated bond  D

# [4]: C2F4(g) (TFE product)        E

# [5]: C3F6(g) (HFP product)        F

# [6]: COF2(f) product              G

# [-2]: Time (s)

# [-1]: Temperature (C)

num_species = 7

conc_array = [[]]

for i in range(num_species):

conc_array[0].append(0.)

conc_array[0][0] = 1.

changes_array = [[]]

change_rates = []

change_factors = []

for i in range(len(conc_array[0])):

changes_array[0].append(0.)

change_rates.append(0.)

change_factors.append(0.)

conc_array[0].append(time)

conc_array[0].append(temperature_start - 273.15)

record_interval = 1e6

record_interval2 = 1e6

force_interval = record_interval / 500

#for item in conc_array[0]:

#    outfile.write(str(item) + ",")

#outfile.write(",")

# Create lists for activation energies and rates:

#                                                                        [] denotes using carbons from carbon chain:

#                                                                        Affects amounts consumed/produced but not kinetics

# [0]: CF2-CF2-CF2-CF2- --> CF2-CF2-*-CF2-CF2- (bond activation)                             A --> B

# [1]: CF2-CF2-*-CF2-CF2- --> CF2-CF2-CF2-CF2- (deactivation)                                B --> A

# [2]: CF2-CF2-*-CF2-CF2 --> C2F4(g) + CF2-CF2-CF2-CF2- (TFE release and deactivation)       [2A + ] B --> E + A

# [3]: CF2-CF2-*-CF2-CF2 --> CF2-CFCF3-*-CF2-CF2- (F-shift from secondary to primary carbon) [A + ] B --> C

# [4]: CF2-CFCF3-*-CF2-CF2- --> CF2-CF2-*-CF2-CF2 (F-shift from primary to secondary carbon) C --> B [+ A]

# [5]: CF2-CFCF3-*-CF2-CF2- --> C3F6(g) + CF2-CF2-CF2-CF2- (HFP release and deactivation)    [2A +] C --> F + A

# [6]: CF2-CF2-CF2-CF2- --> CF2-CF2-O2-CF2-CF2- (bond oxygenation)                           A --> D

# [7]: CF2-CF2-O2-CF2-CF2- --> CF2-CF2-*-CF2-CF2- (oxygen removal)                           D --> A

# [8]: CF2-CF2-O2-CF2-CF2- --> CF2-CF2-CF2- + COF2 + O* (oxygen splitting and COF2 removal)  [A + ] D --> G + A

#      (Reverse reaction very slow, subsequent COF2 removal very fast)

num_reactions = 9

act_energies = []

rates = []

for i in range(num_reactions):

act_energies.append(0.)

rates.append(0.)

prefactor1 = 2.41e17

prefactor2 = 4.00e21

jump_flag = False

jump_count = 0

stall_count = 0

stall_limit = 10000

max_change_rate = 1e6

#

# Begin main loop

#

while conc_array[-1][0] > 0.01 and num_cycles < (5e9 + 1):

last_change_rate = max_change_rate

if num_cycles % record_interval == 0:

for item in conc_array[-1]:

outfile.write(str(item) + ",")

outfile.write(",")

#    prefactor = k_B * temperature / h_P # 1/s

#### Calculate activation energies:

delta_G_CCsplit = 79.1 - (0.056855 * temperature)

delta_G_Fshift = -8.4 + (-0.0012072 * (temperature - 298))

delta_G_oxy = -16.6 + (0.041650 * (temperature - 298))

delta_G_directoxy = delta_G_CCsplit + delta_G_oxy

K_eq_CCsplit = math.exp(-delta_G_CCsplit / (gas_constant * temperature))

K_eq_Fshift = math.exp(-delta_G_Fshift / (gas_constant * temperature))

K_eq_oxy = math.exp(-delta_G_oxy / (gas_constant * temperature))

act_energies[0] = 78.6 + (0.0 * (temperature - 298))

act_energies[1] = act_energies[0] - delta_G_CCsplit

act_energies[2] = 34.6 + (-0.0044266 * (temperature - 298))

act_energies[3] = 35.9 + (-0.00020121 * (temperature - 298))

act_energies[4] = 44.3 + (0.0010060 * (temperature - 298))

act_energies[5] = 30.5 + (-0.0024145 * (temperature - 298))

act_energies[6] = delta_G_CCsplit + 9.8 + (0.041650 * (temperature - 298))

act_energies[7] = 26.4 + (0.0 * (temperature - 298))

act_energies[8] = 55.4 + (0.0 * (temperature - 298))

#### Calculate rates

for i in range(len(act_energies)):

if i == 8:

rates[i] = prefactor2 * math.exp(-act_energies[i] / (gas_constant * temperature))

else:

rates[i] = prefactor1 * math.exp(-act_energies[i] / (gas_constant * temperature))

rates[0] *= conc_array[-1][0]

rates[1] *= conc_array[-1][1]

rates[2] *= conc_array[-1][1] * 2 # Either side of active bond can react to release TFE

rates[3] *= conc_array[-1][1]

rates[4] *= conc_array[-1][2]

rates[5] *= conc_array[-1][2]

rates[6] *= conc_array[-1][0]

rates[7] *= conc_array[-1][3]

rates[8] *= conc_array[-1][3]

#### Calculate change rates for each component

changes_array.append([])

changes_array[-1].append(-rates[0] + rates[1] - rates[2] - rates[3] + rates[4] - rates[5] - rates[6] + rates[7])

changes_array[-1].append(rates[0] - rates[1] - rates[2] - rates[3] + rates[4])

changes_array[-1].append(rates[3] - rates[4] - rates[5])

changes_array[-1].append(rates[6] - rates[7] - rates[8])

changes_array[-1].append(rates[2])

changes_array[-1].append(rates[5])

changes_array[-1].append(rates[8])

#### Calculate change factors (max time step that does not result in negative concentrations)

for i in range(len(changes_array[-1])):

if changes_array[-1][i] < 0:

change_factors[i] = -conc_array[-1][i] / changes_array[-1][i]

else:

change_factors[i] = big_time_step

#### Change concentrations

#### Use large time steps occasionally to speed of model and small time steps to re-establish equilibrium

if jump_flag == True:

time_step = min(big_time_step, min(change_factors))

else:

time_step = small_time_step

conc_array.append([])

for i in range(len(conc_array[-2]) - 2):

conc_array[-1].append(conc_array[-2][i] + changes_array[-1][i] * time_step)

time += time_step

jump_flag = False

#### Calculate rate of changes

for i in range(len(change_rates)):

if changes_array[0][i] == 0:

change_rates[i] = 1e6

else:

change_rates[i] = abs((changes_array[1][i] - changes_array[0][i]) / changes_array[0][i])

max_change_rate = max(change_rates[1:4])

#### Set jump flag if change rate is low enough

#### Also adjust small time step: increase when jump flag is set, decrease if rates are too high/equilibrium not re-establishing

if max_change_rate < 0.001 or num_cycles % force_interval == force_interval / 2:

jump_flag = True

small_time_step *= 1.05

clutch = 0

stall_count = 0

jump_count += 1

elif max_change_rate > 1.0 and max_change_rate > last_change_rate:

clutch += 1

else:

stall_count += 1

if clutch == clutch_limit:

small_time_step *= 0.95

clutch = 0

stall_count = 0

elif stall_count == stall_limit:

small_time_step *= 1.05

#### Update temperature

temperature = temperature_start + (time/60) * heating_rate

conc_array[-1].append(time)

conc_array[-1].append(temperature - 273.15)

#### Delete older values in these arrays to keep variable size manageable

del conc_array[0]

del changes_array[0]

#### Write results to output file

if num_cycles % record_interval == 0:

for item in act_energies:

outfile.write(str(item) + ",")

outfile.write(",")

for item in rates:

outfile.write(str(item) + ",")

outfile.write(",")

for item in changes_array[-1]:

outfile.write(str(item) + ",")

outfile.write(",")

for item in change_rates:

outfile.write(str(item) + ",")

outfile.write(",")

outfile.write(str(max_change_rate) + ",")

outfile.write(str(time_step) + ",")

outfile.write(str(jump_count) + ",")

outfile.write("\n")

if num_cycles % record_interval2 == 0:

print(num_cycles, conc_array[-1][0], temperature - 273.15, jump_count)

num_cycles += 1

#

# End main loop

#

outfile.close()