Table 1. Optimization of the Hantzsch four-component reaction for the synthesis of 6a catalyzed by Cs/ECH-TMA (1).a

| Yield (%) | Time (min) | Temperature (0C) | Solventb | Catalyst loading (mg) | Entry |
| --- | --- | --- | --- | --- | --- |
| 25 | 180 | Reflux | EtOH | - | 1 |
| 30 | 120 | Reflux | EtOH | 20c | 2 |
| 97 | 30 | Reflux | EtOH | 20 | 3 |
| 97 | 30 | Reflux | EtOH | 15 | 4 |
| 96 | 35 | Reflux | EtOH | 10 | 5 |
| 88 | 35 | Reflux | EtOH | 7 | 6 |
| 82 | 25 | Reflux | EtOH | 10 | 7 |
| 74 | 90 | 50 | H2O | 10 | 8 |
| 35 | 100 | rt | EtOH | 10 | 9 |
| 75 | 50 | Reflux | H2O | 10 | 10 |
| 70 | 50 | 110 | - | 10 | 11 |
| 78 | 80 | 50 | EtOH/H2O (1:1) | 10 | 12 |
| 65 | 90 | Reflux | CH3CN | 10 | 13 |
| 67 | 70 | 100 | DMSO | 10 | 14 |
| 54 | 80 | Reflux | EtOAc | 10 | 15 |
| 60 | 100 | Reflux | THF | 10 | 16 |
| 45 | 110 | 60 | - | 10 | 17 |
| 86 | 50 | Reflux | EtOH/H2O (1:1) | 10 | 18 |

aReaction conditions: Dimedone (3, 1 mmol), ethyl acetoacetate (4, 1 mmol), 4-chlorobenzaldehyde (2a, 1 mmol), ammonium acetate (5, 1.2 mmol), Cs/ECH-TMA (1), and solvent (2 mL). bIsolated yields. cCommercial chitosan (MW = 600,000 – 800,000 Dalton) without any post-modification was used as catalyst.

Table 2. Synthesis of PHQ derivatives 6a-n from different aldehydes 2a-n catalyzed by Cs/ECH-TMA (1) under optimized conditions.a

| M.P/Rep. (oC) | M.P/Obs. (oC) | Yield (%) | Time (min) | Product 6 | Aldehyde 2 | Entry |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 244-246 85 | 241-243 | 96 | 35 | 6a | 4-Chlorobenzaldehyde (2a) |  | 1 |
| 240-243 86 | 240-242 | 94 | 35 | 6b | 2,4-Dichlorobenzaldehyde (2b) |  | 2 |
| 240-242 87 | 240-242 | 82 | 45 | 6c | 4-Nitrobenzaldehyde (2c) |  | 3 |
| 210-212 88 | 210-212 | 90 | 45 | 6d | 4-Hydroxy-3-methoxybenzaldehyde (2d) |  | 4 |
| 177-178 88 | 178-180 | 77 | 50 | 6e | 3-Nitrobenzaldehyde (2e) |  | 5 |
| 183-185 89 | 183-184 | 96 | 35 | 6f | 4-Florobenzaldehyde (2f) |  | 6 |
| 203-204 90 | 202-204 | 92 | 30 | 6g | Benzaldehyde (2g) |  | 7 |
| 210-212 91 | 206-208 | 90 | 35 | 6h | 2-Chlorobenzaldehyde (2h) |  | 8 |
| 253-256 86 | 250-252 | 84 | 35 | 6i | 4-Methoxybenzaldehyde (2i) |  | 9 |
| 229-232 92 | 228-230 | 86 | 35 | 6j | 4-Hydorxybenzaldehyde (2j) |  | 10 |
| 258-260 88 | 260-263 | 90 | 40 | 6k | 4-Methylbenzaldehyde (2k) |  | 11 |
| 252-254 88 | 253-255 | 92 | 35 | 6l | 4-Bromobenzaldehyde (2l) |  | 12 |
| 246-248 93 | 244-246 | 94 | 35 | 6m | Furfural (2m) |  | 13 |
| 173-174 94 | 173-175 | 95 | 35 | 6n | Formaldehyde (2n) |  | 14 |

aReaction conditions: Ethyl acetoacetate (4, 1 mmol), aldehyde (2, 1 mmol), NH4OAc (5, 1.2 mmol), dimedone (3, 1 mmol) and Cs/ECH-TMA(1, 10 mg) in EtOH (2 mL) under reflux conditions. bAll products are known compounds and their structures were established from their spectral data and melting points as compared with authentic samples or literature values.

Table 3. Synthesis of PHA derivatives 5a-l from different aldehydes 2a-l catalyzed by Cs/ECH-TMA (1) under optimized conditions.a

| M.P/Rep. (oC) | M.P/Obs. (oC) | Yield (%) | Time (min) | Product 7 | Aldehyde 2 | Entry |
| --- | --- | --- | --- | --- | --- | --- |
| 303-305 95 | 306-308 | 95 | 25 | 5a | 4-Chlorobenzaldehyde (2a) | 1 |
| 321 96 | 319-322 | 94 | 25 | 5b | 2,4-Dichlorobenzaldehyde (2b) | 2 |
| 302-305 97 | 301-303 | 84 | 40 | 5c | 4-Nitrobenzaldehyde (2c) | 3 |
| 295-298 98 | 293-296 | 88 | 35 | 5d | 4-Hydroxy-3-methoxybenzaldehyde (2d) | 4 |
| 294-296 99 | 292-294 | 80 | 40 | 5e | 3-Nitrobenzaldehyde (2e) | 5 |
| 246-248 100 | 246-248 | 96 | 25 | 5f | 4-Florobenzaldehyde (2f) | 6 |
| 189-191 100 | 190-191 | 92 | 25 | 5g | Benzaldehyde (2g) | 7 |
| 221-222 101 | 222-224 | 92 | 25 | 5h | 2-Chlorobenzaldehyde (2h) | 8 |
| 296-298 102 | 295-297 | 86 | 25 | 5i | 4-Methoxybenzaldehyde (2i) | 9 |
| >300 103 | 303-305 | 87 | 25 | 5j | 4-Hydorxybenzaldehyde (2j) | 10 |
| >300 103 | 300-302 | 89 | 25 | 5k | 4-Methylbenzaldehyde (2k) | 11 |
| 252-254 104 | 253-255 | 90 | 25 | 5l | 2-Bromobenzaldehyde (2l) | 12 |

aReaction conditions: Dimedone (3, 2 mmol), aryl aldehydes (2, 1 mmol), ammonium acetate (5, 1.2 mmol) and the Cs/ECH-TMA (1, 10 mg) in EtOH under reflux conditions. bAll products are known and their structures were established from their spectral data and melting points compared to authentic samples or literature values. cIsolated yields were reported.

Table 4. Comparison of the catalytic efficiency of Cs/ECH-TMA (1) with other heterogeneous or homogeneous catalysts for the synthesis of 6a.

| Entry | Catalyst | Catalyst loading | Solvent | Temp. oC | Time (min) | Yield (%) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Co3O4-CNTs | 30 mg | EtOH | Reflux | 35 | 97 | 105 |
|  | Vitamin-B1 | 20 mol% | EtOH | Reflux | 60 | 90 | 106 |
|  | Fe(HSO4)3/SiO2 | 10 mol% | EtOH | 80 | 60 | 95 | 107 |
|  | FeF3 | 5 mol% | EtOH | Reflux | 60 | 92 | 108 |
|  | Al2(SO4)3 | 10 mol% | EtOH | Reflux | 300 | 87 | 109 |
|  | Cs/ECH-TMA | 10 mg | EtOH | Reflux | 35 | 96 | This Work |