Mild activation strategy for porous carbon materials: using Sodium bicarbonate and Potassium bicarbonate as activators for high-performance supercapacitors

Zixuan Zhang, Yuzhuo Luzhang, Zhentao Bian*, Yu Jia, Dandan Shen, Xusheng Xie, Na Zhang*

Bio-based Functional Materials and Composite Technology Research Center, Anhui Key Laboratory of Spin Electron and Nanomaterials (Cultivating Base), Suzhou University, Suzhou 234000, Anhui Province, P.R. China

*Corresponding author:

zhentaobian@126.com (Zhentao Bian)

szxyzn@163.com (Na Zhang)

Fig. S1 Specific capacitances of CC-C/Na/K-1:2:1 calculated from CV curves.

Fig. S2 (a) GCD curves of CC at different current densities (b) CV curves of CC at different scan rates

Fig. S3 (c) GCD curves of CC-C/Na/K-1:1.5:1.5 at different current densities (d) CV curves of CC-C/Na/K-1:1.5:1.5 at different scan rates

Fig. S4 (e) GCD curves of CC-C/Na/K-1:1:2 at different current densities (f) CV curves of CC-C/Na/K-1:1:2 at different scan rates

Fig. S5 (g) GCD curves of CC-C/Na-1:3 at different current densities (h) CV curves of CC-C/Na-1:3 at different scan rates

Fig. S6 (i) GCD curves of CC-C/K-1:3 at different current densities (j) CV curves of CC-C/K-1:3 at different scan rates

Fig. S7 Storage contributions from capacitive process and diffusion-controlled process for CC-C/Na/K-1:2:1 at varied scan rates.

Table S1 Pore structure parameters of the samples

| Sample | SBET (m2 g-1) | Smicro (m2 g-1) | Vmicro (cm3 g-1) | Vtol (cm3 g-1) |
| --- | --- | --- | --- | --- |
| CC | 3.5 | 0 | - | - |
| CC-C/Na/K-1:1.5:1.5 | 107.6 | 99.2 | 0.04 | 0.05 |
| CC-C/Na/K-1:1:2 | 164.4 | 139.6 | 0.07 | 0.08 |
| CC-C/Na-1:3 | 470.9 | 380.8 | 0.20 | 0.25 |
| CC-C/Na/K-1:2:1 | 688.2 | 669.9 | 0.35 | 0.37 |