Supporting Information

Hydrogen Bonding-Driven Structural and Mechanical Regulation of Poly(ε-caprolactone)-Based Polyurethane with Poly(glycolic acid)

# Han Wu1, Wenjie Pan2, Yuan Gao2, Mingyang Wang2, Zhenbo Ning2, Ni Jiang2*

1 China Institute of Atomic Energy. Beijing 102413, China

2 Beijing Laboratory of Biomedical Materials, State Key Laboratory of Organic-Inorganic Composites, College of Life Science and Technology, Beijing University of Chemical Technology, Beijing 100029, China

Fig. S1. The in situ FTIR spectra of (a,b) PU and (c,d) 10PUGA from 30oC to 220oC.

Fig. S2. The Lorentz-corrected SAXS profiles of PU and PUGAs.

Fig. S3. SEM images of tensile-fractured surfaces of (a) PU and (b) 10PUGA.

Table S1. The qmax and long period (L) of PU and PUGAs

| Sample | qmax (nm-1) | L (nm) |
| --- | --- | --- |
| PU | 0.465 | 13.5 |
| 5PUGA | 0.563 | 11.2 |
| 10PUGA | 0.540 | 11.6 |
| 20PUGA | 0.507 | 12.4 |

Table S2. Thermal properties of PU and PUGAs

| Sample | Tc(PCL) (°C) | ΔHc(PCL) (J/g) | Tm(PCL) (°C) | ΔHm(PCL) (J/g) | Tm(PGA) (°C) |
| --- | --- | --- | --- | --- | --- |
| PU | 1.9 | 28.3 | 43.5 | 28.6 | - |
| 5PUGA | -4.6 | 26.3 | 43.1 | 27.4 | - |
| 10PUGA | -5.6 | 25.5 | 39.9 | 25.6 | 200.1 |
| 20PUGA | -10.8 | 22.4 | 35.9 | 23.0 | 199.9 |

Table S3. Mechanical properties of PU and PUGAs

| Sample | Tensile strength (MPa) | Elongation at break (%) | Tensile toughness (MJ·m-3) |
| --- | --- | --- | --- |
| PU | 17.7±1.8 | 832.3±77.6 | 109.1±16.6 |
| 5PUGA | 26.0±5.7 | 1090.6±136.3 | 164.3±42.1 |
| 10PUGA | 54.1±4.8 | 1389.0±45.4 | 329.0±36.7 |
| 20PUGA | 43.3±0.1 | 1191.7±70.6 | 245.2±13.3 |