Supplementary Material

Eco-Conscious Synthesis of a Starch-Magnetic Hydrogel for Effective Methylene Blue Decontamination in Wastewater Treatment

Anibal Alviz-Meza1; Silvia Álvarez-Torrellas2*; Ysabel Huaccallo-Aguilar3; María Verónica Carranza-Oropeza4; Juan Manuel Garrido-Zoido5; María Victoria Gil5; Juan García2

1Escuela de posgrado, Universidad Continental, Lima, Peru;

2Catalysis and Separation Processes Group (CyPS), Chemical Engineering and Materials Department, Faculty of Chemical Sciences, Complutense University of Madrid, Avda. Complutense s/n, 28040 Madrid, Spain;

3Clean Water Technology Lab (CLEWATEC), Institute of Fluid Dynamics, Helmholtz-Zentrum Dresden-Rossendorf, Bautzner Landstraße 400, 01328 Dresden, Germany;

4Departamento de Química e Ingeniería Química, Facultad de Química e Ingeniería Química, Universidad Nacional Mayor de San Marcos, Lima, Peru;

5Department of Organic and Inorganic Chemistry, Faculty of Sciences, and Green Chemistry and Sustainable Development Unit (IACYS), University of Extremadura, 06006 Badajoz, Spain.

*Corresponding author: Silvia Alvarez-Torrellas (satorrellas@ucm.es)

Supplementary Material content

Figure S1. Photographs showing: (a) magnetic response of the hydrogel immersed in a MB aqueous solution; (b) supernatant magnetite separated from the hydrogel composite after magnetic decantation; and (c) wet hydrogel after magnetic separation and washing with ultrapure water.

Table S1. Cartesian coordinates for optimized structure of methylene blue cation (MB+) at MN12-SX/aug-cc-pVTZ level, with the SMD solvation model; solvent = water.

Table S2. Energetic data, electronic parameters and chemical descriptors for optimized structure of methylene blue cation (MB+) at MN12-SX/aug-cc-pVTZ level, with the SMD solvation model; solvent = water.

Figure S1. Photographs showing: (a) magnetic response of the hydrogel immersed in a MB aqueous solution; (b) supernatant magnetite separated from the hydrogel composite after magnetic decantation; and (c) wet hydrogel after magnetic separation and washing with ultrapure water.

Table S1. Cartesian coordinates for optimized structure of methylene blue cation (MB+) at MN12-SX/aug-cc-pVTZ level, with the SMD solvation model; solvent = water.

ATOM TYPE               x             y             z_____

C                  3.58696200   -1.41390700   -0.00001100

C                  3.76471200    0.00595200   -0.00001900

C                  2.61236100    0.82342100   -0.00001200

C                  1.35867200    0.26476800   -0.00001400

C                  1.16999600   -1.15253000   -0.00001800

C                  2.34538600   -1.95229700   -0.00001300

S                  0.00000000    1.33440300   -0.00001100

C                 -1.35867200    0.26476800   -0.00001600

C                 -1.16999600   -1.15253100   -0.00002000

N                  0.00000000   -1.77909100   -0.00001900

C                 -2.61236100    0.82342100   -0.00001000

C                 -3.76471200    0.00595200   -0.00002000

C                 -3.58696200   -1.41390700   -0.00001300

C                 -2.34538600   -1.95229800   -0.00001600

N                 -4.99089400    0.53898000   -0.00003400

N                  4.99089400    0.53898000   -0.00003000

C                  5.16704100    1.97744700    0.00004500

C                  6.16906600   -0.30748100    0.00003100

C                 -6.16906600   -0.30748100    0.00007900

C                 -5.16704000    1.97744700    0.00002900

H                  4.45129400   -2.06628500    0.00000100

H                  2.71010300    1.90283700   -0.00000800

H                  2.21024600   -3.03029300   -0.00000600

H                 -2.71010300    1.90283700    0.00000600

H                 -4.45129500   -2.06628500   -0.00000500

H                 -2.21024600   -3.03029300   -0.00001200

H                  4.71453500    2.43259100   -0.88779700

H                  4.71462100    2.43249400    0.88798200

H                  6.23075200    2.20529000    0.00000200

H                  6.20082500   -0.94693600    0.88850200

H                  6.20080300   -0.94708600   -0.88832900

H                  7.05494400    0.32388900   -0.00003800

H                 -7.05494400    0.32389000    0.00004600

H                 -6.20084200   -0.94708700   -0.88828000

H                 -6.20078700   -0.94693400    0.88855200

H                 -4.71446500    2.43259000   -0.88777700

H                 -6.23075100    2.20529100   -0.00009800

H                 -4.71468800    2.43249500    0.88800200

Table S2. Energetic data, electronic parameters and chemical descriptors for optimized structure of methylene blue cation (MB+) at MN12-SX/aug-cc-pVTZ level, with the SMD solvation model; solvent = water.

| Descriptor* | Value | Unit | Formula of electronic parameters |
| --- | --- | --- | --- |
| Electronic energy | −741981.7 | kcal/mol |  |
| Free energy | −741813.6 | kcal/mol |  |
| Enthalpy | −741772.3 | kcal/mol |  |
| Entropy | 138.5 | cal/(mol·K) |  |
| EHOMO | −5.66 | eV |  |
| ELUMO | −3.58 | eV |  |
| Egap | 2.08 | eV |  |
| EFL | −4.62 | eV |  |
| IP | 5.66 | eV |  |
| EA | 3.58 | eV |  |
| η | 1.04 | eV |  |
| S | 0.96 | eV |  |
| μ | −4.62 | eV |  |
| ω | 10.26 | eV−1 |  |

*Energetic data, Energy gap (Egap), Fermi level (EFL), ionization potential (IP), electron affinity (EA), global hardness (η), global softness (S), chemical potential (μ) and electrophilicity index (ω).