Supplementary Information for

The role of chalcogen vacancies for atomic defect emission in MoS2

Elmar Mitterreiter1,2, Bruno Schuler3,4, Katja Barthelmi1,2, Katherine A. Cochrane3, Jonas Kiemle1,2, Florian Sigger1,2, Julian Klein1,5, Edward Wong3, Edward S. Barnard3, Sivan Refaely-Abramson6, Diana Y. Qiu7, Michael Lorke8,9, Frank Jahnke9, Kenji Watanabe10, Takashi Taniguchi11, Johnathan J. Finley1,2, Adam M. Schwartzberg3, Alexander W. Holleitner1,2*, Alexander Weber-Bargioni3§, Christoph Kastl1,2#

1 – Walter Schottky Institut and Physics Department, Technical University of Munich, Am Coulombwall 4a, 85748 Garching, Germany

2 – Munich Center for Quantum Science and Technology (MCQST), Schellingstrasse 4, 80799 München, Germany

3 – Molecular Foundry, Lawrence Berkeley National Laboratory, 1 Cyclotron Road, Berkeley, CA 94720, United States

4 – nanotech@surfaces Laboratory, Empa – Swiss Federal Laboratories for Materials Science and Technology, 8600 Dübendorf, Switzerland

5 – Department of Materials Science and Engineering, Massachusetts Institute of Technology, Cambridge, MA 02139, United States

6 – Department of Materials and Interfaces, Weizmann Institute of Science, Rehovot, Israel

7 – Department of Mechanical Engineering and Materials Science, Yale University, New Haven, CT, USA

8 – Bremen Center for Computational Materials Science, University of Bremen, Am Fallturm 1, 28359 Bremen, Germany

9 – Bremen Institute for Theoretical Physics, University of Bremen, Otto-Hahn-Allee 1, 28359 Bremen, Germany

10 – Research Center for Functional Materials, National Institute for Materials Science, 1-1 Namiki, Tsukuba 305-0044, Japan

11 – International Center for Materials Nanoarchitectonics, National Institute for Materials Science, 1-1 Namiki, Tsukuba 305-0044, Japan

*holleitner@wsi.tum.de

§ afweber-bargioni@lbl.gov

#christoph.kastl@wsi.tum.de

S1: Schematic of in-vacuo annealing. a) Microscope image of a sample consisting of bottom hBN (b-hBN), MoS2 , and top hBN (t-hBN) on SiO2. A and B represent the resulting fully, and half-encapsulated MoS2 heterostructure, respectively. b) Schematic measurement setup showing a modified optical cryostat with integrated heater enabling in-vacuo high-temperature annealing (up to Tannealing  900 K) and successive low-temperature PL measurements (Tsample  20 K). c) Temperature profile of the entire PL study. The red-shaded areas highlight the temperature profile during the annealing processes. Upon reaching the desired annealing temperature, the latter was maintained constant for 30 minutes. The blue-shaded areas represent the low-temperature PL measurements.

S2: Annealing temperature dependent evolution of low-temperature PL spectra. a) PL spectra of fully encapsulated pristine MoS2, and after annealing to 420 K, 450 K, 510 K, 600 K, 700 K, 800 K, 900 K, and again 900 K. Pristine MoS2 exhibits a broad emission peak, which is strongly reduced after mild annealing. A single emission peak appears and its intensity increases with rising annealing temperature. The intensity of the single emission peak decreases after annealing to 900 K and the PL disappears after a subsequent annealing step to 900 K (gray). b) PL spectra of pristine MoS2 on h-BN, and after annealing to 420 K, 450 K, 510 K, 600 K, 700 K, and 800 K. A similar behavior to fully encapsulated MoS2 occurs. However, lower annealing temperatures of about 700 K already reduce the intensity of single emission line before it vanishes at 800 K.

S3: Laser power dependent PL of fully encapsulated MoS2 after annealing to 800 K. a) Power dependent PL spectra. Curves are offset for clarity. b) Power dependent integrated intensity of the neutral exciton (XA) (red) and the single emission line XL (blue). We do not observe a laser power dependent saturation for the emission of the exciton. However, the defect emission line exhibits a saturating behavior, which we can be fitted by I ∝ PP + PSat. The turnover for saturation where P = Psat occurs at approximately 50 µW.

S4: STM overview image of single layer MoS2 on graphene/SiC after mild annealing. Within our experimental statistics, the only observed defects are oxygen passivated sulfur top and bottom vacancies. The bright spots correspond to adsorbed molecules on the MoS2 surface.

S5: Low-temperature PL spectrum of homogeneously He-ion irradiated single-layer MoS2 on graphene/SiC. The He-ion dose was 5·1014 cm-2. The defect emission is absent due to quenching from the underlying graphene substrate.

S6: Details of DFT calculations for defect orbitals in MoS2 with sulfur vacancies

DFT calculations were performed using the Vienna Ab initio Simulation Package, Vasp 5.4.41,2, using the projector augmented wave method and treating the semi-core d-states as part of the valence shell in the PBE variant of the generalized gradient approximation3. For defect calculations, 9x9 supercells, consisting of 243 atoms were used with the experimental lattice constant, applying the G-point approximation. The defect geometries were fully relaxed. A 450eV (900eV) cutoff was applied for the expansion of the wave functions (charge density).

S7: Details of GW-BSE calculations for absorbance spectra of MoS2 with sulfur vacancies

We first performed density functional theory (DFT) calculations within the local density approximation (LDA) using the Quantum-ESPRESSO code4. The calculations were done on a 5×5 supercell arrangement of a MoS2 monolayer with one S vacancy, following prior work5. We used a plane-wave basis and norm-conserving pseudopotentials with a 125 Ry plane-wave cutoff. We included the Mo semi-core 4d, 4p, 4s, 5s and 5p states as valence states in our pseudopotential. The distance between repeated supercells in the out-of-plane direction was 15 Å. We relaxed the geometry within DFT and used DFT charge density as a starting point for our GW and Bethe Salpeter equation (GW-BSE) calculations. Our GW calculations are performed with the BerkeleyGW code6 using the generalized plasmon-pole model7, an energy cutoff of 25 Ry for the planewave components of the dielectric matrix, and a nonuniform k-point sampling corresponding to a 30×30 uniform k-grid. We included 4,000 unoccupied states in the sum over empty states in the self-energy and polarizability and tested the convergence with respect to unoccupied states by comparing to a calculation using up to 20,000 effective states obtained by averaging high-energy states within a small energy window. We find that these parameters converge the relative quasiparticle energies for the defect and pristine states at the K point to within 100 meV. The BSE was also solved with the BerkeleyGW code6,8. We diagonalize the BSE Hamiltonian within the Tamm-Dancoff approximation with 10 valence and 10 conduction bands. The clustered sampling interpolation (CSI) scheme9 was used to interpolate a nonuniform k point sampling to a uniform k-grid of 18×18×1 k points. A 5 Ry cutoff was used for the planewave components of the dielectric matrix used in the BSE. Spin orbit coupling was added as a perturbation. We find that these parameters converge the calculated exciton excitation energies up to 200 meV.

Supplemental References

1.	Kresse, G. & Furthmüller, J. Efficiency of ab-initio total energy calculations for metals and semiconductors using a plane-wave basis set. Comput. Mater. Sci. 6, 15–50 (1996).

2.	Kresse, G. & Furthmüller, J. Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys. Rev. B 54, 11169–11186 (1996).

3.	Perdew, J. P., Burke, K. & Ernzerhof, M. Generalized Gradient Approximation Made Simple. Phys. Rev. Lett. 78, 1396–1396 (1997).

4.	Giannozzi, P. et al. QUANTUM ESPRESSO: a modular and open-source software project for quantum simulations of materials. J. Phys. Condens. Matter 21, 395502 (2009).

5.	Refaely-Abramson, S., Qiu, D. Y., Louie, S. G. & Neaton, J. B. Defect-Induced Modification of Low-Lying Excitons and Valley Selectivity in Monolayer Transition Metal Dichalcogenides. Phys. Rev. Lett. 121, 167402 (2018).

6.	Deslippe, J. et al. BerkeleyGW: A massively parallel computer package for the calculation of the quasiparticle and optical properties of materials and nanostructures. Comput. Phys. Commun. 183, 1269–1289 (2012).

7.	Hybertsen, M. S. & Louie, S. G. Electron correlation in semiconductors and insulators: Band gaps and quasiparticle energies. Phys. Rev. B 34, 5390–5413 (1986).

8.	Rohlfing, M. & Louie, S. G. Electron-Hole Excitations in Semiconductors and Insulators. Phys. Rev. Lett. 81, 2312–2315 (1998).

9.	da Jornada, F. H., Qiu, D. Y. & Louie, S. G. Nonuniform sampling schemes of the Brillouin zone for many-electron perturbation-theory calculations in reduced dimensionality. Phys. Rev. B 95, 035109 (2017).