Four Novel Metal Complex Borates: Syntheses, Crystal Structures, and ORR Electrocatalysis

Bo-Wei Liao1, Zhen-Ping Liao1, Xiao-Ting Zhang1 and Chun-Yang Pan1*

1School of Light Industry and Chemical Engineering, Guangdong University of Technology, Guangzhou, Guangdong, 510006, China; *Corresponding author: Chun-Yang Pan, Tel: +86-020-39322231; panchuny@gdut.edu.cn.

Electrochemical characterization

A carbon rod and Hg/HgO electrode were used as the counter electrode and reference electrode, respectively. All the potential of the reference electrode was converted to reversible hydrogen energy (RHE) by using the following equation:

E(vs. RHE) = E(Hg/HgO) + E0Hg/HgO,0.098V + 0.0591*(pH).

Linear sweep voltammetry (LSV) polarization curves were recorded in O2-saturated 0.1 M KOH, scanning from 0.2 V to 1.1 V (vs. RHE) at a rate of 5 mV s−1, with rotation rates incrementing from 400 rpm to 1600 rpm.

Table. S1 Crystal Data of 1 and 2,

| Compound | 1 | 2 |
| --- | --- | --- |
| Empirical formula | [Ni(Ac)(bpy)2]2·[B5O6(OH)4]·py | [CuCl(bpy)2]·[B5O6(OH)4] |
| Formula weight | 727.30 | 629.44 |
| Temperature/K | 150.0 | 150.0 |
| Crystal system | triclinic | triclinic |
| Space group | P-1 | P-1 |
| a/Å | 9.7077(2) | 9.1171(4) |
| b/Å | 12.9884(5) | 11.7003(4) |
| c/Å | 14.5148(6) | 12.4734(5) |
| α/° | 111.0980(10) | 77.2050(10) |
| β/° | 95.4710(10) | 77.9430(10) |
| γ/° | 108.0020(10) | 79.7020(10) |
| V/Å3 | 1591.02(11) | 1256.60(9) |
| Z | 2 | 2 |
| Dc/g cm-3 | 1.518 | 1.664 |
| μ/mm-1 | 0.681 | 1.04 |
| F(000) | 748.0 | 638.0 |
| 2θ range for data collection/° | 4.502-52.882 | 4.458-52.958 |
| Index ranges | -12 ≤ h ≤ 12, -16 ≤ k ≤ 16, -18 ≤ l ≤ 18 | -11 ≤ h ≤ 11, -14 ≤ k ≤ 14, -15 ≤ l ≤ 15 |
| Reflections collected | 40081 | 37381 |
| Independent reflections | 6533 [Rint = 0.0495, Rsigma = 0.0341] | 5178 [Rint = 0.0275, Rsigma = 0.0160] |
| Data/restraints/parameters | 6533/0/456 | 5178/0/374 |
| Goodness-of-fit on F2 | 1.023 | 1.054 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0349, wR2 = 0.0763 | R1 = 0.0261, wR2 = 0.0700 |
| Final R indexes [all data] | R1 = 0.0526, wR2 = 0.0829 | R1 = 0.0310, wR2 = 0.0725 |

R1 = Σ||Fo| − |F||/Σ|Fo| and wR2 = [Σw (Fo2 – Fc2) 2 /ΣwFo4] 1/2

Table. S2 Crystal Data of 3 and 4,

| Compound | 3 | 4 |
| --- | --- | --- |
| Empirical formula | [Co(Me3tacn)]·[B6O7(OH)6]·11H2O | [Ga(Cyclen)B2O3(OH)2]·[B5O6(OH)4] |
| Formula weight | 707.30 | 563.72 |
| Temperature/K | 150.0 | 150.0 |
| Crystal system | triclinic | triclinic |
| Space group | P-1 | P-1 |
| a/Å | 9.1977(15) | 8.9585(13) |
| b/Å | 11.1388(19) | 9.7999(14) |
| c/Å | 16.013(3) | 12.979(2) |
| α/° | 98.096(5) | 82.038(4) |
| β/° | 95.858(5) | 81.153(4) |
| γ/° | 102.487(5) | 82.512(4) |
| V/Å3 | 1570.8(5) | 1108.1(3) |
| Z | 2 | 2 |
| Dc/g cm-3 | 1.495 | 1.689 |
| μ/mm-1 | 0.639 | 1.321 |
| F(000) | 746.0 | 576.0 |
| 2θ range for data collection/° | 4.944 to 56.576 | 4.224 to 50.35 |
| Index ranges | -12 ≤ h ≤ 10, -14 ≤ k ≤ 14, -21 ≤ l ≤ 21 | -10 ≤ h ≤ 10, -11 ≤ k ≤ 11, -15 ≤ l ≤ 15 |
| Reflections collected | 28639 | 3941 |
| Independent reflections | 7687 [Rint = 0.0562, Rsigma = 0.0824] | 3941 [Rint = 0.0833, Rsigma = 0.0679] |
| Data/restraints/parameters | 7687/23/439 | 3941/0/323 |
| Goodness-of-fit on F2 | 1.039 | 1.059 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0694, wR2 = 0.1301 | R1 = 0.0845, wR2 = 0.2285 |
| Final R indexes [all data] | R1 = 0.1322, wR2 = 0.1589 | R1 = 0.1143, wR2 = 0.2484 |

R1 = Σ||Fo| − |F||/Σ|Fo| and wR2 = [Σw (Fo2 – Fc2) 2 /ΣwFo4] 1/2

Table. S3 H-Bs for 1.

| D–H···A | d(D–H) (A˚) | d(H···A) (Å) | d(D···A) (Å) | ∠D—H···A () |
| --- | --- | --- | --- | --- |
| O12–H12A···O21 | 0.84 | 2.06 | 2.8438(19) | 155.5 |
| O5–H5A···O62 | 0.84 | 1.90 | 2.7338(19) | 175.1 |
| O10–H10A···O83 | 0.84 | 1.98 | 2.810(2) | 171.2 |
| O3–H3A···O1 | 0.84 | 1.89 | 2.724(2) | 169.8 |

- 12-X,1-Y,1-Z; 2-X,-Y,1-Z; 31-X,-Y,1-Z

Table. S4 H-Bs for 2.

| D–H···A | d(D–H) (A˚) | d(H···A) (Å) | d(D···A) (Å) | ∠D—H···A () |
| --- | --- | --- | --- | --- |
| O10–H10···O15 | 0.84 | 1.98 | 2.739(3) | 163.4 |
| O22–H22···O191 | 0.84 | 1.88 | 2.788(3) | 165.0 |
| O5–H5···O1 | 0.84 | 1.98 | 2.696(2) | 163.6 |
| O3–H3A···O62 | 0.84 | 1.91 | 2.788(3) | 169.9 |
| O12–H12A···O93 | 0.84 | 1.88 | 2.788(3) | 170.9 |
| O13–H13A···O164 | 0.84 | 1.92 | 2.788(3) | 171.3 |

12-X, 1-Y, 1-Z; 21-X, 1-Y,2-Z; 32-X, 1-Y,2-Z; 41-X, 1-Y, 1-Z

Table. S5 H-Bs for 3.

| D–H···A | d(D–H) (A˚) | d(H···A) (Å) | d(D···A) (Å) | ∠D—H···A () |
| --- | --- | --- | --- | --- |
| O1–H1···O14 | 0.866(9) | 1.968(10) | 2.834(5) | 178(4) |
| O2–H2···O23 | 0.865(8) | 1.956(9) | 2.818(4) | 173.4(19) |
| O3–H3···O18 | 0.873(9) | 1.936(11) | 2.806(4) | 174(4) |
| O4–H4···O17 | 0.74(3) | 1.95(3) | 2.683(5) | 169(5) |
| O7–H7···O20 | 0.84 | 1.88 | 2.719(5) | 174.5 |
| O14–H14A···O15 | 0.87 | 2.01 | 2.787(6) | 148.5 |
| O14–H14B···O191 | 0.87 | 2.03 | 2.891(7) | 171.1 |
| O15–H15B···O242 | 0.87 | 2.17 | 2.891(6) | 140.2 |
| O16–H16B···O83 | 0.87 | 2.07 | 2.836(4) | 146.0 |
| O17–H17B···O16 | 0.87 | 1.94 | 2.741(6) | 153.1 |
| O19–H19A···O7 | 0.87 | 1.92 | 2.785(5) | 169.7 |
| O20–H20A···O224 | 0.87 | 2.03 | 2.885(5) | 165.6 |
| O20–H20B···O21 | 0.87 | 1.97 | 2.834(6) | 170.0 |
| O23–H23B···O24 | 0.87 | 2.05 | 2.745(5) | 136.7 |
| O24–H24A···O125 | 0.87 | 1.95 | 2.817(4) | 171.5 |
| O24–H24B···O10 | 0.87 | 1.92 | 2.765(4) | 162.6 |

11+X,1+Y,+Z; 2+X,1+Y,+Z; 31-X,2-Y,1-Z; 4-X,-Y,1-Z; 51-X,1-Y,2-Z

Table. S6 H-Bs for 4.

| D–H···A | d(D–H) (A˚) | d(H···A) (Å) | d(D···A) (Å) | ∠D—H···A () |
| --- | --- | --- | --- | --- |
| O6–H6···O2 | 0.84 | 2.07 | 2.867(10) | 159.2 |
| O13–H13···O111 | 0.84 | 1.99 | 2.770(10) | 153.2 |
| O5–H5···O9 | 0.84 | 1.93 | 2.714(10) | 155.3 |
| O15–H15···O72 | 0.84 | 2.14 | 2.766(9) | 131.0 |
| O8–H8···O103 | 0.84 | 1.96 | 2.784(9) | 168.7 |

11-X,1-Y,-Z; 21+X,+Y,+Z; 31-X,-Y,-Z

Fig. S1 The FTIR spectra of a) 1, b) 2, c) 3 and d) 4.

Fig. S2 Experimental and Simulated Powder XRD patterns of a) 1, b) 2, c) 3 and d) 4.