Supporting Information to

Host-guest Encapsulation of Photosensitizer to Construct Antibacterial Silicon Rubber: Enhanced Homogeneity and Dual-action.

Jin Han1, Yaocheng Zhu1, Ziqiang Zhang1, Taolei Qiu1, Lei Wang1, Zhengping Zhao1, Xiaoxue Yin2, Dawei Zhang2, Kun Shen2,*, Dong Xu3, Boshi Yu3, Tongdong Shen4, Zhixiong Liu5

1)	State Key Laboratory of Advanced Separation Membrane Materials, Zhejiang Key Laboratory of Advanced Polymer Materials Modification and Application Technology, Zhejiang University of Technology, Hangzhou, 310014, PR China

2) Zhejiang Tongxuan Medical Technology Co., Ltd., Hangzhou, 317300, PR China

3) Polymer Research Institute, Wenzhou Gettel High-Tech Materials Co., Ltd, Wenzhou, 325802, PR China

4) Zhejiang Collaborative Innovation Center for Full-Process Monitoring and Green Governance of Emerging Contaminants, Interdisciplinary Research Academy, Hangzhou 310015, China

5) College of Chemistry and Chemical Engineering, Shanxi Datong University, Datong, 037009, PR China

Scheme S1 Synthetic route of MeHPEI, CCA and Am-HQAS nanocapsule host.

Table S1 The feeding ratios of the amphiphilic hyperbranched QAS Nanocapsules

| Sample | Quaternization degree (%) | MeHPEI (g) | CCA (g) |
| --- | --- | --- | --- |
| Am30-HQAS | 30 | 1.0 | 1.6865 |
| Am40-HQAS | 40 | 1.0 | 2.2487 |
| Am50-HQAS | 50 | 1.0 | 2.8109 |
| Am60-HQAS | 60 | 1.0 | 3.3730 |
| Am70-HQAS | 70 | 1.0 | 3.9352 |

Table S2 The Feeding ratios of the various silicone rubber

| Sample | PDMS (g) | Amx-HQAS (g) | KH-560 (g) | R812S (g) | TEOS (g) | DBTDL (g) |
| --- | --- | --- | --- | --- | --- | --- |
| RTV | 10 | / | 3.0 | / | / | 0.005 |
| RTV-Am30 | 10 | 1.23 (Am30-HQAS) | 3.0 | / | / | 0.005 |
| RTV-Am40 | 10 | 1.49 (Am40-HQAS) | 3.0 | / | / | 0.005 |
| RTV-Am50 | 10 | 1.74 (Am50-HQAS) | 3.0 | / | / | 0.005 |
| RTV-Am60 | 10 | 2.00 (Am60-HQAS) | 3.0 | / | / | 0.005 |
| RTV-Am70 | 10 | 2.26 (Am70-HQAS) | 3.0 | / | / | 0.005 |
| e-RTV | 10 | / | 0.2 | 0.5 | 1.5 | 0.005 |
| e-RTV-Am60 | 10 | 1.00 (Am60-HQAS) | 0.2 | 0.5 | 1.5 | 0.005 |
| e-RTV-Am60-RB | 10 | 1.20 (RB@Am60-HQAS) | 0.2 | 0.5 | 1.5 | 0.005 |

Fig. S1 A standard work curve of RB in ultrapure water (λ=540nm)

Fig. S2 A plot of encapsulating capability vs the RB concentration

Fig. S3 1H-NMR spectra of Amx-HQAS.

Fig. S4 The static water contact angle  (A)  and the contact angle images (B) of RTV and RTV-Amx.

Fig. S5 The static water contact angle  (A)  and the contact angle images (B) of e-RTV, e-RTV-Am60 and e-RTV-Am60-RB.

Fig. S6 The stress-strain diagram of the various silicone rubber samples.

Fig. S7 60% compressive stress-strain diagram of the various silicone rubber samples.

Fig. S8 The compressive stress-strain diagram of the various silicone rubber samples during the 10 loading-unloading cycles with 60% deformation (A: RTV, B: RTV-Am30, C: RTV-Am40, D: RTV-Am50, E: RTV-Am60, F: RTV-Am70).

Fig. S9 The compressive stress-strain diagram of the various silicone rubber samples during the 10 loading-unloading cycles with 60% deformation (A: e-RTV, B: e-RTV-Am60, C: e-RTV-Am60-RB).

Fig. S10 A) UV scanning spectrum of DPBF of e-RTV-Am60-RB under LED light irradiation; B) changing trend of intensity of characteristic absorption peak (410 nm) of DPBF of e-RTV-Am60-RB under LED light irradiation.

Fig. S11 (A) Confocal images of S. aureus adhered on the e-RTV, e-RTV-Am60 , e-RTV-Am60-RB and e-RTV-Am60-RB-Light samples; (B) Bacterial growth curve of S. aureus on the various silicone rubber before and after LED light irradiation; (C) The killing efficiency of the various silicone rubbers towards S. aureus before and after LED light irradiation

Fig. S12 Fluorescence image of the e-RTV-Am60, e-RTV-Am60-RB and e-RTV-Am60-RB-Light samples after culturing in S. aureus at regular time interval.