Table 1 - Proximate analysis of the initial hydrolysis lignin

| Parameter | Unit | Value |
| --- | --- | --- |
| Moisture content, Wa | % | 59,557 |
| External moisture | % | 12,167 |
| As-received moisture | % | 64,477 |
| Ash content on a dry basis, Aa | % | 0,346 |
| Ash content on an as-received basis, Ad | % | 0,140 |
| Volatile matter on a dry basis, Vd | % | 76,048 |
| Volatile matter on a dry ash-free basis, Vdaf | % | 76,312 |
| Higher heating value on an as-received basis | kJ/kg | 22957,32 |
| Lower heating value on an as-received basis | kJ/kg | 19919,20 |
| Lower heating value on a dry basis | kJ/kg | 21593,69 |

Table 2 - Ultimate analysis of the initial hydrolysis lignin

| Parameter | Unit | Value |
| --- | --- | --- |
| C | % | 46,3 |
| O | % | 45,7 |
| H | % | 5,51 |
| N | % | <0,1 |
| S | % | 1,19 |
| Ca | % | 0,853 |
| Si | % | 0,265 |
| Al | % | 0,153 |
| Fe | % | 0,020 |
| K | % | 0,012 |
| Mg | % | 0,013 |
| Cu | % | 0,004 |
| Ti | % | 0,004 |
| Mn | % | 0,002 |
| Cr | % | 0,001 |
| Zn | % | 0,001 |
| Sr | % | 0,001 |

Table 3 - Heating parameters of hydrolysis lignin in the vertical glass reactor

| T, °C | Sample | m1, g | m2, g | Δm, % | Ys, % | τh/τhold, min |
| --- | --- | --- | --- | --- | --- | --- |
| 200 | 5 g | 5,094 | 3,796 | 25,5 | 74,5 | 20/30 |
| 200 | 10 g | 10,003 | 9,307 | 7,0 | 93,0 | 20/30 |
| 200 | 15 g | 15,094 | 14,643 | 3,0 | 97,0 | 20/30 |
| 300 | 5 g | 5,047 | 3,524 | 30,2 | 69,8 | 30/30 |
| 300 | 10 g | 10,016 | 7,884 | 21,3 | 78,7 | 30/30 |
| 300 | 15 g | 15,057 | 12,312 | 18,2 | 81,8 | 30/30 |
| 400 | 5 g | 5,096 | 2,619 | 48,6 | 51,4 | 40/30 |
| 400 | 10 g | 10,064 | 5,302 | 47,3 | 52,7 | 40/30 |
| 400 | 15 g | 15,041 | 7,402 | 50,8 | 49,2 | 40/30 |
| 500 | 5 g | 5,046 | 2,334 | 53,7 | 46,3 | 50/30 |
| 500 | 10 g | 10,095 | 4,700 | 53,4 | 46,6 | 50/30 |
| 500 | 15 g | 15,014 | 6,720 | 55,2 | 44,8 | 50/30 |
| 600 | 5 g | 5,052 | 2,236 | 55,7 | 44,3 | 60/30 |
| 600 | 10 g | 10,091 | 4,153 | 58,8 | 41,2 | 60/30 |
| 600 | 15 g | 15,047 | 6,221 | 58,7 | 41,3 | 60/30 |

Table 4 - Summary parameters of pyrolytic GC-MS analysis of hydrolysis lignin

| T, °C | Sample mass, µg | Pyrolysis time, min | Number of peaks | ΣTIC, million arb. units | CO₂, % | Water, % |
| --- | --- | --- | --- | --- | --- | --- |
| 200 | 271 | 1 | 2 | 4,60 | 3,74 | 96,26 |
| 300 | 271 | 1 | 17 | 17,03 | 18,43 | 54,80 |
| 400 | 271 | 1 | 64 | 143,30 | 8,31 | 12,82 |
| 500 | 271 | 1 | 22 | 31,85 | 4,58 | 58,88 |
| 600 | 271 | 1 | 4 | 15,09 | 5,26 | 92,20 |

Table 5 - Group distribution of products by relative TIC area

| T, °C | CO₂ | H₂O | Light oxygen-containing compounds | Phenolic and aromatic compounds | Carbohydrate and furan compounds | Hydrocarbons and aromatics |
| --- | --- | --- | --- | --- | --- | --- |
| 200 | 3,74 | 96,26 | 0,00 | 0,00 | 0,00 | 0,00 |
| 300 | 18,43 | 54,80 | 14,29 | 3,97 | 3,28 | 5,23 |
| 400 | 8,31 | 12,82 | 20,60 | 25,26 | 16,92 | 16,09 |
| 500 | 4,58 | 58,88 | 15,06 | 22,48 | 0,00 | 4,99 |
| 600 | 5,26 | 92,20 | 0,00 | 2,54 | 0,00 | 0,00 |

Table 6 - Proximate analysis of hydrolysis lignin solid residues

| Temperature, °C | Wr, % | Ad, % | Ar, % | Qsr, MJ/kg | Qir, MJ/kg | Qsr, kcal/kg | Qir, kcal/kg |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 200 | 4,770 | 2,550 | 2,428 | 21,992 | 20,786 | 5252,699 | 4964,651 |
| 300 | 4,716 | 3,190 | 3,040 | 23,776 | 22,571 | 5678,800 | 5390,991 |
| 400 | 4,661 | 6,064 | 5,781 | 25,560 | 24,355 | 6104,901 | 5817,092 |
| 500 | 3,323 | 13,250 | 12,810 | 26,634 | 25,447 | 6361,422 | 6077,912 |
| 600 | 1,985 | 24,580 | 24,092 | 27,707 | 26,538 | 6617,703 | 6338,492 |