Table 1 CF-160 group test results

| Specimen number | Impact speed，m/s | Penetration / Nonpenetration |
| --- | --- | --- |
| 1# | 273 | Penetration |
| 2# | 237 | Nonpenetration |
| 3# | 259 | Nonpenetration |
| 4# | 262 | Penetration |
| 5# | 273 | Penetration |
| 6# | 260 | Penetration |
| 7# | 247 | Nonpenetration |
| 8# | 244 | Nonpenetration |
| 9# | 258 | Penetration |
| 10# | 257 | Nonpenetration |
| 11# | 258 | Nonpenetration |

Table 2 CF-200 group test results

| Specimen number | Impact speed，m/s | Penetration / Nonpenetration |
| --- | --- | --- |
| 1# | 252 | Nonpenetration |
| 2# | 269 | Penetration |
| 3# | 259 | Penetration |
| 4# | 256 | Nonpenetration |
| 5# | 263 | Penetration |
| 6# | 256 | Penetration |
| 7# | 258 | Nonpenetration |
| 8# | 255 | Penetration |
| 9# | 258 | Penetration |
| 10# | 255 | Nonpenetration |
| 11# | 237 | Nonpenetration |

Table 3 Sequence of visual inspection of impact damage

| detection sequence | Specimen number | Impact speed，m/s | Penetration / Nonpenetration |
| --- | --- | --- | --- |
| 1 | #8 | 244 | Nonpenetration |
| 2 | #11 | 248 | Nonpenetration |
| 3 | #6 | 260 | Penetration |

Table 4 Stiffness discounting scheme[29]

| Failure mode | The reduction of scheme of materials |
| --- | --- |
| tensile failure of fibers | ,, |
| compressive failure of fibers | ,, |
| tensile failure of matrix | ,, |
| compressive failure of matrix | ,, |