Electronic Supplementary Material

Buffer-disciplined freezing-directed conjugation of an anti-HER2 aptamer to gold nanoparticles with a salt-challenge quality gate

Delima Engga Maretha¹* · Chairul Ichsan² · Rohmatulaili² · Bagus Rizkyantoro² · Irfan Muzakki² · Rindy Apriliani² · Nabillah Bilqis Haffizhoh²

¹ Department of Biology, Faculty of Science and Technology, Universitas Islam Negeri Raden Fatah Palembang, Palembang, South Sumatra 30267, Indonesia

² Department of Chemistry, Faculty of Science and Technology, Universitas Islam Negeri Raden Fatah Palembang, Palembang, South Sumatra 30267, Indonesia

* Corresponding author: Delima Engga Maretha, delimaenggamaretha_uin@radenfatah.ac.id

Submitted to Microchimica Acta

Table S1 Upstream unit operations and their design rationale

| Step | Operation | Rationale |
| --- | --- | --- |
| Reduction | DTT 50 mM, 1–2 h | Cleaves the 5′-disulfide to the free thiol; a ~500-fold excess is sufficient while limiting the DTT to be removed |
| Purification | Ethanol precipitation | Removes DTT completely; dissolving the pellet in a measured volume fixes the aptamer concentration (e.g. 50 µM) |
| Buffer discipline | Water or low-salt media upstream | Keeps NaCl below the CCC; PBS only after conjugation |
| Conjugation | Freeze at −20 °C for ≥2 h, then slow thaw | Reagentless, dense loading; no salt, acid or surfactant |
| Ratio | ~500:1 aptamer to particle | Ensures adequate surface protection (raised from ~216:1) |
| Quality gate | Salt-challenge at 500 mM NaCl | Equipment-free pass/fail before washing |

Table S2 Interpretation of the salt-challenge quality gate

| Observation at ~500 mM NaCl | Interpretation | Action |
| --- | --- | --- |
| Stays red | Adequate loading; true conjugate | Proceed to washing |
| Turns purple or blue | Insufficient loading | Do not wash; add a freeze–thaw cycle or raise the ratio to 800–1000:1 |
| Purple pellet after centrifugation | Pseudo-stable; died on concentration | Improve loading first; reduce g-force and time; resuspend stepwise |