Supporting Information

Flexible FeCo@(SiO2/C) hybrid nanofibers with hierarchical interfaces for microwave absorption and ablation-resistant property

Bo Xionga,b, Qihui Suna,b, Tao Zengb,c, Chuankai Yangb, Xiong Hed, Jingsong Zhang e, Yang Guo f, , Shengzhe Zhaob, Suyun Tianb, Junwei Wangb, Xian Jiana,

a School of Materials and Energy, University of Electronic Science and Technology of China, Chengdu 611731, China.

b Yangtze Delta Region Institute (Huzhou), University of Electronic Science and Technology of China, Huzhou 313001, China.

c School of Materials Science and Engineering, University of Science and Technology Beijing, Beijing 100083, China.

d Sichuan Hanglong Aviation Industry Co., Ltd. Chengdu 610100, China.

e Baowu Carbon Technology Co., Ltd. 201900，shanghai，China.

f School of Electrical and Information Engineering, Panzhihua University, Panzhihua 617000, China.

Equations:

ɑ=(2πfc)×μ׳׳ε״-μ׳ε׳+(μ״ε״-μ׳ε׳)2+(μ״ε״+μ׳ε׳)2#S1

ε׳-εs+ε∞22+ε״2=εs-ε∞22#S2

Where εs represents the static dielectric constant, and ε∞ represents the relative dielectric constant. Each semicircle on the plot of ε′-ε″ is referred to as a Cole-Cole semicircle.

∆=sinh2Kfd-M#S(3)

K=4πμ'ε'sinδe+δm2 ccosδecosδm#S(4)

M=4μ'cos δe ε'cos δmμ'cos δe-ε'cos δm2+tanδm2-δe22μ'cos δe+ε'cos δm2      S(5)

Where d represents the thickness of the materials, while |Δ| represents the impedance matching of the materials. The larger range of |Δ| less than 0.4 indicates the better impedance matching characteristics. The ɑ value indicates the ability of materials to attenuate electromagnetic waves.

tm=λ4=14fmεrμr#S6

Figures:

Fig. S1 The optical images of (a) SiO2, (b) FeCo@ (SiO2/PVA)-5%, (c) FeCo@ (SiO2/PVA)-10%, (d) FeCo@ (SiO2/PVA)-15%.

Fig. S2 SEM image and (insert) fiber size distribution of SiO2/C.

Fig. S3 (a) 3D RL plots of SiO2/C. (b) The 2D RL curves with discrepant colors of SiO2/C; FeCo@ (SiO2/C)-5%; FeCo@ (SiO2/C)-10%; d FeCo@ (SiO2/C)-15%.

Fig. S4 The C0 values of SiO2/C, FeCo@(SiO2/C)-5%, FeCo@(SiO2/C)-10%, and FeCo@(SiO2/C)-15%.

Fig. S5 Cole–Cole plots of SiO2/C, FeCo@(SiO2/C)-5%, FeCo@(SiO2/C)-10%, and FeCo@(SiO2/C)-15%.

Fig. S6 Impedance matching of SiO2/C (a), FeCo@(SiO2/C)- 5% (b), FeCo@(SiO2/C)-10% (c), FeCo@(SiO2/C)-15% (d), and rGNC-8 (e).

Fig. S7 Open-circuit voltages of FeCo and FeCo@(SiO2/C)-15%.

Table S1 The comparison of FeCo-based composite absorber performance involves RL and EAB values.

| Materials | Minimum RL (dB) | EAB (GHz) | Frequency (GHz) | Thickness (mm) | Range | Refs |
| --- | --- | --- | --- | --- | --- | --- |
| FeCo nanocapsules | -29.00 | 4.00 | / | 5.00 | 2-18 | [1] |
| (FeCo/PVP)@GO | -40.94 | 4.90 | 14.25 | 2.00 | 2-18 | [2] |
| FeCo/graphene hybrids | 40.20 | 5.90 | 8.90 | 2.50 | 0.1-18 | [3] |
| FeCo/PPy | -52.30 | 5.06 | 13.40 | 2.15 | 1-18 | [4] |
| FeCo/CNF | -24.05 | 2.87 | 14.88 | 4.00 | 2-18 | [5] |
| FeCo@SnO2@graphene@PANI | -39.80 | 3.10 | 6.40 | 3.00 | 2-18 | [6] |
| FeCo@porous carbon | -54.70 | 5.48 | / | 1.90 | 2-18 | [7] |
| FeCo/CNTs | -46.50 | 3.92 | 12.56 | 1.70 | 2-18 | [8] |
| FeCo-BN | -46.40 | 5.04 | 11.30 | 1.50 | 0.5-18 | [9] |
| Fe0.9Co0.1 nano-alloys | -48.70 | 4.20 | 4.20 | 3.20 | 2-18 | [10] |
| This work | -56.25 | 5.3 | 12.23 | 2.50 | 2-18 | # |

References:

[1] Han Z, Li D, Wang H, Liu XG, Li J, Geng DY and Zhang ZD, Broadband electromagnetic-wave absorption by FeCo/C nanocapsules, Applied Physics Letters, 2009, 95(2):023114. https://doi.org/10.1063/1.3177067.

[2] Cui E, Pan F, Xiang Z, Liu Z, Yu L, Xiong J, Li X and Lu W, Engineering Dielectric Loss of FeCo/Polyvinylpyrrolidone Core‐Shell Nanochains@Graphene Oxide Composites with Excellent Microwave Absorbing Properties, Advanced Engineering Materials, 2020, 23(1): 2000827. https://doi.org/10.1002/adem.202000827.

[3] Li X, Feng J, Du Y, Bai J, Fan H, Zhang H, Peng Y and Li F, One-pot synthesis of CoFe2O4/graphene oxide hybrids and their conversion into FeCo/graphene hybrids for lightweight and highly efficient microwave absorber, Journal of Materials Chemistry A, 2015, 3(10): 5535. https://doi.org/10.1039/c4ta05718j.

[4] Wang H, Yan Z, An J, He J, Hou Y, Yu H, Ma N, Yu G and Sun D, Iron cobalt/polypyrrole nanoplates with tunable broadband electromagnetic wave absorption, RSC Advances, 2016, 6(95): 92152. https://doi.org/10.1039/c6ra16003d.

[5] Huang B, Yue J, Wei Y, Huang X, Tang X and Du Z, Enhanced microwave absorption properties of carbon nanofibers functionalized by FeCo coatings, Applied Surface Science, 2019, 483: 98. https://doi.org/10.1016/j.apsusc.2019.03.301.

[6] Wang Y, Zhang W, Luo C, Wu X and Yan G, Superparamagnetic FeCo@SnO2 nanoparticles on graphene-polyaniline: Synthesis and enhanced electromagnetic wave absorption properties, Ceramics International, 2016, 42(10): 12496. https://doi.org/10.1016/j.ceramint.2016.05.038.

[7] Wu Y, Tan S, Zhang T, Zhou M, Fang G and Ji G, Alkali and ion exchange co-modulation strategies to design magnetic–dielectric synergistic nano-absorbers for tailoring microwave absorption, Nano Research, 2023, 16(7): 8522. https://doi.org/10.1007/s12274-023-5799-3.

[8] Yang B, Wu Y, Li X and Yu R, Surface-oxidized FeCo/carbon nanotubes nanorods for lightweight and efficient microwave absorbers, Materials & Design, 2017, 136: 13. https://doi.org/10.1016/j.matdes.2017.09.055.

[9] Se Chang M, Hwang S-s, Jeong S-J, Won Jeong J, Park B, Yang S, Rae Park C and Kwon Y-T, FeCo-BN magnetic composite membrane prepared via an atomized aerosol process for electromagnetic wave absorption and thermal management, Chemical Engineering Journal, 2023, 475: 146496. https://doi.org/10.1016/j.cej.2023.146496.

[10] Hu R, Li L, Xu X, Pan D, Dong J, Zhen C, Gu MD and Wang H, Dimensional design of Fe0.9Co0.1 nano-alloys with enhanced low-frequency microwave absorption, Chemical Engineering Journal, 2024, 482: 148864. https://doi.org/10.1016/j.cej.2024.148864.

Corresponding authors. E-mail addresses: jianxian@uestc.edu.cn (X. Jian), guoyangchn@126.com (Y. Guo).