Supplementary Information

Catalytic Etherification of Furfuryl Alcohol to Isopropyl Furfuryl Ether over MIL-68(V) and MOF-Derived V₂O₃@C

Ubed SF Arrozi1*§, Aryan B. Saputra1§, M. Rafi Pratama1, Istifhamy Irnanda1, Surjani Wonorahardjo1, Yessi Permana2, Witri W. Lestari3, Wirawan Ciptonugroho4, Yudha P. Budiman5, Khoa D. Nguyen6, Hadi Nur1, Sheela Chandren7, Lee H. Voon8

1Department of Chemistry, Faculty of Mathematics and Natural Sciences, State University of Malang, Jl. Semarang 5, Malang 65145, East Java, Indonesia

2Inorganic and Physical Chemistry Research Division, Faculty of Mathematics and Natural Sciences, Institut Teknologi Bandung, Jl. Ganesha 10, Bandung 40132, Indonesia

3Department of Chemistry, Faculty of Mathematics and Natural Sciences, Universitas Sebelas Maret, Jl. Ir. Sutami No. 36, Kentingan-Jebres Surakarta, Central Java, Indonesia, 57126

4Department of Chemistry Education, Faculty of Teacher Training and Education, Universitas Sebelas Maret, Jl. Ir. Sutami No. 36, Kentingan-Jebres Surakarta, Central Java, Indonesia, 57126

5Department of Chemistry, Faculty of Mathematics and Natural Sciences, Universitas Padjadjaran, 45363 Sumedang, Indonesia

6Department of Chemical Engineering, Ho Chi Minh City University of Technology (HCMUT), VNU-HCM, 268 Ly Thuong Kiet street, Dien Hong ward, Ho Chi Minh City, Vietnam

7Department of Chemistry, Faculty of Science, Universiti Teknologi Malaysia, 81310 UTM Johor Bahru, Johor, Malaysia

8Nanotechnology & Catalysis Research Centre (NANOCAT), Block A, Level 3, Advanced Studies Complex, Universiti Malaya, 50603 Kuala Lumpur, Malaysia

Corresponding author: ubedsonai.fmipa@um.ac.id

§Authors contribute equally

Figure S1. Physical appearance of MIL-68(V) (left) and the corresponding V2O3@C.

Figure S2. BET plot of MIL-68(V) and V2O3@C

Table S1. BET surface area and pore volume of the vanadium MOFs and V2O3@C

| Samples | BET surface area [m2g-1] |
| --- | --- |
| MIL-68(V) | 91 |
| V2O3@C | 131 |

Figure S3. PXRD plot of MIL-68(V) after reusability test