Supplementary Information

Cation Locking Accelerates Exciton Recombination in Polar Two-Dimensional Hybrid Perovskites

Yuhong Mao,1 Liwei Tang,2 Songhao Guo,1 Xingyu Chen,1 Yifan Zhang,1 Qingyang Hu,1 Zhihua Sun,2 Junhua Luo,2 Wenge Yang,1 and Xujie Lü1,*

1 Center for High Pressure Science and Technology Advanced Research (HPSTAR), Shanghai, 201203, China

2 State Key Laboratory of Structural Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences Institution, Fuzhou, Fujian, 350002, China

* Corresponding authors: Email: xujie.lu@hpstar.ac.cn

Supplementary Tables

Supplementary Table 1. Crystallographic information for (iBA)2(MA)2Pb3Br10

| Crystal data |  |
| --- | --- |
| Chemical formula | [(CH3)2CHCH2NH3]2(CH3NH3)2Pb3Br10 |
| Mr | 1633.10 |
| Crystal system, space group | Tetragonal, I4/mmm |
| a, c (Å) | 5.9204 (3), 50.863 (4) |
| V (Å3) | 1782.8 (2) |
| Z | 2 |
| Radiation type | Mo Ka |
| m (mm-1) | 25.34 |
| Data collection |  |
| Rint | 0.043 |
| (sin q/l)max (Å-1) | 0.595 |
| Refinement |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.051, 0.139, 1.13 |
| No. of reflections | 543 |
| No. of parameters | 45 |
| No. of restraints | 28 |
| H-atom treatment | H-atom parameters constrained |
|  | w = 1/[s2(Fo2) + (0.0708P)2 + 47.6557P] where P = (Fo2 + 2Fc2)/3 |
| Dρmax, Dρmin (e Å-3) | 2.28, -3.07 |

Supplementary Table 2. Crystallographic information for (iBA)2(EA)2Pb3Br10

| Crystal data |  |
| --- | --- |
| Chemical formula | [(CH3)2CHCH2NH3]2(CH3CH2NH3)2Pb3Br10 |
| Mr | 1661.15 |
| Crystal system, space group | Orthorhombic, Cmc21 |
| a, b, c (Å) | 50.617 (2), 8.5192 (3), 8.5183 (4) |
| V (Å3) | 3673.2 (3) |
| Z | 4 |
| Radiation type | Mo Ka |
| m (mm-1) | 24.60 |
| Data collection |  |
| Rint | 0.040 |
| (sin q/l)max (Å-1) | 0.650 |
| Refinement |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.065, 0.235, 1.08 |
| No. of reflections | 4222 |
| No. of parameters | 152 |
| No. of restraints | 76 |
| H-atom treatment | H-atom parameters constrained |
|  | w = 1/[s2(Fo2) + (0.0779P)2 + 134.1122P] where P = (Fo2 + 2Fc2)/3 |
| Dρmax, Dρmin (e Å-3) | 1.88, -1.38 |

Supplementary Table 3. Crystallographic information for (iBA)2(MHy)2Pb3Br10

| Crystal data |  |
| --- | --- |
| Chemical formula | [(CH3)2CHCH2NH3]2(CH3NH2NH3)2Pb3Br10 |
| Mr | 1663.13 |
| Crystal system, space group | Monoclinic, Pc |
| a, b, c (Å) | 11.7467 (1), 49.2238 (6), 11.8147 (1) |
| b (°) | 90.537 (1) |
| V (Å3) | 6831.16 (12) |
| Z | 4 |
| Radiation type | Ga Ka, l = 1.3405 Å |
| m (mm-1) | 29.35 |
| Data collection |  |
| Rint | 0.043 |
| (sin q/l)max (Å-1) | 0.595 |
| Refinement |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.082, 0.237, 1.04 |
| No. of reflections | 16703 |
| No. of parameters | 1099 |
| No. of restraints | 1035 |
| H-atom treatment | H-atom parameters constrained |
|  | w = 1/[s2(Fo2) + (0.1801P)2 + 86.P] where P = (Fo2 + 2Fc2)/3 |
| Dρmax, Dρmin (e Å-3) | 5.60, -3.22 |

Supplementary Table 4. Crystallographic information for (EA)4Pb3Br101

| Crystal data |  |
| --- | --- |
| Chemical formula | (CH3CH2NH3)4Pb3Br10 |
| Mr | 1605 |
| Crystal system, space group | Orthorhombic, C2cb |
| a, b, c (Å) | 8.4267 (12), 46.351 (5), 8.4298 (10) |
| V (Å3) | 3292.5 (7) |
| Z | 4 |
| Radiation type | Mo Ka |
| m (mm-1) | 27.44 |
| Data collection |  |
| Rint | 0.073 |
| (sin q/l)max (Å-1) | 0.685 |
| Refinement |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.096, 0.185, 3.14 |
| No. of reflections | 5228 |
| No. of parameters | 81 |
| No. of restraints | 6 |
| H-atom treatment | H-atom parameters constrained |
| Dρmax, Dρmin (e Å-3) | 2.83, -3.84 |

Supplementary Table 5. Crystallographic information for (iBA)2(EA)Pb2Br72

| Crystal data |  |
| --- | --- |
| Chemical formula | [(CH3)2CHCH2NH3]2CH3CH2NH3Pb2Br7 |
| Mr | 1168.13 |
| Crystal system, space group | Monoclinic, Cc |
| a, b, c (Å) | 36.800 (4), 8.4400 (5), 8.3776 (6) |
| b (°) | 90.029 (8) |
| V (Å3) | 2602.0 (4) |
| Z | 4 |
| Radiation type | Mo Ka |
| m (mm-1) | 23.67 |
| Data collection |  |
| Rint | 0.052 |
| (sin q/l)max (Å-1) | 0.696 |
| Refinement |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.055, 0.155, 1.02 |
| No. of reflections | 6257 |
| No. of parameters | 208 |
| No. of restraints | 163 |
| H-atom treatment | H-atom parameters constrained |
| Dρmax, Dρmin (e Å-3) | 2.68, -1.58 |

Supplementary Table 6. Crystallographic information for (BA)2(EA)2Pb3I103

| Crystal data |  |
| --- | --- |
| Chemical formula | (CH3CH2CH2NH3)2(CH3CH2NH3)2Pb3I10 |
| Mr | 2103 |
| Crystal system, space group | Monoclinic, Cc |
| a, b, c (Å) | 52.209 (6), 8.9061 (6), 8.9400 (11) |
| b (°) | 90.002 (9) |
| V (Å3) | 4156.9 (8) |
| Z | 4 |
| Radiation type | Mo Ka |
| m (mm-1) | 19.54 |
| Data collection |  |
| Rint | 0.054 |
| (sin q/l)max (Å-1) | 0.687 |
| Refinement |  |
| R[F2 > 2s(F2)], wR(F2), S | 0.109, 0.113, 4.78 |
| No. of reflections | 7083 |
| No. of parameters | 166 |
| No. of restraints | 16 |
| H-atom treatment | H-atom parameters constrained |
| Dρmax, Dρmin (e Å-3) | 7.09, -7.16 |

Supplementary Figures

Figure S1. Extended crystal structure of (iBA)2(MA)2Pb3Br10.

Figure S2. Extended crystal structure of (iBA)2(EA)2Pb3Br10.

Figure S3. Extended crystal structure of (iBA)2(MHy)2Pb3Br10. Pb-N coordinate bonds are removed for clarity.

Figure S4. (a) SHG polarization polar plots of iBA-EA with the parallel configurations at different pressures. (b) Corresponding SHG intensity as a function of pressure in iBA-EA.

Figure S5. (a) SHG polarization polar plots of iBA-MHy with the parallel configurations at different pressures. (b) Corresponding SHG intensity as a function of pressure in iBA-MHy.

Figure S6. Extended crystal structure of (EA)2(EA)2Pb3Br10.

Figure S7. Parallel mode SHG polarization polar plots of (EA)2(EA)2Pb3Br10 and its corresponding SHG intensity as a function of pressure.

Figure S8. Extended crystal structure of (iBA)2(EA)Pb2Br7.

Figure S9. Extended crystal structure of (BA)2(EA)2Pb3I10.

Figure S10. Parallel mode SHG polarization polar plots of (iBA)2(EA)Pb2Br7 and its corresponding SHG intensity as a function of pressure.

Figure S11. Parallel mode SHG polarization polar plots of (BA)2(EA)Pb3I10 and its corresponding SHG intensity as a function of pressure.

Figure S12. (a) p-XRD spectra of iBA-EA at different pressures. (b) Normalized lattice constants as a function of pressure.

Figure S13. Absorption spectrum evolutions of (a) iBA-MA, (b) iBA-EA, and (c) iBA-MHy between 0 and 0.8 GPa.

Figure S14. Inorganic lattice Raman signals of iBA-MA at selected pressures.

Figure S15. The PL symmetry factor of iBA-EA and iBA-MA as a function of pressure.

Figure S16. PL Lifetime of (a) iBA-MA, (b)(c) iBA-EA, and (d) iBA-MHy at different pressures.

Figure S17. Normalized radiative (kr/k0, black) and non-radiative (knr/k0, red) recombination rates of iBA-EA as a function of pressure.

Figure S18. Comparison of the pressure-dependent evolution of PL lifetime and deff of iBA-MHy.

Figure S19. TA spectra of iBA-EA at selected pressures.

Figure S20. Photo of the iBA-EA high-pressure photoelectric response testing circuit.

Figure S21. I-T curves of iBA-EA in 1-3 and 2-4 directions at selected pressures.

References

1.	Mao, L.; Wu, Y.; Stoumpos, C. C.; Traore, B.; Katan, C.; Even, J.; Wasielewski, M. R.; Kanatzidis, M. G., Tunable White-Light Emission in Single-Cation-Templated Three-Layered 2D Perovskites (CH3CH2NH3)4Pb3Br10-xClx. J. Am. Chem. Soc. 2017, 139 (34), 11956-11963.

2.	Peng, Y.; Bie, J.; Liu, X.; Li, L.; Chen, S.; Fa, W.; Wang, S.; Sun, Z.; Luo, J., Acquiring High-T(C) Layered Metal Halide Ferroelectrics via Cage-Confined Ethylamine Rotators. Angew. Chem. Int. Ed. 2021, 60 (6), 2839-2843.

3.	Fu, Y.; Jiang, X.; Li, X.; Traore, B.; Spanopoulos, I.; Katan, C.; Even, J.; Kanatzidis, M. G.; Harel, E., Cation Engineering in Two-Dimensional Ruddlesden–Popper Lead Iodide Perovskites with Mixed Large A-Site Cations in the Cages. J. Am. Chem. Soc. 2020, 142 (8), 4008-4021.