Investigating the kinetics of the thermolysis of 3-nitro-2,4-dihydro-3H-1,2,4-triazol-5-one (NTO) and reduced size NTO  the presence of cobalt ferrite additive

Pragnesh N. Davea, Ruksana Siracha, Riddhi Thakkara, M P Deshpande

aDepartment of Chemistry, Sardar Patel University, Vallabh Vidyanagar, 388 120, Gujarat,

India

bDepartment of Physics, Sardar Patel University, Vallabh Vidyanagar, 388 120, Gujarat,

India

*Corresponding author: pragnesh7@yahoo.com

Supporting Information

Supporting figures

Fig. S 1 UV-Vis Spectrum of TO, NTO, and r-NTO

Fig. S 2 TG curve of CoF

Fig. S 3 DTA curves of NTO, NTO+CoF, r-NTO, and r-NTO+CoF at various heating rates

Fig. S 4 FWO, KAS, and Starink plots of NTO, and NTO+CoF at various conversion points

Fig. S 5 FWO, KAS, and Starink plots of r-NTO, and r-NTO+CoF at various conversion points

Supporting tables

Table S 1. Value of most suitable g(α) for NTO, r-NTO, NTO+CoF, and r-NTO+CoF

| Composition | g(α) |
| --- | --- |
| NTO | α1/4 |
| NTO+CoF | [-ln(1-α)]2/3 |
| r-NTO | α1/3 |
| r-NTO+CoF | α3/2 |

Table S 2. Raman shift values of NTO

| Peak list | Raman shift (cm-) | Intensity (a.u.) |
| --- | --- | --- |
| Peak1 | 39.5897 | 794 |
| Peak2 | 67.7162 | 982 |
| Peak3 | 93.8717 | 4568 |
| Peak4 | 121.789 | 10444 |
| Peak5 | 144.047 | 2080 |
| Peak6 | 190.195 | 1278 |
| Peak7 | 343.078 | 718 |
| Peak8 | 414.711 | 306 |
| Peak9 | 471.476 | 918 |
| Peak10 | 581.843 | 1168 |
| Peak11 | 690.374 | 306 |
| Peak12 | 724.447 | 1596 |
| Peak13 | 746.497 | 1136 |
| Peak14 | 825.575 | 1078 |
| Peak15 | 1003.5 | 1004 |
| Peak16 | 1014.85 | 1400 |
| Peak17 | 1100.1 | 6972 |
| Peak18 | 1251.35 | 282 |
| Peak19 | 1328.53 | 7030 |
| Peak20 | 1356.05 | 8094 |
| Peak21 | 1470.71 | 4688 |
| Peak22 | 1543.33 | 2710 |
| Peak23 | 1588.75 | 4520 |