## Slide 1
Chart: VOC Measurement
| 1 | 2 | 3 | 4 | 5
WB Ink | 3122 | 2690 | 2450 | 2148 | 1978
SB Ink | 3498 | 3172 | 3381 | 3366 | 3448
VOCs emissions in SB and WB inks during printing process.
Quality measurement with formulated ink
Difference between electronic and laser engraving
Chart: Analysis of reduction in depth and properties
| Depth | Dot% | Color Density | Depth | Dot% | Color Density | Electronic | Laser
18 | 18.4 | 85 | 2.21 | 14.4 | 85 | 2.26
15 | 15.2 | 82 | 2.13 | 12.4 | 82 | 2.17
12 | 12 | 81 | 1.94 | 10.4 | 80 | 1.98
Graphical Abstract