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Tab. S1. Specific surface areas, average pore volumes, and average pore diameters of InOOH, SnO2, and 5:5 In/Sn
	Samples
	Specific surface area
(m2·g-1)
	Average pore volume
(cm3·g-1)
	Average pore diameter
(nm)

	InOOH
	49.8305
	0.174497
	15.1885

	SnO2
	117.2515
	0.098558
	3.3739

	5:5 In/Sn
	134.9369
	0.128921
	3.4617
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Fig. S1. XRD patterns of the catalyst before and after reaction.
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