Supplementary information

Synergistic effect of In doping and heterojunction in InOOH/Sn1-xInxO2-x/2 for efficient photothermocatalytic CO2 reduction

Yuhan Lin,a Yufei Jiang,a Yi He,a Wei Peng,b* Chuanyi Wang a*.

a School of Environmental Science and Engineering, Shaanxi University of Science and Technology, Xi’an 710021, P. R. China.

b Key Laboratory of the Forensic Science, Hubei University of Police,Wuhan 430000, P. R. China.

*Corresponding Authors.

E-mail addresses: pengwei1015@hbpa.edu.cn (W. Peng), wangchuanyi@sust.edu.cn (C. Wang).

Tab. S1. Specific surface areas, average pore volumes, and average pore diameters of InOOH, SnO2, and 5:5 In/Sn

| Samples | Specific surface area (m2·g-1) | Average pore volume (cm3·g-1) | Average pore diameter (nm) |
| --- | --- | --- | --- |
| InOOH | 49.8305 | 0.174497 | 15.1885 |
| SnO2 | 117.2515 | 0.098558 | 3.3739 |
| 5:5 In/Sn | 134.9369 | 0.128921 | 3.4617 |

Fig. S1. XRD patterns of the catalyst before and after reaction.