Table 10 Humidity buffering parameters of each group in sealed containers (mean ± SD, n = 3)
	Group
	Peak RH (%)
	24 h equilibrium RH (%)
	Stabilisation time (h)
	24 h MBV (g/(kg·%RH))

	Blank container
	82.1 ± 0.3
	81.2 ± 0.4
	–
	–

	Untreated poplar
	81.8 ± 0.5
	72.5 ± 0.8
	14.0 ± 0.9
	0.72 ± 0.06

	Optimally modified poplar
	78.1 ± 0.6
	67.3 ± 0.7
	9.0 ± 0.6
	1.07 ± 0.08


[bookmark: _GoBack]Note: MBV, moisture buffering value. "–" indicates that the parameter is not applicable.
