Table 10 Humidity buffering parameters of each group in sealed containers (mean ± SD, n = 3)

| Group | Peak RH (%) | 24 h equilibrium RH (%) | Stabilisation time (h) | 24 h MBV (g/(kg·%RH)) |
| --- | --- | --- | --- | --- |
| Blank container | 82.1 ± 0.3 | 81.2 ± 0.4 | – | – |
| Untreated poplar | 81.8 ± 0.5 | 72.5 ± 0.8 | 14.0 ± 0.9 | 0.72 ± 0.06 |
| Optimally modified poplar | 78.1 ± 0.6 | 67.3 ± 0.7 | 9.0 ± 0.6 | 1.07 ± 0.08 |

Note: MBV, moisture buffering value. "–" indicates that the parameter is not applicable.