Table 2 Experimental design for glycerol mass fraction

| Test Samples | Formulation (glycerol mass fraction) |
| --- | --- |
| 1 | Base solution (55 wt% anhydrous ethanol + 10 wt% deionized water) |
| 2 | Base solution + 0.5 wt% purple sweet potato anthocyanin |
| 3 | Base solution + 0.5 wt% purple sweet potato anthocyanin + 20 wt% glycerol |
| 4 | Base solution + 0.5 wt% purple sweet potato anthocyanin + 22 wt% glycerol |
| 5 | Base solution + 0.5 wt% purple sweet potato anthocyanin + 24 wt% glycerol |
| 6 | Base solution + 0.5 wt% purple sweet potato anthocyanin + 26 wt% glycerol |
| 7 | Base solution + 0.5 wt% purple sweet potato anthocyanin + 28 wt% glycerol |

Note: Sample 1 served as the blank control group, and Sample 2 served as the reference control group. Samples 3–7 corresponded to groups with different glycerol dosages. Three replicate specimens were prepared for each group. The optimal glycerol mass fraction determined from this experiment is denoted as x in subsequent tables. Objective: to determine the optimal glycerol mass fraction x.