Table 11 Changes in humidity buffering performance and mass of modified specimens before and after the 60-day (30-cycle) wet–dry aging test (mean ± SD, n = 3)
	Index
	Before cycling
	After 30 cycles
	Retention rate (%)

	WPG (%)
	3.82 ± 0.64
	3.21 ± 0.58
	84.0 ± 2.1

	Peak RH (%)
	78.1 ± 0.6
	79.4 ± 0.7
	–

	24 h equilibrium RH (%)
	67.3 ± 0.7
	69.5 ± 0.8
	–

	Stabilisation time (h)
	9.0 ± 0.6
	10.5 ± 0.7
	–

	24 h MBV (g/(kg·%RH))
	1.07 ± 0.08
	0.89 ± 0.07
	83.2 ± 2.4


[bookmark: _GoBack]Note: "–" indicates that retention rate is not applicable for this indicator. MBV, moisture buffering value.
