Table 11 Changes in humidity buffering performance and mass of modified specimens before and after the 60-day (30-cycle) wet–dry aging test (mean ± SD, n = 3)

| Index | Before cycling | After 30 cycles | Retention rate (%) |
| --- | --- | --- | --- |
| WPG (%) | 3.82 ± 0.64 | 3.21 ± 0.58 | 84.0 ± 2.1 |
| Peak RH (%) | 78.1 ± 0.6 | 79.4 ± 0.7 | – |
| 24 h equilibrium RH (%) | 67.3 ± 0.7 | 69.5 ± 0.8 | – |
| Stabilisation time (h) | 9.0 ± 0.6 | 10.5 ± 0.7 | – |
| 24 h MBV (g/(kg·%RH)) | 1.07 ± 0.08 | 0.89 ± 0.07 | 83.2 ± 2.4 |

Note: "–" indicates that retention rate is not applicable for this indicator. MBV, moisture buffering value.