Laser-Induced Surface Structuring of Silicon for Enhanced Antibacterial Performance of Silver Thin Films

Lynda Lounis1, Barthélemy Aspe*1, Pierre Birnal1, Hervé Rabat1, Loïc Gimenez1, Arnaud Stolz1, Fabienne Brulé-Morabito2, Anne-Lise Thomann1, Eric Millon1, Nadjib Semmar1

1 Université d’Orléans, CNRS, GREMI UMR7344, 14 rue d’Issoudun, F-45067 Orléans, France

2 Université d'Orléans – INSERM, InTheRNA UMR1364, CHU Orléans, 14 avenue de l'Hôpital, 45100 Orléans La Source, France

*Corresponding author: barthelemy.aspe@univ-orleans.fr

ORCID Barthélemy Aspe: 0000-0001-8927-4013

Apprendix

Estimation of the surface enhancement by LIPSS

Fig. S1: Schematic of LIPSS structures approximated as elliptical half-cylinders (EHC).

The specific surface area of the surface after LIPSS formation was calculated using the method described by Karim et al. [1]. Initially, the flat, unstructured surface (S0) was considered to be rectangular, its surface area being defined by:

S0=Lx×Ly      (1 SEQ Eq \* ARABIC )

After laser structuring, the shape of the D‑LIPSS is assumed to be approximated by elliptical half-cylinders (EHC), as shown in Fig. S1. The surface area of an EHC is given by:

SEHC=P×Ly2

Where P is the perimeter of the EHC and Ly likely refers to the length of the EHC along the y-direction. If Nx elliptical half-cylinders (Nx protrusions) are considered, the total surface area is given by:

SEHCtot=P×Nx×Ly2

The number of nano-structures Nx is calculated as:

Nx=LxΛ

Where Λ denotes the spatial period of the LIPSS equal to 850 ± 20 nm. The specific surface area is then expressed as:

SECtot=P×Lx×Ly2Λ     (2 SEQ Eq \* ARABIC )

To calculate the perimeter, Ramanujan’s approximation for the perimeter of an ellipse was used [2]:

P= πA+Λ2+3A-Λ2210A+Λ2+A2+14AΛ2+Λ22

Where A represents the amplitude of the LIPSS, taking into account the oxide layer formed after laser structuring. The value of A is approximately 900 nm.  The surface enhancement ratio (Σ) induced by LIPSS formation can be determined from expressions (1) and (2).

Σ= SECtotS0=P×Lx×Ly2Λ×1Lx×Ly=P2Λ

In this study, the surface enhancement ratio (Σ) is approximately 3, indicating that the surface area is enhanced by 200%.

References

[1]	W. Karim, A. Petit, H. Rabat, M. Tabbal, A.-L. Thomann, et N. Semmar, « Picosecond laser beam nanostructuring of GDC thin films: exchange surface enhancement by LIPSS », Appl. Phys. A, vol. 128, no 8, p. 731, 2022, doi: 10.1007/s00339-022-05866-6.

[2]	M. B. Villarino, « Journal of Inequalities in Pure and Applied Mathematics », 2006.