Development and Optimization of Puerarin-loaded ion-triggered in situ gel for ocular delivery in dry eye disease

Table S1. UV calibration profile of puerarin at 250 nm

| Concentration (µg/mL) | Absorbance (Mean ± SD, n=3) |
| --- | --- |
| 2 | 0.148 ± 0.006 |
| 4 | 0.286 ± 0.009 |
| 6 | 0.438 ± 0.012 |
| 8 | 0.571 ± 0.015 |
| 10 | 0.728 ± 0.018 |
| 12 | 0.846 ± 0.021 |

Cumulative In Vitro Drug Release

Table S2: Cumulative In Vitro Drug Release (%) of Puerarin-Loaded Ion-Triggered In Situ Gel Formulations F1–F9 Across 12 Hours

| Time (h) | F1 | F2 | F3 | F4 | F5 | F6 | F7 | F8 | F9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 |
| 1 | 18.42 ± 0.54 | 15.36 ± 0.48 | 12.18 ± 0.41 | 16.84 ± 0.52 | 13.72 ± 0.44 | 10.96 ± 0.38 | 14.28 ± 0.46 | 11.84 ± 0.39 | 9.64 ± 0.32 |
| 2 | 31.24 ± 0.72 | 26.48 ± 0.63 | 21.86 ± 0.57 | 28.36 ± 0.68 | 23.94 ± 0.59 | 19.42 ± 0.51 | 24.72 ± 0.61 | 20.88 ± 0.54 | 17.36 ± 0.46 |
| 4 | 51.68 ± 0.91 | 44.72 ± 0.84 | 37.54 ± 0.76 | 47.36 ± 0.87 | 40.82 ± 0.79 | 33.96 ± 0.68 | 42.14 ± 0.82 | 36.48 ± 0.72 | 29.84 ± 0.61 |
| 6 | 68.34 ± 1.12 | 60.16 ± 1.04 | 51.28 ± 0.94 | 63.72 ± 1.08 | 55.46 ± 0.97 | 46.84 ± 0.86 | 57.92 ± 1.01 | 49.36 ± 0.89 | 41.62 ± 0.78 |
| 8 | 81.46 ± 1.34 | 73.28 ± 1.21 | 63.84 ± 1.09 | 76.54 ± 1.27 | 67.92 ± 1.14 | 58.36 ± 1.02 | 70.18 ± 1.18 | 61.74 ± 1.06 | 52.48 ± 0.94 |
| 10 | 90.72 ± 1.48 | 83.64 ± 1.36 | 74.16 ± 1.22 | 86.38 ± 1.42 | 78.46 ± 1.29 | 68.92 ± 1.16 | 80.84 ± 1.33 | 72.36 ± 1.19 | 62.74 ± 1.08 |
| 12 | 97.28 ± 1.62 | 91.42 ± 1.51 | 83.56 ± 1.38 | 93.74 ± 1.56 | 87.18 ± 1.43 | 78.64 ± 1.28 | 89.36 ± 1.47 | 82.42 ± 1.34 | 73.86 ± 1.21 |

All values Mean ± SD, n=3

Cumulative Ex Vivo Corneal Permeation

Table S3: Cumulative Ex Vivo Corneal Permeation (%) of Puerarin-Loaded Ion-Triggered In Situ Gel Formulations F1–F9 Using Freshly Excised Goat Cornea (Mean ± SD, n=3)

| Time (h) | F1 | F2 | F3 | F4 | F5 | F6 | F7 | F8 | F9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 | 0.00 ± 0.00 |
| 1 | 8.24 ± 0.32 | 9.46 ± 0.38 | 10.82 ± 0.43 | 9.84 ± 0.36 | 11.36 ± 0.46 | 12.74 ± 0.51 | 11.18 ± 0.44 | 12.56 ± 0.48 | 14.12 ± 0.54 |
| 2 | 14.36 ± 0.48 | 16.72 ± 0.54 | 19.24 ± 0.61 | 17.48 ± 0.52 | 20.14 ± 0.63 | 22.86 ± 0.71 | 19.62 ± 0.59 | 22.34 ± 0.67 | 25.46 ± 0.76 |
| 4 | 24.68 ± 0.67 | 28.34 ± 0.74 | 32.46 ± 0.82 | 29.72 ± 0.71 | 34.18 ± 0.86 | 38.24 ± 0.94 | 33.14 ± 0.81 | 37.42 ± 0.91 | 42.68 ± 1.02 |
| 6 | 36.42 ± 0.86 | 41.28 ± 0.94 | 47.64 ± 1.08 | 43.86 ± 0.98 | 50.24 ± 1.12 | 56.38 ± 1.24 | 48.72 ± 1.06 | 54.96 ± 1.18 | 62.14 ± 1.34 |
| 8 | 46.84 ± 1.04 | 53.62 ± 1.16 | 61.28 ± 1.29 | 56.74 ± 1.21 | 64.86 ± 1.36 | 72.46 ± 1.48 | 62.38 ± 1.31 | 70.24 ± 1.43 | 79.56 ± 1.58 |
| 10 | 55.16 ± 1.18 | 63.48 ± 1.31 | 72.84 ± 1.44 | 67.24 ± 1.36 | 76.42 ± 1.52 | 84.68 ± 1.63 | 73.86 ± 1.47 | 82.14 ± 1.58 | 91.32 ± 1.74 |
| 12 | 62.34 ± 1.32 | 71.86 ± 1.46 | 82.46 ± 1.58 | 76.12 ± 1.48 | 86.24 ± 1.64 | 94.38 ± 1.78 | 83.62 ± 1.61 | 92.46 ± 1.72 | 98.74 ± 1.84 |

All values Mean ± SD, n=3