Table S1 | Relative EDS elemental compositions of the three regions of M632:1 after exclusion of C and O (wt%).

| Element Region | Pb | Ba | Cu | Si | Ca | S | Na | Mg | Al | Cl | K | Fe | Ni |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Center | 29.97 | 38.24 | 8.10 | 18.32 | 0.97 | 0.38 | 1.10 | 0.20 | 0.93 | 0.89 | 0.22 | 0.54 | 0.14 |
| Transition | 29.18 | 38.81 | 10.14 | 17.14 | 0.60 | 1.68 | - | 0.17 | 1.28 | - | 0.06 | 0.81 | 0.14 |
| Edge | 29.74 | 38.57 | 8.60 | 18.42 | 0.82 | 1.21 | - | 0.17 | 1.43 | - | 0.06 | 0.82 | 0.14 |

Table S2 | Area fractions of indexed phases within the EBSD fields of view in different regions of M632:1 (%).

| Phase Region | BaCuSi2O6 | BaPbSi2O6 | Ba2PbSSi2O10 | BaSi2O5 | Ba5Si8O21 | BaCa2Si3O9 | PbCO3 | BaSO4 | Unindexed |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Center | 35.27 | 22.25 | 5.36 | 2.82 | 3.13 | 3.01 | - | - | 28.16 |
| Transition | 38.80 | 12.20 | 6.07 | 0.31 | 1.15 | 2.21 | 2.17 | 3.65 | 33.44 |
| Edge | 29.62 | 26.68 | 8.72 | 0.31 | 0.91 | 3.07 | 2.91 | 1.35 | 26.43 |

Table S3 pXRF-determined oxide compositions of the central and marginal measurement areas of sample M632:1 (wt%)

| Oxide Region | Center |  |  | Edge |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 1 | 2 | 3 | 1 | 2 | 3 |
| MgO | 0.22 | 0.33 | 0.30 | 0.31 | 0.31 | 0.35 |
| Al2O3 | 1.51 | 1.43 | 1.49 | 1.88 | 1.87 | 1.90 |
| SiO2 | 26.49 | 26.56 | 26.44 | 25.25 | 25.29 | 25.11 |
| P2O5 | 0.08 | 0.08 | 0.08 | 0.15 | 0.15 | 0.15 |
| K2O | 0.19 | 0.19 | 0.20 | 0.13 | 0.13 | 0.13 |
| CaO | 1.06 | 1.07 | 1.06 | 0.98 | 0.99 | 0.98 |
| TiO2 | 0.22 | 0.27 | 0.25 | / | / | / |
| V2O5 | 0.34 | 0.34 | 0.37 | 0.33 | 0.34 | 0.35 |
| MnO | 0.14 | 0.14 | 0.15 | 0.13 | 0.14 | 0.13 |
| Fe2O3 | 0.70 | 0.71 | 0.70 | 0.81 | 0.82 | 0.82 |
| CoO | 0.06 | 0.06 | 0.06 | 0.05 | 0.04 | 0.04 |
| NiO | 0.02 | 0.02 | 0.02 | 0.03 | 0.03 | 0.02 |
| CuO | 6.02 | 6.03 | 6.06 | 6.71 | 6.70 | 6.74 |
| ZnO | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 | 0.04 |
| GeO2 | 0.03 | 0.02 | 0.02 | 0.02 | 0.02 | 0.02 |
| As2O3 | 0.10 | 0.10 | 0.09 | 0.10 | 0.10 | 0.10 |
| SrO | 0.21 | 0.21 | 0.21 | 0.20 | 0.19 | 0.20 |
| SnO2 | 0.04 | 0.04 | 0.04 | 0.12 | 0.12 | 0.12 |
| BaO | 34.45 | 34.29 | 34.37 | 34.03 | 33.90 | 34.03 |
| PbO | 28.08 | 28.05 | 28.06 | 28.73 | 28.81 | 28.77 |

Note: The transition zone was not measured independently because its width was smaller than the effective spot size of pXRF.

Table S4 Crystallographic parameters and identification evidence for the phases identified by EBSD in sample M632:1

| Phase | Crystal System | Laue Group | Space group No. | Unit-cell parameters |  |  |  |  |  | Representative EDS spectrum | Representative Kikuchi pattern |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | a / Å | b / Å | c / Å | α / ° | β / ° | γ / ° |  |  |
| BaCuSi2O6 | Tetragonal | 4/mmm | 119 | 7.04 | 7.04 | 11.13 | 90.00 | 90.00 | 90.00 |  |  |
| BaPbSi2O6 | Orthorhombic | mmm | 63 | 5.51 | 15.45 | 7.29 | 90.00 | 90.00 | 90.00 |  |  |
| Ba2PbSSi2O10 | Orthorhombic | mmm | 62 | 7.25 | 5.48 | 24.35 | 90.00 | 90.00 | 90.00 |  |  |
| BaSi2O5 | Orthorhombic | mmm | 62 | 4.63 | 7.69 | 13.51 | 90.00 | 90.00 | 90.00 |  |  |
| Ba5Si8O21 | Monoclinic | 2/m | 15 | 32.68 | 4.70 | 13.89 | 90.00 | 98.10 | 90.00 |  |  |
| BaCa2Si3O9 | Triclinic | -1 | 2 | 6.73 | 9.62 | 6.72 | 69.62 | 102.33 | 96.90 |  |  |
| PbCO3 | Orthorhombic | mmm | 62 | 5.18 | 8.49 | 6.14 | 90.00 | 90.00 | 90.00 |  |  |
| BaSO4 | Orthorhombic | mmm | 62 | 8.88 | 5.46 | 7.15 | 90.00 | 90.00 | 90.00 |  |  |