Supporting information

Synergistic adsorption of heavy metals by magnetic composite biochar: Performance and mechanisms in co‑contamination systems

Guiling Gao1, Haofeng Zhu1, Ping Wang2, Lei Hu3, Xuanyu Zhou3, Chenghao Wang1, Zhenyu Chen1, Zhenya Zhu1*

1 Hangzhou Polytechnic University, Hang Zhou,310018, P.R. China

2 Zhejiang Radiation Environment Monitoring Station (Technical Center for Radiation Environment Monitoring, Ministry of Ecology and Environment), Hangzhou, 310012, P. R. China.

3 Ecological and Environmental Monitoring Center of Zhejiang Province, Hangzhou 310012, P. R. China

*Corresponding author: Zhenya Zhu

E-Mail: dgjj1982@163.com

Address: Xueyuan Street No. 68, College of Chemical and Biological Engineering, Hangzhou Polytechnic University, Qiantang District, 310018 Hangzhou, P. R. China

Section S3.1 Adsorption kinetic study

To Investigate the adsorption kinetics of TC in the binary system, the related fitting parameters for pseudo-first-order and pseudo-second-order models were shown in Table S1. From the table, it can be seen that with the change in Pb(II) concentration, the correlation coefficients of the pseudo-second-order adsorption kinetics were all significantly higher than those of the pseudo-first-order model. This indicated that in binary system, the adsorption of TC was influenced by the coexisting Pb(II) , and the process involved both physical and chemical adsorption mechanisms.

The related kinetics fitting parameters of Pb(II) adsorption in binary system were shown in Table S2. As was shown, with different TC concentrations, the correlation coefficients of the pseudo-first-order adsorption kinetics were significantly higher than those of the pseudo-second-order adsorption kinetics, which indicated that the adsorption process was rapidly happend and mainly depended on the adsorption sites on the surface of the composite material.

Section S3.2 Equilibrium adsorption isotherms

The Langmuir and Freundlich isotherm models were taken to describe the adsorption isotherm processes of TC and Pb(II) in binary system. The calculated corresponding parameters were listed in Table S3 and Table S4, respectively. It can be seen that with different coexisting ion conditions, the Langmuir model relative coefficients (R2) of both TC and Pb(II) all exceeded 0.95, which were higher than those in Freundlich isotherm model. The adsorption isotherms data matched the Langmuir model better, indicating that the adsorption process may be monolayer chemical adsorption, which were highly favorable.

Table S1 Kinetic constants of the composites for TC adsorption (303 K)

| c(Pb（II）) (mg/L) | qe,exp (mg/g) | Pseudo first-order |  |  | Pseudo second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | q1,cal (mg/g) | k1 (1/min) | R2 | q2,cal (mg/g) | k2qe2 | R2 |
| 0 | 27.49 | 40 | 0.0864 | 0.9267 | 30.9756 | 0.0633 | 0.9539 |
| 5 | 32.81 | 54 | 0.1003 | 0.9228 | 35.8802 | 0.0582 | 0.9362 |
| 10 | 37.11 | 44 | 0.082 | 0.9373 | 40.1428 | 0.0514 | 0.9793 |
| 15 | 30.74 | 43 | 0.091 | 0.9509 | 31.4545 | 0.0641 | 0.9895 |
| 20 | 23.89 | 40 | 0.094 | 0.8577 | 22.4615 | 0.0726 | 0.9325 |
| 25 | 18.81 | 27 | 0.085 | 0.9057 | 20.4827 | 0.1034 | 0.9725 |
| 30 | 14.95 | 24 | 0.106 | 0.9245 | 13.2558 | 0.1272 | 0.9666 |

Table S2 Kinetic constants of the composites for Pb(II) adsorption (303 K)

| c(TC) (mg/L) | qe,exp (mg/g) | Pseudo first-order |  |  | Pseudo second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | q1,cal (mg/g) | k1 (1/min) | R2 | q2,cal (mg/g) | k2qe2 | R2 |
| 0 | 184.218 | 183.636 | 0.1506 | 0.9946 | 109 | 0.0938 | 0.8931 |
| 5 | 190.99 | 193.111 | 0.1289 | 0.9975 | 121 | 0.0689 | 0.9313 |
| 10 | 195.018 | 197.526 | 0.1332 | 0.9987 | 164 | 0.0553 | 0.9496 |
| 15 | 180.373 | 177.647 | 0.0982 | 0.9915 | 144 | 0.0949 | 0.9658 |
| 20 | 162.218 | 164.942 | 0.1028 | 0.9918 | 134 | 0.1027 | 0.9505 |
| 25 | 145.516 | 149.890 | 0.1279 | 0.9921 | 109 | 0.1238 | 0.9099 |
| 30 | 118.067 | 120.040 | 0.1336 | 0.9817 | 99 | 0.1476 | 0.8644 |

Table S3 Adsorption isotherm parameters of TC in binary system

| c(Pb（II）) (mg/L) | T(K) | Langmuir isotherm model |  |  |  | Freundlichisotherm model |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qm(mg/g) | KL(L/mg) | R2 |  | KF(mg/g) | n | R2 |  |
| 0 | 288.15 | 21.17 | 0.1531 | 0.9894 |  | 31.84 | 0.9878 | 0.8681 |  |
|  | 298.15 | 26.91 | 0.1834 | 0.9653 |  | 38.02 | 0.7404 | 0.9021 |  |
|  | 308.15 | 28.73 | 0.2279 | 0.9720 |  | 43.79 | 0.6609 | 0.9378 |  |
| 5 | 288.15 | 30.49 | 0.1784 | 0.9937 |  | 48.64 | 1.2721 | 0.8173 |  |
|  | 298.15 | 32.86 | 0.1917 | 0.9911 |  | 50.97 | 1.3619 | 0.8633 |  |
|  | 308.15 | 34.39 | 0.2052 | 0.9830 |  | 56.09 | 1.4732 | 0.8868 |  |
| 10 | 288.15 | 32.47 | 0.1931 | 0.9794 |  | 21.84 | 0.9878 | 0.8681 |  |
|  | 298.15 | 36.66 | 0.2134 | 0.9683 |  | 28.02 | 0.7404 | 0.9021 |  |
|  | 308.15 | 38.54 | 0.2489 | 0.9720 |  | 33.79 | 0.6609 | 0.9378 |  |
| 15 | 288.15 | 28.66 | 0.1883 | 0.9794 |  | 21.84 | 0.8878 | 0.7381 |  |
|  | 298.15 | 31.58 | 0.1992 | 0.9683 |  | 28.02 | 0.7324 | 0.7821 |  |
|  | 308.15 | 33.93 | 0.2117 | 0.9730 |  | 33.79 | 0.7009 | 0.8378 |  |
| 20 | 288.15 | 18.76 | 0.1583 | 0.9844 |  | 23.84 | 0.7378 | 0.8381 |  |
|  | 298.15 | 23.43 | 0.1472 | 0.9853 |  | 27.02 | 0.7114 | 0.8921 |  |
|  | 308.15 | 25.11 | 0.1327 | 0.9790 |  | 29.79 | 0.6709 | 0.7978 |  |
| 25 | 288.15 | 16.96 | 0.1483 | 0.9914 |  | 20.34 | 0.7178 | 0.7381 |  |
|  | 298.15 | 18.73 | 0.1412 | 0.9953 |  | 22.62 | 0.6714 | 0.7721 |  |
|  | 308.15 | 20.31 | 0.1387 | 0.9803 |  | 23.89 | 0.6309 | 0.8578 |  |
| 30 | 288.15 | 13.36 | 0.1513 | 0.9714 |  | 21.34 | 0.6948 | 0.7981 |  |
|  | 298.15 | 15.13 | 0.1402 | 0.9853 |  | 19.62 | 0.7714 | 0.7521 |  |
|  | 308.15 | 17.37 | 0.1357 | 0.9863 |  | 24.89 | 0.5909 | 0.6778 |  |

Table S4 Adsorption isotherm parameters of Pb in binary system

| c(Pb（II）) (mg/L) | T(K) | Langmuir isotherm model |  |  |  |  |  | Freundlichisotherm model |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | qm(mg/g) |  | KL(L/mg) |  | R2 |  | KF(mg/g) | n | R2 |  |
| 0 | 288.15 | 188.17 | 0.2351 |  | 0.9794 |  |  | 161.84 | 1.1278 | 0.8481 |  |
|  | 298.15 | 192.22 | 0.2734 |  | 0.9853 |  |  | 176.02 | 1.0504 | 0.8721 |  |
|  | 308.15 | 193.75 | 0.2979 |  | 0.9820 |  |  | 178.79 | 1.0009 | 0.8378 |  |
| 5 | 288.15 | 192.33 | 0.1984 |  | 0.9837 |  |  | 179.64 | 0.8721 | 0.8773 |  |
|  | 298.15 | 194.96 | 0.2217 |  | 0.9711 |  |  | 183.97 | 0.7619 | 0.8973 |  |
|  | 308.15 | 195.39 | 0.2452 |  | 0.9930 |  |  | 186.09 | 0.6732 | 0.8768 |  |
| 10 | 288.15 | 197.97 | 0.2231 |  | 0.9894 |  |  | 181.84 | 0.6678 | 0.8981 |  |
|  | 298.15 | 206.56 | 0.2634 |  | 0.9883 |  |  | 188.02 | 0.5404 | 0.9121 |  |
|  | 308.15 | 208.24 | 0.2789 |  | 0.9820 |  |  | 193.79 | 0.4609 | 0.9278 |  |
| 15 | 288.15 | 172.68 | 0.2383 |  | 0.9894 |  |  | 161.84 | 0.8968 | 0.8381 |  |
|  | 298.15 | 174.52 | 0.2592 |  | 0.9983 |  |  | 164.02 | 0.8324 | 0.8821 |  |
|  | 308.15 | 175.53 | 0.2617 |  | 0.9830 |  |  | 166.79 | 0.8109 | 0.9178 |  |
| 20 | 288.15 | 130.26 | 0.1983 |  | 0.9744 |  |  | 153.84 | 1.7378 | 0.8881 |  |
|  | 298.15 | 133.13 | 0.2172 |  | 0.9653 |  |  | 157.02 | 1.7114 | 0.8721 |  |
|  | 308.15 | 135.31 | 0.2327 |  | 0.9780 |  |  | 159.79 | 1.6709 | 0.8978 |  |
| 25 | 288.15 | 122.76 | 0.1883 |  | 0.9814 |  |  | 140.34 | 1.7578 | 0.8381 |  |
|  | 298.15 | 125.43 | 0.1912 |  | 0.9753 |  |  | 142.62 | 1.6314 | 0.8721 |  |
|  | 308.15 | 126.71 | 0.1987 |  | 0.9883 |  |  | 144.89 | 1.5509 | 0.8678 |  |
| 30 | 288.15 | 105.26 | 0.1913 |  | 0.9614 |  |  | 121.34 | 1.8948 | 0.8981 |  |
|  | 298.15 | 108.83 | 0.2402 |  | 0.9753 |  |  | 126.62 | 1.5714 | 0.9021 |  |
|  | 308.15 | 99.07 | 0.2573 |  | 0.9763 |  |  | 128.89 | 1.4909 | 0.9178 |  |