Electronic Supporting Information

A one-dimensional Cd(II) coordination polymer based on 2,5-dibromobenzene-1,4-dicarboxylate: Crystal structure and dielectric properties

Bakhtiyor Chori ugli Tursunov a, Yakubov Yuldash Yusupbaevich a, Khayit Khudaynazarovich Turaev b, A. Aditya Prasad c*, Abrorbek Khamidjanovich Ruzmetov a, Adkhamjon Sadullayevich Normamatov d,e, Avazbek Bakhtiyarovich Ibragimov d, Lutfullo Bozorov f, Sadridin Eshkaraev g, Aziz Bakhtiyarovich Ibragimov a,g*, Chellakarungu Balakrishnan a

a Institute of General and Inorganic Chemistry of Uzbekistan Academy of Sciences, 100170, Mirzo Ulug’bek str., 77a Tashkent, Uzbekistan.

b Department of Chemistry, Termez State University, 43 Barkamol Avlod Street, Termez-190111, Uzbekistan.

c Department of Chemistry, CMR Technical Campus, Kandlakoya, Medchal, Secunderabad - 501401, Telangana, India.

d Institute of Bioorganic Chemistry, Uzbekistan Academy of Sciences, Kh. Abdullaev Str., 83, Tashkent, 100143, Uzbekistan.

e Department of Chemistry, National University of Uzbekistan named after Mirzo Ulugbek, Tashkent 100174, Uzbekistan.

f Termiz State Pedagogical Institute, At-Termiziy Str., 191204, Termez, Uzbekistan.

g Department of Medicine, Termez University of Economics and Service, Surkhandarya, Termez, Farovon street 4-b,190111, Uzbekistan.

∗Corresponding authors: E-mail addresses: adityaaraveti@gmail.com (A. Aditya Prasad); aziz_ibragimov@mail.ru (Aziz Bakhtiyarovich Ibragimov).

*Address for correspondence

Dr. A. Aditya Prasad

Associate Professor

Department of Chemistry

CMR Technical Campus

Kompally, Medchal, Hyderabad - 500100, India.

Mobile No.: +91 94900 37019

E-mail address: adityaaraveti@gmail.com

Supplementary Figure Captions

| Fig. S1. | Crystal packing diagrams of the coordination polymer [Cd(Br2-BDC)(2-MeIm)2(DMF)]n viewed along the (a) bc, (b) ac, and (c) ab crystallographic planes. The structure exhibits a one-dimensional coordination chain constructed from Cd(II) centers interconnected by Br2BDC ligands, while 2-methylimidazole and DMF molecules complete the coordination environment. The CdO5N2 coordination polyhedra are shown in purple. hydrogen atoms are omitted for clarity. |
| --- | --- |
| Fig. S2. | Hirshfeld surface maps of (1) and (2) (a) dnorm (b) di (c) de and (d) curvedness |
| Fig. S3. | Percentages of molecular interactions represented as a 3D bar chart. |
| Fig. S4. | FT-IR spectra of complex [Cd(Br2-BDC)(2-MeIm)2(DMF)]n. |
| Fig. S5. | Raman spectra of complex [Cd(Br2-BDC)(2-MeIm)2(DMF)]n. |
| Fig. S6. | SEM images (top) and EDS spectrum (bottom) of compound [Cd(Br2-BDC)(2-MeIm)2(DMF)]n. |
| Fig. S7. | TG-DTA curves of complex [Cd(Br2-BDC)(2-MeIm)2(DMF)]n. |
| Table S1. | The selected bond lengths (Å), angles (°) and dihedral angles (°) of [Cd(Br2-BDC)₂(2-MeIm)2(DMF)]n. |

c

a

b

Fig. S1. Crystal packing diagrams of [Cd(Br2-BDC)(2-MeIm)2(DMF)]n viewed along the (a) bc, (b) ac, and (c) ab crystallographic planes. Hydrogen atoms are omitted for clarity.

c

b

Fig. S2 Hirshfeld surface maps of [Cd(Br2-BDC)(2-MeIm)2(DMF)]n: (a) de (b) di (c) dnorm and (d) fragment patch.

a

b

c

d

Fig. S3 Percentages of molecular interactions represented as a 3D bar chart.

Fig. S4 FT-IR spectrum of [Cd(Br2-BDC)(2-MeIm)2(DMF)]n.

Fig. S5 Raman spectrum of [[Cd(Br2-BDC)(2-MeIm)2(DMF)]n].

Fig. S6 SEM images (top) and EDS spectrum (bottom) of [Cd(Br2-BDC)(2-MeIm)2(DMF)]n

Fig. S7 TG-DTA curves of [Cd(Br2-BDC)2(2-MeIm)2(DMF)]n.

Table S1. Bond lengths [Å], angles and dihedral angles [°] for [Cd(Br2-BDC)2(2-MeIm)2(DMF)]n

| Bond | Length (Å) | Bond | Length (Å) |
| --- | --- | --- | --- |
| Cd1-O2 | 2.385(3) | C1-C3 | 1.393(5) |
| Cd1-O1 | 2.531(3) | C7-C5 | 1.398(6) |
| Cd1-O4 | 2.312(3) | C7-C6 | 1.385(6) |
| Cd1-O3 | 2.621(3) | N2-C11 | 1.341(6) |
| Cd1-N1 | 2.252(3) | N2-C10 | 1.361(7) |
| Cd1-N3 | 2.315(4) | N4-C15 | 1.340(6) |
| Cd1-O5 | 2.474(4) | N4-C14 | 1.352(6) |
| Br1-C2 | 1.898(4) | C5-C6 | 1.386(5) |
| Br2-C6 | 1.901(4) | C5-C8 | 1.502(5) |
| O2-C4 | 1.263(5) | C2-C3 | 1.377(5) |
| O1-C4 | 1.242(5) | O5-C19 | 1.191(7) |
| O4-C8 | 1.247(5) | N5-C19 | 1.327(7) |
| O3-C8 | 1.247(5) | N5-C18 | 1.454(8) |
| N1-C11 | 1.336(5) | N5-C17 | 1.446(7) |
| N1-C9 | 1.372(6) | C15-C16 | 1.479(6) |
| N3-C15 | 1.322(5) | C11-C12 | 1.480(7) |
| N3-C13 | 1.379(5) | C13-C14 | 1.330(7) |
| C1-C2 | 1.400(5) | C9-C10 | 1.350(7) |
| C1-C4 | 1.504(5) |  |  |
| Bond | Angle(°) | Bond | Angle(°) |
| O1-Cd1-O2 | 52.88(9) | C6-C7-C5 | 120.6(4) |
| O4-Cd1-O2 | 82.47(11) | C10-N2-C11 | 108.6(4) |
| O4-Cd1-O1 | 133.54(10) | C14-N4-C15 | 108.3(4) |
| O3-Cd1-O2 | 131.70(10) | C6-C5-C7 | 117.4(4) |
| O3-Cd1-O1 | 154.04(12) | C8-C5-C7 | 118.0(4) |
| O3-Cd1-O4 | 52.40(10) | C8-C5-C6 | 124.5(4) |
| N1-Cd1-O2 | 138.17(11) | C1-C2-Br1 | 121.6(3) |
| N1-Cd1-O1 | 85.30(11) | C3-C2-Br1 | 117.1(3) |
| N1-Cd1-O4 | 137.68(11) | C3-C2-C1 | 121.3(3) |
| N1-Cd1-O3 | 85.38(11) | C19-O5-Cd1 | 129.5(4) |
| N3-Cd1-O2 | 98.86(12) | O1-C4-O2 | 122.2(4) |
| N3-Cd1-O1 | 108.24(12) | C1-C4-O2 | 119.1(4) |
| N3-Cd1-O4 | 88.69(12) | C1-C4-O1 | 118.6(4) |
| N3-Cd1-O3 | 96.56(12) | C7-C6-Br2 | 116.8(3) |
| N3-Cd1-N1 | 94.10(13) | C5-C6-Br2 | 121.2(3) |
| O5-Cd1-O2 | 83.49(13) | C5-C6-C7 | 122.0(4) |
| O5-Cd1-O1 | 80.76(13) | C2-C3-C1 | 122.0(4) |
| O5-Cd1-O4 | 82.23(14) | C18-N5-C19 | 119.8(6) |
| O5-Cd1-O3 | 75.11(13) | C17-N5-C19 | 121.6(6) |
| O5-Cd1-N1 | 90.29(14) | C17-N5-C18 | 118.6(5) |
| O5-Cd1-N3 | 170.26(14) | O3-C8-O4 | 123.3(4) |
| C4-O2-Cd1 | 95.5(2) | C5-C8-O4 | 116.5(4) |
| C4-O1-Cd1 | 89.2(2) | C5-C8-O3 | 120.1(4) |
| C8-O4-Cd1 | 99.3(3) | N4-C15-N3 | 109.9(4) |
| C8-O3-Cd1 | 84.8(2) | C16-C15-N3 | 126.0(4) |
| C11-N1-Cd1 | 130.9(3) | C16-C15-N4 | 124.1(4) |
| C9-N1-Cd1 | 122.9(3) | N2-C11-N1 | 109.7(4) |
| C9-N1-C11 | 106.0(4) | C12-C11-N1 | 126.9(4) |
| C15-N3-Cd1 | 129.4(3) | C12-C11-N2 | 123.4(4) |
| C13-N3-Cd1 | 125.0(3) | C14-C13-N3 | 109.6(4) |
| C13-N3-C15 | 105.6(4) | C10-C9-N1 | 109.6(4) |
| C4-C1-C2 | 126.2(4) | C13-C14-N4 | 106.6(4) |
| C3-C1-C2 | 116.6(3) | C9-C10-N2 | 106.0(4) |
| C3-C1-C4 | 117.2(3) | N5-C19-O5 | 127.5(7) |
| Dihedral bond | Angle (°) | Dihedral bond | Angle (°) |
| Cd1-O2-C4-O1 | -6.0(3) | N1-C9-C10-N2 | -0.3(5) |
| Cd1-O2-C4-C1 | 169.3(2) | N3-C15-N4-C14 | -0.0(4) |
| Cd1-O1-C4-O2 | 5.6(3) | N3-C13-C14-N4 | 0.1(4) |
| Cd1-O1-C4-C1 | -169.68(19) | C1-C2-C3-C1 | -1.6(4) |
| Cd1-O4-C8-O3 | 3.0(3) | C7-C5-C6-C7 | 0.1(4) |
| Cd1-O4-C8-C5 | -176.2(2) | C7-C6-C5-C8 | 179.0(4) |
| Cd1-O3-C8-O4 | -2.6(3) | N2-C11-N1-C9 | -0.3(5) |
| Cd1-O3-C8-C5 | 176.58(18) | N4-C15-N3-C13 | 0.1(4) |
| Cd1-N1-C11-N2 | -175.7(4) | C5-C7-C6-C5 | -0.1(4) |
| Cd1-N1-C11-C12 | 5.2(5) | C2-C1-C3-C2 | -1.5(3) |
| Cd1-N1-C9-C10 | 176.2(4) | C2-C3-C1-C2 | 1.5(4) |
| Cd1-N3-C15-N4 | -179.8(4) | C2-C3-C1-C4 | -176.8(4) |
| Cd1-N3-C15-C16 | 2.0(5) | O5-C19-N5-C18 | -1.5(8) |
| Cd1-N3-C13-C14 | 179.7(4) | O5-C19-N5-C17 | 178.8(6) |
| Cd1-O5-C19-N5 | -123.8(5) | C4-C1-C2-C3 | -176.6(4) |
| Br1-C2-C1-C4 | 3.9(4) | C4-C1-C3-C2 | 176.8(4) |
| Br1-C2-C1-C3 | -178.0(3) | C6-C7-C5-C6 | 0.1(4) |
| Br1-C2-C3-C1 | 177.9(3) | C6-C7-C5-C8 | 179.1(4) |
| Br2-C6-C7-C5 | 178.3(3) | C6-C5-C7-C6 | -0.1(3) |
| Br2-C6-C5-C7 | -178.3(3) | C3-C1-C2-C3 | 1.5(3) |
| Br2-C6-C5-C8 | 0.6(4) | C8-C5-C7-C6 | -179.1(4) |
| O2-C4-C1-C2 | 40.0(5) | C15-N3-C13-C14 | -0.2(4) |
| O2-C4-C1-C3 | -138.1(4) | C15-N4-C14-C13 | -0.1(4) |
| O1-C4-C1-C2 | -144.6(4) | C11-N1-C9-C10 | 0.4(4) |
| O1-C4-C1-C3 | 37.3(5) | C11-N2-C10-C9 | 0.1(4) |
| O4-C8-C5-C7 | 48.2(4) | C13-N3-C15-C16 | -178.1(4) |
| O4-C8-C5-C6 | -130.7(4) | C9-N1-C11-C12 | -179.5(4) |
| O3-C8-C5-C7 | -131.0(4) | C12-C11-N2-C10 | 179.3(5) |
| O3-C8-C5-C6 | 50.1(5) | C14-N4-C15-C16 | 178.2(4) |