Supplemental Materials

S1. Materials and Chemicals

All chemical solvents and reactants used in this study were of analytical grade and used as received without purification. Concentrated nitric acid (HNO3, 65 – 68%), hydrogen peroxide (H2O2, ≥ 30.0 w.t.%), and methanol (MeOH) were used to modify biochars. Potassium dichromate (K2Cr2O7) was used for preparing the stock solutions of Cr(VI). Sodium hydroxide (NaOH) and hydrochloride acid (HCl, 36 % – 38 %) were used to adjust the pH in all solutions. All chemical solvents and reactants above and other chemicals employed in this experiment, including Na2CO3, NaHCO3, H2SO4, and H3PO4, were supplied by Sinopharm Chemical Reagent Co. Ltd., Shanghai, China. Milli-Q water (Millipore, 18.25 MΩ cm-1) was used throughout the whole study.

S2. Preparation of BCN-CH3OH and BCN-H2O2

The detailed procedures for the preparation of BCN-CH3OH were as follows [1]: each 1.0 g sample of BCN and 10 ml MeOH solution were mixed in a 50ml conical flask, which was then placed in a sonicator for 1 h. Afterward, the solid part was collected by using a vacuum suction filter, followed by washing with deionized water thoroughly to remove the remaining MeOH on the biochar particles, and finally dried in a vacuum oven at 60 °C for 24 h.

BCN-H2O2 was prepared as follows [2]: 10 g BCN was initially added into 50 mL 5 w t % H2O2 solution, mechanically shaking at a rate of 150 rpm at 55 °C for 24 h. After that, the suspension was treated under the same conditions above. The collected products were labeled as BCN-H2O2.

Fig. S1. Cr(VI) removal by NBC at different initial pH (the initial concentrations of NBC and Cr(VI) were 5 g L−1 and 50 mg L−1, respectively; 25 °C)

Fig. S2. (a) FTIR spectra; and (b) Ph–OH of BC and NBC (the bars are standard errors; letters in the figures indicate significant differences (P < 0.05)).

Fig. S3. Adsorption kinetics of Cr(VI) on NBC under (a)oxic and (b)anoxic conditions at different initial pH (Cr(VI) initial concentration 50 mg L−1, 25 °C)

Fig. S4. Removal efficiency of 50 mg L–1 Cr(VI) by BC and NBC under oxic conditions at different initial pH for 24 h, respectively (the bars are standard errors).

Table S1. The specific surface area, pore volume, pore size of BC and NBC.

| Samples | BET surface area (m2 g−1) | Pore volume (cm3 g−1) | Average pore size (nm) |
| --- | --- | --- | --- |
| BC | 4.8637 | 0.00975 | 21.435 |
| NBC | 27.066 | 0.02266 | 4.383 |

Table S2. Adsorption kinetics parameters for Cr(VI) adsorption by NBC under oxic and anoxic conditions at different pH values.

|  |  | Pseudo-first-order |  |  | Pseudo-second-order |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | k1 (h−1) | Qe (mg g−1) | R2 | k2 (g mg−1 h−1) | Qe (mg g−1) | R2 |
| oxic | pH=2 | 7.63×10–1 | 9.231 | 0.744 | 1.14×10–1 | 9.848 | 0.922 |
|  | pH=5 | 1.74×10–1 | 5.456 | 0.886 | 3.53×10–2 | 6.227 | 0.945 |
|  | pH=7 | 6.60×10–2 | 3.117 | 0.977 | 1.58×10–2 | 4.012 | 0.989 |
| anoxic | pH=2 | 6.85×10–1 | 9.128 | 0.751 | 1.01×10–1 | 9.778 | 0.921 |
|  | pH=5 | 1.45×10–1 | 5.055 | 0.939 | 2.89×10–2 | 5.913 | 0.970 |
|  | pH=7 | 3.00×10–2 | 3.882 | 0.997 | 3.58×10–3 | 5.907 | 0.997 |

References

[1] S. Zhu, X. Huang, X. Yang, P. Peng, Z. Li, C. Jin, Enhanced Transformation of Cr(VI) by Heterocyclic-N within Nitrogen-Doped Biochar: Impact of Surface Modulatory Persistent Free Radicals (PFRs), Environ Sci Technol, 54 (2020) 8123-8132.

[2] D. Zhong, Y. Jiang, Z. Zhao, L. Wang, J. Chen, S. Ren, Z. Liu, Y. Zhang, D.C.W. Tsang, J.C. Crittenden, pH Dependence of Arsenic Oxidation by Rice-Husk-Derived Biochar: Roles of Redox-Active Moieties, Environ Sci Technol, 53 (2019) 9034-9044.