ADDITIONAL FILE 2

Table S5.  Key FTIR absorption bands used for polymer identification in P. exilis microplastics.

| Polymer | Wavelength (cm-1) |  | Absorption |  | Reference |  |
| --- | --- | --- | --- | --- | --- | --- |
| PVC | 609.51 | C-CI |  | (Bayu et al. 2019) |  |
|  | 690.52 | C-CI |  |  |  |
|  | 960.55 | CH2 |  |  |  |
|  | 1095.57 | C-C |  |  |  |
|  | 1425.40 | CH2 |  | (Bredács et al. 2021) |  |
|  | 1726.29 | C=O (platicizer) |  | (Bredács et al. 2021) |  |
|  | 2853 | CH2 |  |  |  |
| PE | 720 | CH2 |  | (Bayu et al., 2019 |  |
|  | 1445 | CH2 |  |  |  |
|  | 2865 | CH2 |  |  |  |
|  | 2935 | CH2 |  |  |  |
| PET | 1093.64 | C-O |  | (Bredács et al. 2021) |  |
|  | 1241.09 | C-O |  | (Bayu et al. 2019) |  |
|  | 1504.48 | C=C Aromatic |  |  |  |
|  | 1712.79 | C=O |  |  |  |
|  | 720 | CH Aromatic |  |  |  |
|  | 3055.24 | C-O |  |  |  |

Source : Primary data, 2025

Table S5 presents a summary of the wavelength identification results along with the types of absorption detected in the P. exilis mussels sample. In polyvinyl chloride (PVC) polymers, which commonly contain chlorine atoms, a spectrum with strong absorption in the range of 609–690 cm⁻¹ is observed. This range is associated with the vibration of carbon-chlorine (C–Cl) bonds. Additional peaks at 1425–1726 cm⁻¹ indicate the presence of methylene (CH₂) and carbonyl (C=O) groups, suggesting the presence of plasticizers, additives that increase flexibility and are often found in vinyl chloride-based materials. Polyethylene (PE), a polymer composed of simple ethylene monomers, exhibited a simple pattern with firm peaks at 720, 1445, 2865, and 2935 cm⁻¹. These peaks are characteristic of methylene (CH₂) vibrations in straight aliphatic (non-aromatic, open chain) hydrocarbon chains. Meanwhile, polyethylene terephthalate (PET), an aromatic polyester, shows a more complex spectrum, with characteristic peaks from carbon-oxygen (C–O), carbonyl (C=O), and aromatic carbon-carbon (C=C) groups, confirming its identity as an aromatic polyester. This aligns with the literature (Bayu et al., 2019; Bredács et al., 2021), which supports the validity of the analysis results and confirms that these three polymers are the primary contaminants accumulated in mussels at the study site.

REFERENCE

Bayu A, Nandiyanto D, Oktiani R, Ragadhita R (2019) How to Read and Interpret FTIR Spectroscope of Organic Material. 97–118

Bredács M, Barretta C, Castillon LF, et al (2021) Prediction of polyethylene density from FTIR and Raman spectroscopy using multivariate data analysis. Polym Test 104:. https://doi.org/10.1016/j.polymertesting.2021.107406