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[bookmark: _Hlk207048766]Table 2. Total metal concentration for PTEs (mg Kg-1) at the study sites (the “La Concha” and “El Fraile” tailings, and the control zone) in Taxco, Guerrero.
	Site
	Sustrate
	Pb
	Zn
	Cu
	Fe
	Mn

	Tailing pond “La Concha”
	soil contaminated with mining waste (CS)
	14000
	40000
	60
	77500
	3250

	
	
	20000
	47500
	780
	75000
	3600

	
	
	19500
	24000
	575
	97500
	3100

	
	Tailing (CT)
	12000
	30000
	78000
	87500
	5000

	
	
	18000
	25000
	555
	380
	8250

	Tailing pond “El Fraile”
	soil contaminated with mining waste (FS)
	3700
	1000
	102
	62500
	280

	
	Tailing (FT)
	520
	9500
	111
	45000
	3150

	
	
	2800
	1200
	160
	55000
	310

	
	
	2000
	3900
	332
	55000
	3450

	Control Zone
	Soil
	70
	290
	575
	42500
	340

	
	
	100
	360
	50
	30000
	260

	
	
	70
	340
	60
	45000
	350

	phytotoxic levels (Alloway, 1995)
	100-400
	70-400
	60-125
	
	5000

	metalliferous soils (Reeves and Baker, 2000)
	3870-49910
	109-70480
	52-50900
	
	




