Supplementary Information

Quasi-One-Dimensional Sb2(S,Se)3 Self-Powered Photodetector for Diamond Fluorescence Magnetometry

Zhanpeng Zhang1, Jianpeng Li1,2,*, Yanjie Liu2, Xingjia Ren1, Jiabin Dong1, Hao Wang1, Zijun Zhang1, Qianqian Gao1, Yuxuan Luo2, Xiang Ren2, Li Wu3, Yan Shao2, Bo Zhang2,*, Xu Wu2,*, and Yi Zhang1,*

1Institute of Photoelectronic Thin Film Devices and Technology, State Key Laboratory of Photovoltaic Materials and Cells, Tianjin Key Laboratory of Thin Film Devices and Technology, and Engineering Research Center of Thin Film Optoelectronics Technology, Ministry of Education, Nankai University, Tianjin 300350, China.

2Key Laboratory of Advanced Optoelectronic Quantum Architecture and Measurement (MOE), School of Physics, Advanced Research Institute of Multidisciplinary Sciences, Beijing Institute of Technology, Beijing 100081, China.

3Key Laboratory of Weak-Light Nonlinear Photonics (MOE), School of Physics, Nankai University, Tianjin 300071, China.

This file includes:

Figures S1-S12

Supplementary Notes 1-3

Supplementary Figures

Figure S1. Schematic illustration of the temperature-dependent precursor release and Sb2(S,Se)3 film formation during hydrothermal growth. At 105 °C, the slow release of S, Se, and Sb precursors leads to insufficient nucleation of the absorber film, resulting in incomplete surface coverage. At 135 °C, a balanced release of S, Se, and Sb precursors promotes the formation of a dense and continuous film. At 165 °C, the release becomes excessively rapid, causing disordered nucleation and leading to a rough film with poor uniformity.

Figure S2. Photos of solution-state conditions for temperature-regulated hydrothermal growth. a-c, the pH and temperature meter readings for precursor solutions corresponding to Samples A (a), B (b), and C (c), documenting the growth conditions at 105, 135 and 165 °C.

Figure S3. Atomic Force Microscope images of Sb2(S,Se)3 films prepared at different hydrothermal temperatures. a-c, Surface height images of Samples A, B, and C. The root-mean-square roughness values are 31.2 nm, 26.0 nm, and 299.3 nm, respectively.

Figure S4. XRD patterns of Sb2(S,Se)3 films in the 20-45 degree range, corresponding to Samples A, B and C, respectively. The marked diffraction peaks are assigned to the FTO substrate.

Figure S5. Magnified XRD patterns of Samples A, B and C in selected diffraction regions. The highlighted regions show the evolution of the characteristic (020), (120), (130) and (211) reflections relative to the Sb2Se3 and Sb2S3 reference positions.

Figure S6. The absorption spectrum (a) and the plots of (h2 versus h with corresponding fitting curves (b) of the Sb2(S,Se)3 film. The direct bandgap of Samples A, B and C are 1.19, 1.29 and 1.38 eV, respectively.

Figure S7. The ultraviolet photo-electron spectroscopy (UPS) curves of the Sb2(S,Se)3 films showing the valence band maximum (VBM, a) and the secondary electron cut-off (SEC) edge (b), corresponding to Samples A, B and C, respectively.

Figure S8. Energy-level diagram of CdS/Sb2(S,Se)3/Spiro-OMeTAD hetero-structures[1].

Figure S9. Temporal photoresponse J-T curves of the Devices A, B and C. The measurements were taken under 645 nm illumination with 2 mW·cm-2 for 10000 s. The step of each laser pulse is 10 s.

Figure S10. The time-domain waveforms of the dark current for the Devices A, B and C, respectively.

Figure S11. The measurement photograph of the nitrogen vacancy (NV) centers in diamond used for fluorescence detection. The setup integrates the excitation/collection optics, filter module and photodetector readout path.

Figure S12. Demodulated optically detected magnetic resonance (ODMR) spectra obtained using 532 nm excitation wavelength. The fitted slopes of the commercial photodetector are 5.65 × 10-3 and 5.27 × 10-3 V·GHz-1, respectively.

Supplementary Notes

Supplementary Note S1. Deposition Mechanism of Sb2(S,Se)3 from Na2SeSO3 and Na2S2O3

1. Reactants: Potassium antimony tartrate, sodium thiosulfate, sodium selenosulfate and water

2. Analysis of the reaction conditions:

Sodium selenosulfate is more reactive and can be converted completely at a lower temperature and within a shorter reaction time to form Sb2Se3. By contrast, sodium thiosulfate is less reactive and requires a higher temperature and longer reaction time. Preferential decomposition of sodium selenosulfate therefore causes Sb2Se3 to deposit first. As sodium selenosulfate is consumed, decomposition of sodium thiosulfate becomes dominant, leading sequentially to the deposition of Sb2(S,Se)3 and Sb2S3. The as-deposited precursor film consequently contains an Sb2Se3/Sb2(S,Se)3/Sb2S3 compositional gradient and a corresponding graded bandgap that persists after annealing. This band alignment may facilitate electron extraction and transport but may impede hole transport.

3. Mechanistic analysis:

K2Sb2(C4H2O6)2 + 2H2O = 2K+ + 2SbO+ + 2C4H2O62-

∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙(The aqueous solution is acidic)

Na2SO3 + H2O = NaHSO3 + NaOH

∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙(Origin of the alkaline solution)

SbO+ + OH− + H2O = Sb(OH)3 ↓

∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙(White precipitate, dissolves at high temperature)

S2O32− + H2O = S2− + SO32− + 2H+

∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙(Rate-limiting step; requires a higher temperature)

SeSO32− + H2O = Se2− + SO32− + 2H+

∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙∙(Rate-limiting step; proceeds at a lower temperature)

K2Sb2(C4H2O6)2 + 3Na2S2O3 + 3H2O = 3Na2SO4 + K2C4H4O6 + C4H6O6 +Sb2S3 ↓

∙∙∙∙∙∙∙∙∙∙(Amorphous red precipitate; rate-limiting step; requires a higher temperature; the solution becomes more acidic after reaction)

K2Sb2(C4H2O6)2 + 3Na2SeSO3 + 3H2O = 3Na2SO4 + K2C4H4O6 + C4H6O6+Sb2Se3 ↓

∙∙∙∙(Amorphous reddish-brown precipitate; rate-limiting step; proceeds at a lower temperature; the solution becomes more acidic after reaction. )

𝑥Sb2S3 + 𝑦Sb2Se3 = Sb2(S𝑥, Se𝑦)3	 (x + y = 1)

Supplementary Note S2. Band alignment of Sample A, Sample B, and Sample C thin films.

Ultraviolet photoelectron spectroscopy (UPS) was carried out to measure the band alignment of thin films. According to the secondary electron cut-off (Ecut-off) edge and valence band (VB) position, the Fermi level (EF), the valence band (EV), and the conduction band (EC) can be determined based on the equations:

EF=Ecut-off-hv	(1)

EV=EF-VB	(2)

EC=EV+Eg	(3)

where hv is the excitation energy in the ultraviolet regime, i.e., HeI, hv= 21.22 eV, and Eg is the bandgap. The calculated EC/EF/EV levels of Sample A, Sample B, and Sample C are -4.25 eV/-4.73 eV/-5.44 eV, -3.96 eV/-4.48 eV/-5.25 eV, and -4.11 eV/-4.63 eV/-5.49 eV, respectively.

Supplementary Note S3. NV readout and magnetic sensitivity.

The lock-in output was recorded while the microwave frequency was swept across the ODMR transition. The slopes obtained by fitting the steepest regions on both sides of the resonance were used to convert ODMR frequency shifts into changes in the electrical readout signal. Magnetic sensitivity was then compared between the laboratory-built PD and the commercial PD under the same optical and electronic readout configuration.

Reference

[1]	Dong, J. et al. Carrier management through electrode and electron-selective layer engineering for 10.70% efficiency antimony selenosulfide solar cells. Nature Energy.  10, 857-868 (2025).